## Slide 1: Nuclear Fuel Performance
NE 533: Spring 2024

## Slide 2: Last Time
All reactors have basic requirements they must meet
Typically, the “fuel system” is thought to consist of the fuel itself, the gap, the cladding, and the coolant
Mining -> Processing -> Conversion -> Enrichment -> Powder -> Compaction/Sintering -> Rod/Assembly
U3O8 must be converted to UF6 for enrichment, which is then converted to UO2 powder for pellet manufacture
UO2 microstructure from fabrication strongly impacts fuel performance
Heat generation rate: Q = Ef x Nf x sf x f

## Slide 3: heat transport

## Slide 4: Heat transport route
Heat is produced in the fuel, transports through the cladding and gap, and into the coolant
Important quantities include
  Volumetric heat generation rate Q (W/cm3)
  Fuel Centerline temperature T0
  Surface temperature of the fuel TS
  Inner cladding temperature TCI
  Outer cladding temperature TCO
  Coolant temperature Tcool
  Fuel pellet radius rF
  Gap thickness tG
  Cladding thickness tc
  Coolant heat transfer hc

## Slide 5: Heat can be transported in three ways
Convection
  Heat transfer through mass movement of liquid or gas
Radiation
  Heat transfer by means of photons in electromagnetic waves
Conduction
  Heat transfer by molecular, phonon, and electronic vibration/collisions

## Slide 6: Heat transfer mode in fuel systems?
How is heat transported through the fuel?
  Conduction
How is the heat transported through the gap?
  Mostly conduction, some convection
How is heat transported through the cladding?
  Conduction
How is heat transported to the coolant?
  Convection

## Slide 7: Heat conduction equation
ρ is the density, cp is the specific heat, T is the temperature, t is the time, and k is the thermal conductivity, Q is heat generation
It is a partial differential equation in time and space of the temperature, T(x, t), where x is a vector defining the position in space
What do we need to know to solve this equation?
The geometry of our problem
The initial condition of T
The boundary conditions of T
Is each parameter is a function of T
If they aren’t a function of T, do they vary in space and time for some other reason?

## Slide 8: What is our geometry for the problem?
Reactor geometry depends on reactor type
The ideal geometry of each fuel rod is axisymmetric, but in reality, it is 3D
Fuel pellet defects cause 3D geometry
The stacked pellets may not be stacked perfectly, causing their center axis to not be aligned, also causing 3D geometry

## Slide 9: The initial condition of T
The initial condition of T is set by the state of the reactor directly before startup (or before time of interest)
The initial temperature is uniform throughout the fuel, equal to the initial coolant temperature
T(x, 0) = Tcool(0)

## Slide 10: Boundary conditions?
The boundary conditions on T is set by the coolant flow
The temperature of the coolant Tcool is complicated
  It varies along the length of the fuel rod (axially)
  It various around the circumference of the fuel rod

## Slide 11: Fuel properties
All properties vary as a function of composition, thus as a function of burnup/time
Density varies as a function of T (thermal expansion)
Thermal conductivity also varies with temperature

## Slide 12: The heat capacity is a function of temperature
θ = 548.68,
C2 = 2.285 × 10-3
C3 = 2.360 × 107
Ea = 18531.7

## Slide 13: The heat generation rate is a function of the thermal neutron flux, which varies in time and space
Q = Ef Nf σf ϕth

## Slide 14: Analytical solve of heat conduction

## Slide 15: The most accurate solution is numerical, in 3D, requires modeling the entire core, and is multi-physics
Solution is 3D and changes in time
All the properties are functions of temperature
The boundary conditions comes from information about the coolant flow
The heat generation rate comes from information about the neutronics in the reactor
No analytical solution is possible

## Slide 16: In order to solve, make assumptions!
#1: steady state ->
#2: cylindrical, axisymmetric ->
#3: constant in z
#4: constant thermal conductivity, volume heat

## Slide 17: Directly Solving for Temperature Profile
Boundary conditions: r0 = 0, r1=R, T’(0) = 0, T(R) = Ts
r0
r1

## Slide 18: Linear Heat Rate
  Where Qav is the radially averaged heat generation rate in W/cm3
  LHR is in units of power per unit length: W/cm
Substitute LHR into previous equation on T0-Ts

## Slide 19: Alternate Geometries
Similar derivation with appropriate boundary conditions can be applied to plate and sphere geometries
Plate
x is the distance from the midplane of the fuel and tf is the plate fuel thickness
Sphere
r is the distance from the sphere center and Rf is the radius of the sphere

## Slide 20: Heat transport through the gap
Heat flux is a conserved quantity, described by Fourier’s first and second laws:
If there are no sources of heat, as if the case in the cladding and gap, the temperature field is constant with time and heat flux is unidirectional
For boundary conditions T1 and T2 and a thickness d
This assumes a spatially constant thermal conductivity, consistent with a “thin slab”
l = thermal cond.

## Slide 21: Heat transport through the gap
The heat flux gives the rate, per unit area, at which heat flows in a given direction
The heat flux from the fuel is the LHR/pellet circumference
Heat flux from the fuel is the same as heat flux through the the gap – can make this assumption because Rf >> tg
Gap thickness = RIC-Rf = tg
Cladding thickness = ROC-RIC = tc
R0=0
R1=Rf
R2=RIC
R3=ROC

## Slide 22: Heat transport through the gap
Set heat flux fuel/gap equal
Gap conductance is defined as:
Gap conductance depends on the gas filling the gap
  For pure He, kgap=16x10-6 * T0.79 (W/cm-K)
  For pure Xe, kgap=0.7x10-6 * T0.79 (W/cm-K)
  Simple mixing rule: kgap = kHe(1-y) + kXey
    Where y is the mole/atom fraction of Xe
=

## Slide 23: Heat transport through the cladding
Heat flux through the cladding
Set equal your heat fluxes

## Slide 24: Heat transfer to the coolant
Heat is transported from the cladding to the coolant via convection
Tcool is the coolant temperature, hcool is the convective heat transfer coefficient between cladding wall and coolant
Adding gap + cladding + coolant:
+

## Slide 25: Summary of analytical solutions

## Slide 26: Solving for the temperature profile
You solve for the transition temperatures
Start from the coolant and work inward
Have a linear profile everywhere except in the fuel
Finally, solve for the temperature profile throughout the fuel
  TCO TCI
Tcool

## Slide 27: Fuel and Cladding Thermal Properties
Material | Density (g/cm3) | Heat Capacity Cp (J/g-K) | Thermal Conductivity k (W/cm-K) | Thermal Expansion Coefficient a (K-1)
UO2 | 10.98 | 0.33 | 0.03 | 1.2 x 10-5
Zr | 6.5 | 0.35 | 0.17 | 1.0 x 10-5
Stainless steel | 8.0 | 0.5 | 0.17 | 9.6 x 10-6

## Slide 28: Example Problem

## Slide 29: Temperature profile calculation example
Tcool = 580 K; LHR = 200 W/cm; hcool = 2.65 W/cm2-K
Rfuel = 0.5 cm; tclad = 0.06 cm; tgap = 0.003 cm; kf=0.03 W/cm-K
Work from outside->in, calculate cladding temperature
  Tco = (200)/(2*pi*0.5*2.65) + 580
  Tco = 604 K
Calculate inner cladding temp
Tci = (200*0.06)/(2*pi*0.5*0.17) + 604
Tci = 626 K

## Slide 30: Temperature profile calculation example
Calculate fuel surface temperature
Calculate gap conductance
  gap with He; kgap=16x10-6 * T0.79 (W/cm-k) ; assume Tci is appropriate for entire gap; kgap = 0.0026 W/cm-K; tgap = 0.003 cm
  hgap = 0.87 W/cm2-K
Tfuel = 200/(2*pi*0.5*0.87) + 626
Tfuel = 699 K

## Slide 31: Temperature profile calculation example
Calculate centerline temperature
T0 = 200/(4*pi*0.03) + 699
T0 = 1230 K
Full temperature profile

## Slide 32: Temperature profile calculation example
Parabolic temperature profile in fuel
Linear in gap and clad
Steep temperature drop over gap, very low thermal conductivity
Smaller temperature drop over cladding

## Slide 33: Temperature profile modification
Instead of pure He gap, 30% of gas is Xe; how is T0 affected?
First, how is gap conductance affected?
Gap conductance depends on the gas filling the gap
  For pure He, kgap=16x10-6 * T0.79 (W/cm-K)
  For pure Xe, kgap=0.7x10-6 * T0.79 (W/cm-K)
  Simple mixing rule: kgap = kHe(1-y) + kXey
  TCI, TCO, and Tcool is unchanged from previous example, also T0-Tfuel is unchanged
  kgap = ((16x10-6)*(626)0.79 )(1-0.3) + ((0.7x10-6)*(626)0.79 )(0.3) = 1.85E-3 W/cm-K

## Slide 34: Temperature profile modification
kgap = 1.85E-3 W/cm-K
hgap = 1.85E-3 / 0.003 = 0.62 W/cm2-K
Tfuel = 200/(2*pi*0.5*0.62) + 626 = 729 K
T0 – Tfuel = 530.5 K (unchanged from before)
T0 = 729 + 530.5 = 1259.5 K
Increase in T0 of 30 K
Caveat: linear mixing of gases is not the best approach

## Slide 35: Neutron flux varies axially, so does LHR
Taking a fuel rod with length, L = 2*Z0
LHR0 is the midpoint linear heat rate, i.e. @ z=Z0
, where Zex is the extrapolation distance
A typical value is 1.3; can reduce p/2g to 1.2

## Slide 36: Coolant temperature varies with Z
Each rod has a given flow area
Mass flow rate:
Coolant specific heat:

## Slide 37: Calculate LHR and Tcool with axial variation
mdot = 0.25 kg/s-rod; Z0 = 150 cm; LHR0 = 150 W/cm; CPW = 4200 J/kg-K; Tin= 570 K

## Slide 38: Summary
Developed analytical expressions for the temperature profile within a fuel rod
Required to make four assumptions:
  Steady-state solution
  Temperature is axisymmetric
  T is constant in Z
  Thermal conductivity is independent of temperature
Temperature profile in the fuel is parabolic, assume linear profiles in gap, clad and coolant
Can incorporate axial variation in Tcool with axial variation in LHR