## Slide 1: Nuclear Fuel Performance
NE-591-010
Spring 2021

## Slide 2: Last Time
Metal fuel can go to high burnup, good accident performance, inherent safety, easy to make
Complex phase and composition environment
Rapid, substantial swelling, followed by fission gas release
Fission gas bubble behavior is very phase dependent
Observe constituent redistribution radially, in addition to axially varying microstructure
FCCI is a major factor in cladding failure, dependent upon thermodynamics and kinetics of a number of lanthanides, actinides and transition metals

## Slide 3: Notes on MOOSE Project
You have the freedom to modify your mesh, and can veer from the 100x100 specification, changing mesh densities
This was to serve mostly as a rough guide for the level of fineness that I would like to see you implement
For your report, a full introduction and motivation to the problems is not necessary
I am looking for your understanding of what MOOSE is doing, why you are doing what you are doing (with MOOSE), what reasonable materials properties are, and what reasonable behavior is supposed to be
  the basics of utilizing (in an informed manner) a fuel performance code

## Slide 4: Mechanistic Fuel Performance Modeling
NE 591

## Slide 5: Multiscale Modeling
Modeling and simulation is the essential bridge from good science to good engineering, spanning from fundamental understanding of materials behavior to deliberate design of new materials technologies leveraging new properties and processes
Lower length scale modeling can provide insight, properties, mechanisms, behaviors, etc., that can be input into higher length scale modeling tools to describe, mechanistically, macroscale behavior

## Slide 6: Density Functional Theory
DFT is a computational quantum mechanical modelling method used to investigate the electronic structure of many-body systems, in particular atoms, molecules, and the condensed phases
DFT is primarily utilized to investigate electronic structure, cohesive energy, elastic constants, phonons, entropies, etc.

## Slide 7: Molecular Dynamics
MD is a computer simulation method for analyzing the physical movements of atoms and molecules, determined by numerically solving Newton's equations of motion for a system of interacting particles
MD is still atomistic, and is often utilized to calculate transport properties, melting temperature, clustering, etc., that are properties just beyond DFT capabilities

## Slide 8: Rate Theory/Cluster Dynamics
Provides recipes for calculating reaction rates between individual species of the types which are ubiquitous in chemistry and physics
Is typically a mean-field approach which uses transition state theory as a tool for describing reactions involving radiation-produced defects
Can be utilized to describe clustering, absorption, emission, growth, resolution, etc. to describe microstructural phenomena on an intermediate time scale

## Slide 9: Phase-Field
PF is mathematical model for solving interfacial problems that substitutes boundary conditions at the interface by a partial differential equation for the evolution of an auxiliary field (the phase field) that takes the role of an order parameter
The order parameter takes two distinct values (for instance 1 and 0) in each of the phases, with a smooth change between both values in the zone around the interface, which is then diffuse with a finite width
PF is commonly used for grain growth, phase separation, bubble coalescence, recrystallization, etc.

## Slide 10: Going beyond burnup…
Operating Conditions
Variables
Elasticity tensor
Fracture stress
Melting temperature
Fuel Property values
Dimensional change
Thermal conductivity
Elasticity tensor
Thermal conductivity
Failure criteria
Cladding
Property values
Dimensional change
Yield stress
Gap conductance
Gap pressure
Diffusion constants
Neutron flux
Temperature
Displacement
Coolant T&P
Burn-up
Fuel performance codes historically rely on materials models correlated to temperature and burn-up
Development has begun on models based on microstructure rather than burn-up

## Slide 11: Microstructure-based fuel performance modeling
Operating Conditions
Neutron flux
Variables
Temperature
Displacement
Stoichiometry
Coolant T&P
Fuel
Microstructure variables
Average grain size
Dislocation density
U defect concentrations
Pu concentration
Fission product precipitate fractions
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Crack parameter
Cladding
Microstructure variables
Average grain size
Dislocation density
H concentration
Hydride fraction
Point defect concentrations
Loop density
2nd phase particle fraction
Gap variable
Gap fission gas concentration
Grain growth
Defect prod. & transport
Fission gas behavior
Densification
Microstructure evolution models
Plasticity
Grain growth
Defect prod. & transport
Hydrogen transport
Microstructure evolution models
Loop evolution
Plasticity
Fracture
Structure/property relationships connect the microstructure variables to the property values
Elasticity tensor
Thermal conductivity
Failure criteria
Dimensional change
Yield stress
Cladding
Property values
Elasticity tensor
Fracture stress
Melting temperature
Dimensional change
Thermal conductivity
Diffusion constants
Fuel Property values

## Slide 12: Example: fission gas behavior in the fuel
Take into account a finite set of variables to describe the state of the material
Utilize a mechanistic model of fission gas behavior to predict the evolution of the microstructure
Utilize this updated microstructure to inform a number of structure/property relationships
Model of fission gas behavior
Variables
Temperature
Displacement
Stoichiometry
Structure/property relationships
Elasticity tensor
Fracture stress
Dimensional change
Thermal conductivity
Gap conductance
Gap pressure
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Gap fission gas concentration

## Slide 13: Multiscale separate effects experiments and simulations inform the development of the models
nm
μm
mm

## Slide 14: Microstructure-based models
Can provide a structure/property relationship to replace the existing burnup dependent model
For example, thermal conductivity, taking into account microstructural features and their evolution
Bulk conductivity
Fission gas
Intragranular porosity
Grain boundary and bubbles
κpr
Precipitated fission products
Vacancies and interstitials

## Slide 15: Parametrizing the mechanistic model
We employ multiscale modeling and simulation to determine the various parameters for the model
MD simulations conducted at LANL have been used to determine the coefficients for various point defects
MD simulations have shown that phonon scattering must be accounted for to accurately represent small bubbles
Mesoscale simulations have shown that GB bubbles have a larger impact on the thermal conductivity
Maxwell-Eucken (no phonon scattering)

## Slide 16: Parametrizing the mechanistic model
A thermal resistor model is created to describe the impact of GB bubbles on the thermal conductivity
MARMOT simulations are currently being used to inform the development of the precipitate multiplier

## Slide 17: Parametrizing the mechanistic model
Each term in the expression must be coupled to a corresponding state variable
The full model calculates the thermal conductivity as a function of:
  Temperature
  Point defect concentrations
  Intragranular bubble density and average radius
  Fractional coverage of bubbles on GBs and average radius
  Precipitate volume fractions and average sizes
Currently effects of precipitates fission products and individual point defects are neglected in the model, as they are not tracked or predicted in BISON

## Slide 18: Comparing with experiments…
The model under-predicts the temperature in most cases, but not all
Thus, the model is neglecting some resistive effects from the microstructure
But generally performs as well, and in some cases better, than the burnup based model
RISO-3 AN3
RISO-3 AN4
RISO II-3
US PWR TSQ0002

## Slide 19: UZr Fuel Performance Modeling
Development of a quantitative phase-field model of macroscale constituent redistribution in the U-Zr system, where model parameters were optimized and the model validated against an independent data set
Calculation of surface tension based on molecular dynamics, which is used in the BISON gaseous metallic fuel swelling model

## Slide 20: U3Si2 Fuel Performance Modeling
Point Defect Diffusion, Fission gas swelling, thermal and irradiation creep

## Slide 21: TRISO Particle Fuel Performance Modeling
TRISO particle modeling is still under development from a mechanistic model standpoint
Imperfect data for many critical fission products through different layers
Data typically for UO2 only, not for UC or UCO fuel kernels

## Slide 22: Summary
Researchers are working to develop materials models for the fuel and cladding that are mechanistic rather than empirical and that are based on the evolution of the microstructure rather than the burnup.