## Slide 1: Nuclear Fuel Performance
NE 591-010

## Slide 2: Last Time
Basics of what fuel performance means
  Transfer of heat to the coolant
  Operation without outages
  Performance during off-normal scenarios
Intro to Nuclear Fuels
  Considerations for fuels
  Why not pure U?
  Basics of UO2

## Slide 3: Fuel types continued

## Slide 4: Mixed Oxides (MOX)
Can be combined with PuO2 for a mixed oxide (MOX) fuel for use in fast reactors
Allows to burn excess weapons grade plutonium
About 30 reactors in Europe currently utilize a partial MOX core
Similar behavior to UO2, but different neutronics, fission gas release, thermal conductivity, etc.
Less common is inclusion of minor actinides in MOX to burn waste

## Slide 5: Accident Tolerant Fuel/Advanced Technology Fuel
Kept the acronym, changed the concept
USi fuels (U3Si2)
  A metal-ish compound, with higher thermal conductivity, higher uranium density
  Complex crystal structure (10 atoms unit cell) with effectively two sub-lattices
  Amorphizes at low temperatures
  Poor oxidation resistance
  Will require improved cladding, liners/coatings or fuel dopants

## Slide 6: Accident Tolerant Fuel/Advanced Technology Fuel
Cr-doped UO2
  Larger grain size, theoretically reduced fission gas release
  Cr changes the O potential present within the fuel, changing defect concentrations and mobilities
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 7: Uranium-Zirconium (UZr)
Utilized in sodium cooled fast reactors (SFRs)
  EBR I, EBR II
Varied crystal structure and compositional environment
Easily alloyed with Pu, minor actinides (MA)
Can function as a breeder/burner fuel
Sodium coolant
Fe-based cladding

## Slide 8: Uranium-Zirconium (UZr)
Alloy metallic U with Zr to increase the melting point and to stabilize the high temperature body-centered cubic phase
Interesting phenomena
  30-50% swelling
  Constituent redistribution
  Alpha tearing
  FCCI

## Slide 9: Uranium-Zirconium (UZr)
Good Characteristics
  High thermal conductivity
  Stability to high burnups (> 20%)
  Flexible composition
  Inherent safety- negative reactivity feedback
  Good compatibility with Na coolant
Bad Characteristics
  Low melting point
  Dramatic fuel swelling that must be accounted for
  Incredibly complex microstructures/unpredictable behavior
  Fuel-Clad Chemical Interaction
  Very easily oxidized

## Slide 10: Uranium-Molybdenum (UMo)
New fuel being qualified for research reactors
Fuel foil, with Zr diffusion barrier, Al cladding
Will be utilized in ATR, NBSR, MITR, MURR

## Slide 11: Uranium-Molybdenum (UMo)
Microstructural phenomena of interest:
  Decomposition
  Fission Gas Superlattice
  Recrystallization
  Inter-diffusion region
  Carbides

## Slide 12: UC/UCO TRISO Fuels
TRISO: TRistructural ISOtropic particle fuel
Layered fuel in mm-sized particles
Layers:
  Fuel Kernel
  Buffer
  Inner Pyrolitic Carbon (IPyC)
  SiC
  Outer Pyrolitic Carbon (OPyC)

## Slide 13: UC/UCO TRISO Fuels
Can appear as UC, U2C3, or UC2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Rapidly corrodes in water
  Reacts with some cladding

## Slide 14: UC/UCO TRISO Fuels
High temperature gas reactors (HTGR) or molten salt reactors (MSRs)
Pebble bed and prismatic types
Particles are agglomerated with graphite into a larger pebble, or into a cylindrical block
Current designs utilize UCO, which is a heterogeneous mixture of UO2 and UC fuel
Helium cooled gas or molten salt cooled

## Slide 15: UC/UCO TRISO Fuels
Each individual pebble acts as its own containment, and allows fuels to go to much higher burnups and higher temperatures than UO2
Highly reliant on accurate fabrication processes that create high integrity, uniform layers and spherical particles
Integrity of the SiC is key for fission product retention

## Slide 16: UN – Lead Cooled Reactors
Can appear as UN, U2N3, or UN2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Corrodes in water
  Reacts with some cladding
  Difficult to manufacture
  Requires N-enrichment

## Slide 17: Stable Salt Reactor
Utilizes fuel that is dissolved in molten salts
  NaCl-(U/Pu)Cl3
  Liquid fuel is contained in rods/assemblies
  Molten salt coolant (NaF-ZrF, FLiBe, FLiNaK, etc.)
Can mix other actinides into the fuel in order to burn waste
Designed to be inherently safe
Molten salt corrosion is a big problem, as well as the lack of information on thermophysical properties of complex salt

## Slide 18: Unique Fuel Designs
Lightbridge
  High Zr content UZr alloy
  Cruciform geometry fuel rods, combined into fuel elements
Kairos
  TRISO particle compacts with low density core
  Float in molten salt coolant for online refueling
NASA/LANL
  UMo fuel for space reactors: KRUSTY

## Slide 19: Fuel Summary Table
Property | UZr | UO2 | UC | UN | U3Si2
Corrosion resistance in water | Very poor | Excellent | Very poor | Poor | Poor
Compatibility with clad materials | Reacts with normal clad | Excellent | Variable | Variable | Variable
Thermal stability | Phase change at 665 and 770 °C | Good | Good | Good | Good
Uranium (metal) density (g/cm3) | 19.04 | 9.65 | 12.97 | 13.52 | 11.31
Melting point (°C) | 1132 | 2865 | 2850 | 2860 | 1665
Thermal conductivity (W/m-K) | 38 at 430 °C | 3 at 1000°C | 25 at 500°C | 20 at 750°C | 23 at 773°C

## Slide 20: Fuel Types Summary
There exist a number of nuclear fuels in different stages of utilization and development
Each reactor design or application has individual needs, and no one fuel is one size fits all
Need to balance safety, performance (normal, off-normal, extended), manufacturability, processing, waste, etc.

## Slide 21: Questions/Comments/Summary
Uranium is combined with O, C, N, transition metals for a variety of fuel types
UO2: ceramic, commercial reactor fuel, light water reactors
ATF: U3Si2 and Cr-doped UO2
UZr: fast reactor fuel
UMo: research reactor fuel
UC/UCO: high temperature gas reactors