## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2023

## Slide 2: Last Time
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin walled cylinder
  Thick walled cylinder
Increases in temperature cause most materials to expand
We call this thermal expansion, which is a strain that doesn’t inherently cause stress
Thermal expansion can cause stress when
  Deformation is constrained
  There are gradients in the expansion coefficient
  There is a temperature gradient
We have analytical equations for thermal stresses in the cladding and in the fuel

## Slide 3: The gap changes as a function of time
Both the pellet and the cladding swell
But, as the gap decreases, the temperature changes, which again makes the gap change
The solution using the analytical equations is iterative, due to the dependence of the gap size and temperature

## Slide 4: Example

## Slide 5: Calculate the steady state temperature profile in the rod, including thermal expansion
LHR = 200 W/cm, δ0gap = 30 μm, Rf = 0.6, Tco = 600 K, TEXP,0 = 373 K, kgap = 0.0026 W/cm-K, tC= 0.06 cm, αf = 11.0e-6 1/K, αC = 7.1e-6 1/K
So, TIC = 600 + 11.2 = 611.2 K, Ts = 672.4 K, T0 = 1232.0 K
First, we will deal with expansion in the cladding
  Av(Rc) = 0.6 + 30e-4 + 0.06/2 = 0.633 cm
  Av(TC) = (600+611.2)/2 = 605.6 K
  ΔRc = 0.633*7.1e-6*(605.6 – 373) = 0.001 cm

## Slide 6: Calculate the steady state temperature profile in the rod, including thermal expansion
Second, we deal with the fuel
  Av(Tf) = (1203 + 672.4)/2 = 937.7 K
  ΔRf = 0.6*11e-6*(937.7 – 373) = 0.0037 cm
The total change in the gap is 0.001 – 0.0037 = -0.0027
However, that means the gap is smaller and so our temperatures were wrong!

## Slide 7: This calculation is repeated until the gap width stops changing significantly
The change in the gap does NOT affect the coolant or cladding temperatures, just the gap and fuel temperatures
We only need to repeat the calculation of the fuel and cladding temperatures and the change in the gap
Iteration | δgap (cm) | Ts (K) | T0 (K)
0 | 0.003 | 701 | 1232
1 | 0.00066 | 644 | 1174
2 | 0.00097 | 652 | 1182
3 | 0.00094 | 651 | 1181
4 | 0.00094 | 651 | 1181

## Slide 8: THERMO-Mechanics

## Slide 9: Relating Displacements to Stress
We have been determining the stress due to some internal pressure (or temperature)
Often, the information more readily obtainable are the displacements
Utilizing the previous equations, can develop displacement to stress relationships for our geometry

## Slide 10: Assuming problem is axisymmetric

## Slide 11: Solve for the stress from the strain
Assume isotropic materials
Can perform matrix multiplication for the calculation of the stress, given the displacements

## Slide 12: Further simplify the problem to be 1D
No change in Z:

## Slide 13: Determine the strain and stress in the pellet for 1D case
Assume the radial displacement in the fuel pellet is ur(r) = 0.05r cm.
What is the strain tensor? At the outer edge:
We are dealing with UO2, so E = 200 GPa and ν = 0.345
  C11 = E (1 – ν)/((1+ν)( 1–2 ν)) = 200*(1–0.345)/(1.345*(1–2*.345)) = 314.2 Gpa
  C12 = E ν/((1+ν)( 1–2 ν)) = 200*0.345/(1.345*(1–2*.345)) = 165.5 Gpa
Now we can calculate the stresses
  σrr = 0.05*314.2 + 0.05*165.5 = 23.98 GPa
  σθθ = 0.05*165.5 + 0.05*314.2 = 23.98 GPa

## Slide 14: Example problem
Compute the stress and strain tensors in the center and at the outer edge (r = 0.5 cm) in 1D axisymmetric coordinates in a fuel pellet with ur(r) = r2/5. C11 = 314.2 Gpa, C12 = 165.5 Gpa.
First, calculate the strain tensor
εrr = ur,r = 2r/5
εθθ = ur/r = r/5
At the center there is no strain; at the outer edge
To calculate the stress, convert to a strain vector and multiply by elastic constant matrix
The stress in the center is zero
On the outer edge
  σrr = 0.2*314.2 + 0.1*165.5 = 79.4 GPa
  σθθ = 0.1*314.2 + 0.2*165.5 = 64.52 GPa

## Slide 15: NUMERICAL THERMO-Mechanics

## Slide 16: Now we can solve the temperature and the displacement vector for the full thermomechanical problem
T impacts the value of u through thermal expansion
u impacts the value of T through changes in the thickness of the gap
The value for T evolves with time
The value for u also evolves with time, even though there is not time in its PDE

## Slide 17: The primary tool for solving all thermomechanics problems is the finite element method
Finite difference
  Can solve the heat conduction equation
  Can’t easily solve the mechanics equations
Finite Volume
  Can solve the heat conduction equation
  Can’t easily solve the mechanics equations
Finite Element
  Can solve the heat conduction equation
  Can solve the mechanics equations
  Can handle any geometry
  Can handle any boundary condition

## Slide 18: The 1D thermomechanics problem definition
The initial temperature is set to 273 K
We will take 50 time steps of 0.5 s
The full power of Q = 450 begins at time t = 0.
UO2 material properties are used for both the thermal and mechanics equations
r
Rf
dT/dr = 0
ur = 0
Tr = Ts
dur/dr = 0

## Slide 19: Comparison to analytical theory
If we use a constant thermal conductivity, analytical 1D model matches very well
When k is a function of temperature, there is a difference between the FEM and analytical stress

## Slide 20: There are various available tools for solving coupled thermomechanical problems with FEM
Commercial tools
  ABAQUS
  ANSYS
  COMSOL
Open source
  MOOSE
NRC-based
  FRAPCON/FRAPTRAN

## Slide 21: The purpose of a fuel performance code is to simulate and evaluate fuel rod behavior
The first fuel performance codes were developed in the mid seventies
Advanced fuel performance codes are still under development today
KAIST-3A benchmark results, showing displacement of 3432 rods, from Gaston et al. 2014

## Slide 22: How are fuel performance codes used?
The primary goals are to predict the fuel centerline temperature and the stress in the cladding
Fuel performance codes aren’t focused on predicting power production, but rather to predict safety margins

## Slide 23: A fuel performance code must be able to predict:
Fuel
Temperature profile
Volumetric change
Gap
Gap heat transport
Mechanical interaction between fuel and cladding
Gap pressure
Cladding
Temperature profile
Stress

## Slide 24: The primary focus is solving the thermomechanical problem
Gap
The handling of the gap changes the most between different codes
Fuel
Solved Numerically
Solved Numerically or analytically
Cladding
Solved Numerically or analytically
Solved Numerically

## Slide 25: Various approaches to model the fuel rod
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 26: Early fuel performance codes were made for either steady state or transient operation
Steady state codes
  Leave of the time derivative part of the heat equation
  The material properties still evolve with time as a function of burnup
  The volumetric changes in the fuel are also a function of burnup
  Creep of fuel and cladding change with time
Transient codes
  Include the time derivative
  Have similar burnup dependent models like steady state codes, but don’t include creep
  Have additional models for rapid transients

## Slide 27: Start with FRAPCON
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 28: FRAPCON Flow Chart
FRAPCON iterates to determine fuel rod temperatures, fuel and cladding deformation
This converged data is iterated to produce gas release, void volumes and plenum pressure
Then marches forward in time

## Slide 29: FRAPTRAN
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 30: FALCON
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 31: FALCON
FALCON is a 2D fuel performance code developed by EPRI
Development of FALCON started in 1996
The beta version was released in 2003
It was developed by ANATECH for EPRI
FALCON is proprietary, owned by EPRI
It is no longer under active development in the US

## Slide 32: FALCON is a 2D transient and steady state code
Gap
Pressure is calculated using equation of state
Simplified contact model is used for gap closure
Gap heat transfer model is used
Fuel
Solved with FEM
Solved with FEM
Cladding
Solved with FEM
Solved with FEM

## Slide 33: FALCON can predict the fuel performance in axisymmetric RZ space or in Rθ space

## Slide 34: BISON
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 35: BISON
The next generation fuel performance code under development in the US
It uses the MOOSE framework
Development was begun in 2008
The first paper using BISON was published in 2009 and the paper summarizing its full capabilities was published in 2012
It was developed at Idaho National Laboratory, with some support by ANATECH
BISON is available for free, but it is export controlled and requires a license agreement be signed

## Slide 36: BISON models the fuel behavior ranging from 1D to full 3D and uses FEM
Gap
Pressure is calculated using equation of state
Fully implemented implicit contact algorithm
Gap heat transfer model is used
Fuel
Solved with FEM
Solved with FEM
Cladding
Solved with FEM
Solved with FEM

## Slide 37: Can handle smeared or discrete pellets, asymmetric pellet geometry and deformation

## Slide 38: Because of its unique 3D capability, BISON can model truly 3D fuel performance problems

## Slide 39: Other countries have other fuel performance codes
TRANSURANUS: ITU (Germany)
ALCYONE: CEA (France)
ENIGMA: NNL (UK)
FEMAXI-7: JAEA (Japan)
SFPR: IBRAE (Russia)
DIONISIO: (Argentina)
http://www.materials.cea.fr/en/PDF/PLEIADES-Platform.pdf

## Slide 40: Summary
Gap size changes due to thermal expansion
Often have displacements instead of strains, and can solve for stress via displacements
Fuel performance codes are focused on predict the center temperature of the pellet and the stress in the cladding
All fuel performance codes
  Numerically model the temperature in the fuel
  Numerically model the stress in the cladding
  And consider gap pressure, closure, and heat transfer in some way
The primary US codes are
  FRAPCON – Steady state 1.5D, uses finite difference
  FRAPTRAN – Transient 1.5D, uses finite difference
  FALCON – Steady or transient 2D, uses finite element
  BISON – Steady or transient, 1D – 3D, uses finite element