## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2022

## Slide 2: Housekeeping
Will be posting an optional assignment
  If completed will count as 10% of your total grade, and other assignments will be adjusted uniformly
  Details will be including within the post, but will be a written report, due April 22
Graded exams will be emailed out later today

## Slide 3: Fission products

## Slide 4: Fission Product Generation
Fission releases around 200 MeV
  The fission fragments have 169 MeV of kinetic energy
  2 to 3 neutrons with an average energy of 2 MeV
  7 MeV of prompt gamma ray photons
  The remaining energy is released by beta decay
Every fission product that is produced is now in the crystal lattice of the fuel, changing the microstructure

## Slide 5: There are various types of fission products that form in the fuel
Noble gases (Xe, Kr)
Essentially insoluble in the fuel matrix
Form either intragranular (within grain) voids or bubbles or intergranular (grain boundary) bubbles
Volatiles (Br, Rb, Te, I and Cs)
Exist as gases at high temperatures of the pellet interior
Also exist as solids at the cooler pellet exterior
Metals (Mo, Ru, Pd, and Tc)
Form metallic precipitates
Insoluble oxides (Zr, Ba and Sr)
Form insoluble oxides in the fluorite lattice
Soluble oxides (Y, La and the rare earths)
Dissolved in the cation sublattice

## Slide 6: All of the fission products impact the behavior of the fuel

## Slide 7: Fission Gas Release
Fission gases (Xe, Kr) are released in a process composed of three stages in UO2
Stage 1: Gas atoms are produced throughout the fuel due to fission and diffuse towards grain boundaries
Small intragranular bubbles form within the grains, but never get larger than a few nm radius due to resolution from energized particles
Gas atoms that don’t get trapped within the intragranular bubbles migrate to grain boundaries
Atoms forming a vacancy cluster

## Slide 8: Fission Gas Release
Stage 2: Gas bubbles nucleate on grain boundaries, growing and interconnecting
Stage 3: Gas travels through interconnected bubbles to a free surface

## Slide 9: Fission Gas Release
Fission gas release also occurs due to mechanisms that don’t depend on diffusion
Release can occur to particle recoil and knockout at low temperature
It can occur due to fracture during rapid transients

## Slide 10: Fission Gas Release
Released fission gas enters the gap and plenum, causing various problems
Xe and Kr have very low thermal conductivities, reducing the gap conductance
The plenum pressure increases
The volatile fission gases corrode the cladding
They are also radioactive and hazardous, causing problems when the cladding is breached
Fission gas release experiments:
  Post irradiation annealing
    Fuel is irradiated at low temperature
    Fuel is then placed into a furnace and heated
    Gas atom release is then measured
  In-pile release
    Gas release is measured during reactor operation
    It is much more difficult than post-irradiation annealing
    Total amount released is measured by puncturing cladding after irradiation
    Release with time can be estimated using a pressure transducer inside an instrumented fuel rod

## Slide 11: Fission Gas Release
Fission gas release models attempt to predict the rate at which gas is released from the fuel
To model fission gas release, ideally we must model all three stages of gas release
  Diffusion of gas atoms to grain boundaries
  Growth and interconnection of grain boundary bubbles
  Transport of gas atoms through interconnected bubbles to free surfaces
The earliest models only considered Stage 1
Most models now consider stage 1 and 2
There are no models that consider all three stages, but some are under development

## Slide 12: Booth Model
The Booth model is the earliest model of fission gas release and only considers stage 1
A grain is considered as a simple sphere
Gas atoms are released at the grain boundary
The model solves the diffusion equation in 1D spherical coordinates
Assumptions
  cg(r, t)
  All grains are spheres of radius a
  D is constant throughout the grain
  Gas is produced uniformly throughout the grain
  Gas is released once it reaches the grain boundary
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = 0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 13: Modeling post-irradiation annealing
The initial gas concentration is cg0
No gas is produced
Solving this equation tells us the value of cg at any radius or time
However, we want to know the fraction of gas atoms that have made it to the grain boundary
We use the flux at the grain boundary
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = cg0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 14: Solving the Booth Model
This equation is solved using a Laplace transform after nondimensionalization
Will not go through the derivation (shown in Olander)
τ = D x t / a2
τ < π-2
τ ≥ π-2
Grain boundary
Gas atoms
Release

## Slide 15: Booth Example
For a diffusion coefficient for Xe of D = 8e-15 cm2/s, what fraction of the fission gas trapped in an post-irradiation annealed fuel pellet has escaped after one hour? It has an average grain size of 10 microns
  D = 8e-15 cm2/s
  a = 10e-4 cm
  t = 3600 s
Which f? τ = D x t/a2 = 2.88E-4 < p-2 = 0.101
  f = 6*sqrt(8e-15*3600/(pi*(10e-4)^2)) – 3*8e-15*3600/(10e-4)^2 = 0.0181

## Slide 16: Different expressions for fission gas release
Given the data from the previous example, can plot both
  t < p-2
  t > p-2

## Slide 17: Modeling in-pile release
The initial gas concentration is 0
Gas is produced due to fission, where y is the chain yield (y = 0.3017 for Xe and Kr) and the fission rate
Gas can also decay, where λ is the decay constant
  If we only consider stable stable products, λ = 0
For in pile release, the fraction is equal to
After solving with with a Laplace transform
The total gas production is gas atoms/cm3
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = 0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 18: Example
For a diffusion coefficient for Xe of D = 8e-15 cm2/s, what fraction of the fission gas trapped in an in-pile fuel pellet has escaped after one hour? It has an average grain size of 10 microns.
  D = 8e-15 cm2/s
  a = 10e-4 cm
  We have a short time (t=3600 s), so we can use:
  f = 4*sqrt(8e-15*3600/(pi*(10e-4)^2)) – 3/2*8e-15*3600/(10e-4)^2 = 0.0121

## Slide 19: Gas release
We have calculated the fraction, but how much gas was actually released?
Consider 3% enriched UO2 with a thermal fission cross section of U-235, σf235 = 570 barns or 570 × 10-24 cm2 and a density of UO2, rU = 10.97 g/cm3.
What would be the number of fission gas atoms released after one hour with a neutron flux of 3×1013 n/(cm2 s) from a pellet of radius 0.5 cm and height 1.2 cm?
  Molar mass of 3% enriched UO2: 235*0.03 + 238*0.97 + 2*16 = 269.9 g/mol
  Atom density of U-235 = 10.97 x 1/269.9 x 6.022E23 x 1/1 x 0.03 = 7.34E20 atoms/cm3
  First, we have to calculate the fission rate: Fdot = 7.34E20*570E-24*3e13 = 1.26E13 fissions/(cm3 s)
  Next we calculate the total amount of fission gas produced
    NFG = y Fdot t = 0.3017*1.26E13*3600 = 1.36E16 fission gas atoms/cm3
    Vol = π r2 h = pi*0.5^2*1.2 = 0.94 cm3
    NFG*Vol = 1.36E16*0.94 = 1.28e16 fission gas atoms
  Finally we calculate the total amount of gas released using the fraction
    f = 0.0121
    Gas released = 0.0121*1.28e16 atoms produced = 1.55e14 atoms released

## Slide 20: As time progresses, both the fraction released and the produced gas increase

## Slide 21: Forsberg-Massih model
The Booth model ONLY considers stage one of fission gas release
Two stage Forsberg-Massih mechanistic model
  Considers intragranular diffusion diffusion to grain boundaries (stage 1)
  Also, grain boundary gas accumulation, resolution back into grain, saturation (stage 2)
  Assumes that once the bubbles on the grain face are interconnected, it is released (no stage 3)

## Slide 22: Forsberg-Massih model
2-stage F-M model over-predicts gas release because it neglects grain boundary bubble percolation (Stage 3)
Millett, Tonks, and Biner. JNM, 424.1 (2012): 176-182.

## Slide 23: Gas diffusion
The diffusivity of the fission gas depends on temperature and on irradiation
Experimental data shows three different regimes for the diffusivity
D = D1 + D2 + D3 cm2/s

## Slide 24: Gas diffusion
The effective fission gas diffusivity is slower due to trapping by intragranular bubbles
As the gas atoms diffuse towards the grain boundary, some are trapped by the small intragranular bubbles
Some are later knocked out by energized particles (called resolution)
The effective diffusion constant depends on the trapping rate rt and the resolution rate rr

## Slide 25: Summary
Fission products change the fuel behavior
Fission gas is released in three stages
  Fission gas production and diffusion to grain boundaries
  Grain boundary bubble nucleation, growth, and interconnection
  Gas transport through interconnected bubbles to free surfaces
Fission gas release is measured using post-irradiation annealing and/or in pile experiments
Fission gas release models are used to understand fission gas experiments and to predict gas release for fuel performance codes
Spherical grain models predict a fraction of gas release for post-irradiation annealing or for in-pile gas release
Fission gas diffusivity behavior changes with temperature and fission rate