## Slide 1: Nuclear Fuel Performance
NE-591-010
Spring 2021

## Slide 2: Last Time
Wrapped up thermomechanics
Overviewed US fuel performance codes

## Slide 3: Material Property Evolution

## Slide 4: Pretty much everything we have learned so far, nothing changes once the fuel and cladding reach steady state

## Slide 5: Fuel is dynamic!

## Slide 6: Property changes due to microstructure evolution during reactor operation must be considered
Mid Life
Point defect diffusion
Point defect clustering
Fission gas segregation to GB and voids
Bubble nucleation
Zinkle and Singh 2000
Late life
Fission product swelling
Bubble percolation and fission gas release
Cladding creep
Fuel creep
Brohan 2000
Insertion in reactor
Removal from reactor
Fuel Fabrication
Sintered UO2
Height 2 cm
Diameter 1 cm
~10 μm grain size
Density > 95%
From Pedro Peralta, ASU
Fuel failure
Pellet/cladding interaction
Cladding corrosion
Cladding fracture
Santana et al. 2011
Early life
Thermal expansion
Fracture
Point defect and fission gas generation
Fuel Densification

## Slide 7: The properties and performance of a material are a result of factors across various length scales
Chemical bonds
Crystal structure
Defect interactions
Microstructure
Material properties and performance

## Slide 8: The crystal structure of a material is the shape of the ordered structure of the atoms
The atoms of many materials form an organized lattice, these are called crystalline materials. All reactor materials are crystalline.
The configuration of the atoms in the lattice impacts the properties of the material (density, thermal expansion coefficient, elastic modulus, etc.)
All major light water nuclear materials are either cubic or hexagonal
(d) Hexagonal close packed

## Slide 9: Crystalline materials
In crystalline materials, the lattices are not perfect, they have defects
Defects can be 0D, 1D, 2D, 3D
The interactions between defects seriously impact material properties and how they perform

## Slide 10: Point defects
Point defects (zero-dimensional defects) are lattice imperfections related to one or two lattice sites
There are several types of point defects
  Vacancies
  Self interstitial atoms (SIA)
  Interstitial impurity atoms
  Substitutional impurity atoms
Point defects control the mobility of atoms and, therefore influence all processes that depend on diffusion

## Slide 11: Point defects
Vacancies and interstitials form naturally in materials
Extra atoms can sit on a surface, creating a vacancy, or a surface can have a missing atom, creating a self interstitial atom (SIA)
We define the number of vacancies or interstitials in terms of a concentration
There exists an equilibrium concentration of point defects

## Slide 12: Radiation damage
Ionizing radiation can introduce defects into the crystal lattice, called radiation damage
PKA collisions create a collision cascade, which results in the generation of defects (point and clusters)

## Slide 13: Dislocations are imperfections associated with a line of lattice sites (1D defect)
In a dislocation, an extra half plane of atoms is inserted into the lattice
When it moves, only a small number of bonds are broken at a time
Dislocation motion controls the plastic (permanent) deformation of crystalline materials

## Slide 14: Grain boundaries
Materials are typically composed of various regions where the crystal lattice is oriented differently. These regions are called grains
When two grains meet, there is a plane of atoms that do not follow the crystal lattice called a grain boundary
Most crystalline materials are polycrystalline, not single crystal
High-res transmission eleectron microscopy can also show individual atoms (palladium)
www.knmf.kit.edu/TEM.php
Atomistic simulation of grain boundaries in 3D

## Slide 15: Metals are often cast, and polycrystals naturally form during casting

## Slide 16: Polycrystals naturally form during casting
Solidification begins in different regions of the melt, each with a different orientation
Once the different regions meet, grain boundaries form between them

## Slide 17: Ceramic sintering
Ceramics are typically sintered, and polycrystals also naturally form from sintering
In sintering, powders are compacted at high temperature
The particles are each oriented differently, and as the fuse, grain boundaries form
The differences between the grain orientations result in the grain boundary

## Slide 18: Distribution of grain sizes
In a polycrystal, there is also a distribution of grain sizes
Therefore, we commonly refer to the grain size distribution and the average grain size
The Hillert distribution is an analytical distribution for grain size
Real materials often vary from this behavior

## Slide 19: 3D Defects
When point defects cluster, they form three dimensional defects
The energy of a point defects is reduced when several point defects cluster together
Larger clusters of vacancies are called voids
Clusters of impurity atoms are called precipitates

## Slide 20: Microstructure
Material microstructure is the structure observable with 25x magnification
The microstructure includes grain structure, secondary phases, porosity, and more
The microstructure can strongly influence physical properties such as strength, toughness, ductility, hardness, corrosion resistance, high/low temperature behavior or wear resistance.
These properties in turn govern the application of these materials in industrial practice
Annealed Stainless Steel
Cast Bronze
Sintered UO2
Co-Al-W Superalloy
Friction stir welded stainless steel

## Slide 21: Material processing
The process we use to make a material has a huge impact on its microstructure and properties
Casting – manufacturing process in which a liquid material is poured into a mold and then allowed to solidify
  Can be used to make complex shapes
  The solidified microstructure typically has properties that are far from ideal
Sintering – Forming a solid from a powder using heat and/or pressure without melting the material
  Applicable to metals and ceramics
  Difficult to obtain a material that is fully dense
  Used to make fuel pellets
Heat treatment – heating or cooling a material to extreme temperatures to get desired microstructure and properties
  Used to control the rate of microstructure change, including diffusion, grain growth, or phase change
  Use on many types of materials (metals, ceramics, glasses)

## Slide 22: Summary
Even during steady state operation, fuel and pellet conditions change with time due to microstructure evolution
Atoms in the fuel and cladding materials are arranged in a crystal lattice
The crystal lattice is never perfect; it has defects
  Point defects include vacancies, interstitials, and impurity atoms
  Dislocations are line defects
  Grain boundaries are planar defects
  Voids and precipitates are volume defects
All materials have defects, radiation damage causes many more defects
Microstructure can be tailored through processing

## Slide 23: UO2 Radiation effects

## Slide 25: High Burnup Structure (HBS)
When thermal recovery is not sufficiently efficient (at lower temperatures), the accumulation of defects at high burnup can lead to the instability of the crystalline structure, initiating a restructuring driven by the energy stored in the material
In UO2, grains subdivide (to 100-500 nm size) and a densely porous structure is formed

## Slide 26: High Burnup Structure (HBS)
The increase of the relative porosity volume degrades the material conductivity and reduces the mean grain size
On the other hand, the intragranular irradiation defect-cleaning improves the fuel intrinsic thermal conductivity
Fission gas in HBS bubble is retained, not released

## Slide 27: Fuel chemistry

## Slide 28: Fuel Chemistry
UO2 is an ionic compound that must have balanced charges
What is the charge of a typical oxygen ion?
  O2-
Uranium valance states
  Possible: U3+, U4+, U5+, U6+
  Most stable: U4+, U5+, U6+
  Beyond UO2, can have U4O9, U3O8, UO3
The structure is very stable all the way up to the melting temperature and down to extremely low temperatures, even with irradiation damage
There is space in the uranium lattice that can accommodate fission products

## Slide 29: O/M ratio
The ratio of oxygen to uranium metal (O/M ratio) can vary
This is the stoichiometry
The homogeneity range of uranium dioxide extends to both hypo- and hyperstoichiometric compositions in oxygen
The minimum and maximum oxygen contents in the dioxide correspond to the compounds with the formula of respectively UO1.67 at 2720 K and UO2.25 at approximately 2030 K
Will the O/M ratio go up or down during reactor operation?
  It is complicated, because of the formation of fission products that also react with the oxygen, and O interaction with Zr cladding

## Slide 30: Excess O
The crystal structure of UO2 can accommodate extra oxygen
Excess oxygen resides at interstitial locations
Oxygen in neighboring sites is displaced
Cation valence increases to maintain electrical neutrality
Fuel fabricated to be nearly stoichiometric; i.e., UO2.00± because:
  It is the most stable
  It has the highest melting temperature
[after Olander, 1976]

## Slide 31: Incorporation of Fission Products
As fission products form, the valence state of the uranium can change
Typical valence of soluble fission products is M3+
The uranium valence state changes to compensate
  Oxygen liberated by fission
  Fission products produced with M3+ valance state incorporated in fuel lattice
  Uranium oxidizes from U4+ to U5+ or U6+ to maintain local electrical neutrality

## Slide 32: Oxygen potential
The oxygen potential is a measure of how free the oxygen is to escape/move around
Oxygen potential is defined as:
or, equivalently:
  With = Chemical potential of oxygen in solution
  = Gibbs free energy of gaseous oxygen at temperature T and a standard pressure (1 atm)
It is possible to determine the stoichiometry from the oxygen potential

## Slide 33: Oxygen potential
The oxygen potential changes during irradiation, indicating change in the O/M ratio
Oxygen potential changes during irradiation due to
  Liberation of oxygen by fission; Generation of fission products; Conversion of uranium to plutonium; Reaction of oxygen with U, Pu, fission products, and cladding
Oxygen potential across pellet radius observed to be constant at the approximate value of Mo/MoO2 reaction (from calculations)
Mo serves as a buffer to the O potential, or a means of inferring what the oxygen potential may have been in the fuel from PIE
Oxygen potential is low near the cladding, because the oxygen enters the cladding

## Slide 34: Fuel Stoichiometry/Properties
The stoichiometry of the fuel directly impacts the fuel performance
Stoichiometry impacts
  Melting temperature
  Thermal conductivity
  Processes dependent on diffusion
    Grain growth
    Fission gas release
    Creep
  Chemical state and behavior of fission products
  Chemical reactions at inner cladding surface
Thermal conductivity is highest for stoichiometric UO2

## Slide 35: Fuel Stoichiometry/Properties
The lattice constant of the material decreases with increasing stoichiometry
The vacancy formation energy also changes with stoichiometry

## Slide 36: Fuel Stoichiometry/Properties
The solution energy of Xe, Cs, and Sr in UO2 depends on stoichiometry as well
The coefficient defining Xe diffusion also changes with stoichiometry
Though stoichiometry matters, most fuel performance codes ignore it
Fission product | UO1.97 | UO2 | UO2.03
Xe | 3.88 eV | 3.88 ev | 2.61 eV
Cs | 1.7 eV | -0.04 eV | -3.29 eV
Sr | -3.71 eV | -6.03 eV | -9.55 eV

## Slide 37: Fuel Chemistry Summary
UO2 has a cubic fluorite structure that is very stable
The charges are balanced with a U4+ valence state
However, the ratio of oxygen to uranium can change. We call this the stoichiometry and abbreviate it as O/M ratio
The O/M ratio changes during reactor operation, but it is complicated
The O/M ratio impacts many properties of the fuel