## Slide 1: Nuclear Fuel Performance
NE-591-010
Spring 2021

## Slide 2: Last Time
Solid mechanics predicts the deformation of a body from its applied load
The strain defines the deformation
The stress defines the material’s response to the strain
Materials can have recoverable and permanent deformation
  Elastic deformation is recoverable and occurs due to the stretching of the atomic lattice
  Plastic deformation is permanent and results form the breaking of bonds
Elastic moduli and Elastic constants

## Slide 3: Mechanics

## Slide 4: Stress/Strain Regions
Once the stress reaches the yield stress, it plastically deforms
σy is the yield stress
σU is the ultimate tensile stress
The final stress before rupture is called the fracture stress

## Slide 5: Permanent Strain
After plastic deformation, if you unload the sample, it still has the permanent strain
After unloading, the strain hardening has changed the material
Thus, if you reload, the yield strain is often higher than it was previously

## Slide 6: The hardening behavior changes for different materials
K is a strength coefficient, n is the strain hardening exponent, e0 is the prior plastic strain, ep is the plastic strain, and sy is the yield strength
The strain hardening exponent is a material property, with a value between 0 and 1
A value of 0 means that a material is a perfectly plastic solid, while a value of 1 represents a 100% elastic solid.

## Slide 7: Dislocation motion
Plastic deformation occurs due to dislocation motion
A dislocation is a line defect
  Edge and screw type
When it moves, only a small number of bonds are broken at a time

## Slide 8: Dislocation are produced during deformation

## Slide 9: Dislocation motion causes plastic deformation, dislocation pileup causes hardening

## Slide 10: Dislocation Pile Up
Dislocation motion can be inhibited by barriers, including grain boundaries, precipitates, voids, bubbles, etc.

## Slide 11: Ductility
Ductile materials plastically deform significantly, brittle materials do not
Quantities defining ductility are total percent elongation at fracture (%EL) and the percent reduction in area (%RA)
The ductile–brittle transition temperature (DBTT) of a metal is the temperature at which the fracture energy passes below a predetermined value
Below the DBTT, failure is brittle
Cold working and neutron irradiation can increase the DBTT, potentially reducing ductility of reactor components

## Slide 12: As the strength increases due to dislocation pile-up, the ductility decreases
Toughness is the ability of a material to absorb energy and plastically deform without fracturing
Toughness is related to the area under the stress–strain curve
In order to be tough, a material must be both strong and ductile
Materials are often work hardened prior to utilization to modify mechanical properties

## Slide 13: Determine the stress and strain throughout a body

## Slide 14: The stress divergence equation derivation
Generalized momentum conservation:
Considering a cubic element, surface forces act on the walls of the cube
Force on a wall is the product of the stress and the surface area
  For wall at dx, approximate stress via Taylor expansion

## Slide 15: Simplified Cauchy for our typical system
Assumption 1: We have a static body
Assumption 2: Gravity is negligible
Assumption 3: The problem is axisymmetric
r
q
z

## Slide 16: Consider the material response of the axisymmetric body
We assume small strains (elasticity), so the strain is defined as
We assume isotropic material response, so

## Slide 17: Solve for the stress throughout a pressurized cylinder (cladding tube) with thin walls
Because our cylinder has such thin walls (δ = thickness), we can simplify everything to simple force balance
The hoop stress is the force exerted circumferentially in both directions on every particle in the cylinder wall
First, we need the Force per unit length due to the pressure
Utilize force to hoop stress relation:
Then we equate the forces and solve for the hoop stress

## Slide 18: Find the other two stresses for a thin walled cylinder
To find the stress in the z-direction we do another force balance
Again, we equate the forces and solve for the stress
Last, the stress on the inside of the wall is –p and on the outside is zero, so the average
Ftop
Fwall

## Slide 19: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  R = 0.55 cm, δ = 0.05 cm, σy = 381 MPa
The largest stress will be the hoop stress
The hoop stress is P*(0.55/.05)
  For 5 MPa, σθ = 55 Mpa
  For 9 MPa, σθ = 99 Mpa
With these pressures, we don’t come even close to the yield stress of the cladding

## Slide 20: Stress within a pressurized cylinder that has thick walls (radius/thickness<20)
The cylinder as an inner radius Ri and an outer Radius Ro
We assume there is no shear stress, so σrz = 0
We will begin with the r equation
Now we need our constitutive law
We combine these equations to get

## Slide 21: Develop equations for the stress within a pressurized cylinder with thick walls
We need one more relationship from the definition of the strain
From the previous slide, we have
If we combine these, we get
Again, from the previous slide
We end up with

## Slide 22: We now have an ODE so we can solve to get the stress
Our boundary conditions are σrr(Ri) = -p and σrr(Ro) = 0
After integrating twice, we get
From σrr, we can get σθθ from
From the end condition, we determine σzz
(a)
(b)
(c)

## Slide 23: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  Ri = 0.52, Ro = 0.58 cm, σy = 381 MPa
Which stress is the largest?
  σθθ
At what position r will the hoop stress be the largest?
  r = Ri = 0.52 cm
What is the stress at p = 5 MPa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 46.0 MPa
What is the stress at p = 9 Mpa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 82.7 Mpa
Again, we don’t even get close to yielding

## Slide 24: We’ve now solved this same problem assuming thin and thick walled cylinders

## Slide 25: Summary
Solid mechanics predicts the deformation of a body from its applied load
  The strain defines the deformation
  The stress defines the material’s internal response to the strain
Materials can have recoverable and permanent deformation
  Elastic deformation is recoverable and occurs due to the stretching of the atomic lattice
  Plastic deformation is permanent and results form the breaking of bonds during dislocation (line defect) migration
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin walled cylinder
  Thick walled cylinder