## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2022

## Slide 2: Last Time
However, the ratio of oxygen to uranium can change. We call this the stoichiometry and abbreviate it as O/M ratio
The O/M ratio impacts many properties of the fuel
MOOSE overview
Any progress or problems with MOOSE?

## Slide 3: grain Properties/Behavior

## Slide 4: Grain Boundaries
Materials are typically composed of various regions where the crystal lattice is oriented differently
When two grains meet, there is a plane of atoms that do not follow the crystal lattice called a grain boundary
Grain boundaries add energy to the material that is a function of their structure
A grain boundary’s energy is determined by its:
  Inclination – the orientation of the 2D grain boundary plane (2 degrees of freedom)
  misorientation – the rotation required to align one grain with the other (3 degrees of freedom)

## Slide 5: Grain Texture
The orientation of all the grains in a material is called the texture
The degree of texture is dependent on the percentage of crystals having a preferred orientation
  randomly oriented grains equals no texture
Texture is seen in almost all engineered materials, and can have a great influence on materials properties

## Slide 6: Grain size
In a polycrystal, there is also a distribution of grain sizes
The average grain size of the fuel has a significant impact on its behavior
Typical LWR fuel has an initial average grain size of about 10 microns
The average grain size impacts
  Fission gas release
  Swelling
  Thermal conductivity
  Creep

## Slide 7: Grain boundary diffusion
Diffusion often occurs faster along grain boundaries than in the perfect crystal
Grain boundaries have more space than the perfect lattice
So, atoms diffuse faster along grain boundaries than through the perfect lattice
This means that grain boundary, or intergranular, diffusion increasingly dominates bulk (intragranular) diffusion
This can become more pronounced as the temperature is reduced
Grain boundary diffusion has a large impact on creep

## Slide 8: Grain boundary segregation
Impurity atoms (such as fission gas) and other defects move to grain boundaries
Due to grain boundaries having more open space, impurity atoms have a lower energy when they are on grain boundaries.
This is called grain boundary segregation
Radiation induced segregation (RIS) is where radiation produces defects that drive towards the grain boundary and preferentially drag solute atoms

## Slide 9: Dislocation interaction with grain boundaries
Grain boundaries impede dislocation motion
The number of dislocations within a grain impacts how easily dislocations can traverse grain boundaries and travel from grain to grain
So, by changing grain size one changes barrier density, influencing dislocation movement and yield strength
This is called the Hall-Petch effect
  where σy is the yield stress, σ0 is a materials constant for the starting stress for dislocation movement (or the resistance of the lattice to dislocation motion), ky is the strengthening coefficient (a constant specific to each material), and d is the average grain diameter

## Slide 10: Grain boundaries and cracks
Materials often crack along grain boundaries
Grain boundaries can be weaker than the perfect lattice
  different bonding environment, increased extrinsic particles, etc.
Thus, fracture will often occur along grain boundaries (intergranular fracture)

## Slide 11: Grain size change
A single crystal has a lower energy state than a polycrystal, due to the grain boundary energy
So, grain boundaries migrate to reduce the energy
vGB = MGB (Pd – Pr)
  MGB is the grain boundary mobility
  Pd is the driving force (pressure) for grain growth
  Pr is the pressure resisting grain growth

## Slide 12: Grain growth
Due to grain boundary migration, the average grain size goes up with time during annealing/heat treating
As grain boundaries migrate, some grains grow and some shrink
Shrinking grains eventually disappear
The average grain volume
Therefore, as Ngrains decreases due to grain disappearance, the average grain volume goes up

## Slide 13: Grain boundary mobility
The grain boundary mobility is a function of temperature and GrB type
The grain boundary mobility is determined according to
  m4/(J s)
  kb = 8.6173e-5 eV/K is the Boltzmann constant
Both the pre-factor M0 and the activation energy Q change as a function of the grain boundary misorientation
We often use an average grain boundary for a material, taken from polycrystal measurements-> UO2: M0 (m4 /J-s) = 4.6e-09, Q (eV) = 2.77
What is the mobility of UO2 at 1600 K?
  MGB = 4.6e-9*exp(-2.77/(1600*8.6173303e-5)= 8.7e-18 m4/J-s

## Slide 14: Grain growth
There are various driving forces for grain growth
The most common driving force is the reduction of grain boundary energy
  , where γGB is the GB energy and R is the radius of curvature
  It is often called the curvature driving force, because it drives grain boundaries to be straight
  It also causes larger grains to grow at the expense of smaller ones
Other driving forces include
  Temperature gradients
  Elastic energy gradients
  Dislocation energy gradients
Velocity of a spherical grain:

## Slide 15: Grain growth
Grain boundary motion is inhibited by pores, precipitates, solute atoms, etc.
Solute atoms (whether in interstitial sites or vacancies) can decrease the grain boundary mobility.
  This is called Solute Drag
  Even a small concentration of impurities can decrease the mobility by 3 to 4 orders of magnitude
Particles and pores resist grain boundary motion

## Slide 16: Irradiation can accelerate grain growth, but it is only significant with small grains and low temperature

## Slide 17: Maximum grain size
Consider a material with an average grain size D
The change in D can be written as
  k = 2 MGB γGB is a rate constant that can be determined from experiments
  Dm is the grain size at which the driving force equals the resistive pressure
For UO2:
Dm is a function of temperature microns

## Slide 18: Fuel Densification
Remember that fresh fuel pellets are not fabricated to be 100% dense, more like 95-99% dense
Early in life, fuel pellets shrink and the initial porosity is largely eliminated
In some ways, densification is a continuation of the sintering process
However, irradiation accelerates the process
Small pores close due to effects of fission spikes and vacancy diffusion
Large pores stable (in absence of large hydrostatic stress)
Pellets with higher initial density, densify less

## Slide 19: Densification
The driving force for densification is the change in free energy from the decrease in surface area of pores and lowering of the surface free energy
An empirical relation to describe densification has been built as a function of
  β - Burnup (in FIMA)
  Δρ0 – Total densification that can occur ~ 0.01
  βD – Burnup at which densification stops ~5 MWD/kgU, ~0.005 FIMA
  CD = 7.235 − 0.0086 (T − 25) for T < 750C and CD = 1 for T ≥ 750C

## Slide 20: Empirical models
Many models of reactor fuel behavior are fits to experimental data
They are typically correlated to burnup
Burnup is a measure of how much fissioning has taken place. Typical units are:
  MWD/kgU
  FIMA
It can be calculated from the volumetric fission rate
Units of this equation are FIMA
To convert from FIMA to MWD/kgU, multiply by 950
after Garzarolli in [Rudling et al, 2007]

## Slide 21: Summary
The average grain size in UO2 impacts fuel behavior and performance:
  Fission gas release
  Swelling
  Thermal conductivity
  Creep
The material wants to reduce its energy by having large grains grow at the expense of small grains
Grain growth is reduced due to other defects reducing the grain boundary migration
Fuel densification is driven by reduction in surface area of pores – continuation of sintering process
Empirical models describe densification as a function of burnup

## Slide 22: Fission products

## Slide 23: Fission Product Generation
Fission releases around 200 MeV
  The fission fragments have 169 MeV of kinetic energy
  2 to 3 neutrons with an average energy of 2 MeV
  7 MeV of prompt gamma ray photons
  The remaining energy is released by beta decay
Every fission product that is produced is now in the crystal lattice of the fuel, changing the microstructure

## Slide 24: There are various types of fission products that form in the fuel
Noble gases (Xe, Kr)
Essentially insoluble in the fuel matrix
Form either intragranular (within grain) voids or bubbles or intergranular (grain boundary) bubbles
Volatiles (Br, Rb, Te, I and Cs)
Exist as gases at high temperatures of the pellet interior
Also exist as solids at the cooler pellet exterior
Metals (Mo, Ru, Pd, and Tc)
Form metallic precipitates
Insoluble oxides (Zr, Ba and Sr)
Form insoluble oxides in the fluorite lattice
Soluble oxides (Y, La and the rare earths)
Dissolved in the cation sublattice

## Slide 25: All of the fission products impact the behavior of the fuel

## Slide 26: Fission Gas Release
Fission gases (Xe, Kr) are released in a process composed of three stages in UO2
Stage 1: Gas atoms are produced throughout the fuel due to fission and diffuse towards grain boundaries
Small intragranular bubbles form within the grains, but never get larger than a few nm radius due to resolution from energized particles
Gas atoms that don’t get trapped within the intragranular bubbles migrate to grain boundaries
Atoms forming a vacancy cluster

## Slide 27: Fission Gas Release
Stage 2: Gas bubbles nucleate on grain boundaries, growing and interconnecting
Stage 3: Gas travels through interconnected bubbles to a free surface

## Slide 28: Fission Gas Release
Fission gas release also occurs due to mechanisms that don’t depend on diffusion
Release can occur to particle recoil and knockout at low temperature
It can occur due to fracture during rapid transients

## Slide 29: Fission Gas Release
Released fission gas enters the gap and plenum, causing various problems
Xe and Kr have very low thermal conductivities, reducing the gap conductance
The plenum pressure increases
The volatile fission gases corrode the cladding
They are also radioactive and hazardous, causing problems when the cladding is breached
Fission gas release experiments:
  Post irradiation annealing
    Fuel is irradiated at low temperature
    Fuel is then placed into a furnace and heated
    Gas atom release is then measured
  In-pile release
    Gas release is measured during reactor operation
    It is much more difficult than post-irradiation annealing
    Total amount released is measured by puncturing cladding after irradiation
    Release with time can be estimated using a pressure transducer inside an instrumented fuel rod

## Slide 30: Fission Gas Release
Fission gas release models attempt to predict the rate at which gas is released from the fuel
To model fission gas release, ideally we must model all three stages of gas release
  Diffusion of gas atoms to grain boundaries
  Growth and interconnection of grain boundary bubbles
  Transport of gas atoms through interconnected bubbles to free surfaces
The earliest models only considered Stage 1
Most models now consider stage 1 and 2
There are no models that consider all three stages, but some are under development

## Slide 31: Summary
Five families of fission products
Fission products change the fuel behavior
Fission gas is released in three stages
  Fission gas production and diffusion to grain boundaries
  Grain boundary bubble nucleation, growth, and interconnection
  Gas transport through interconnected bubbles to free surfaces
Fission gas release is measured using post-irradiation annealing and/or in pile experiments

## Slide 32: Notes
Next lecture will be half lecture, half problem session
Exam on 3/10: Week from Thursday
Presentations hopefully graded by this Thursday, with feedback