## Slide 1: NE 591: Advanced Reactor Materials
Fall 2021
Dr. Benjamin Beeler

## Slide 2: Last Time
Intro to molten salts
Salt reactor designs and general benefits
Fluorides and chlorides salts for different applications
Requirements for fuel salts
Control of oxygen and redox conditions is critical to limit precipitation of the fuel and corrosion of the cladding

## Slide 3: Changes During Fission
The fission process continuously alters the fuel salt redox conditions
When a U or Pu ion fissions, the available electrons will rearrange on each fission product to satisfy its valence requirements and produce either net oxidizing or reducing conditions in the melt
For UF4, four F ions are released; often fission products require less than four and thus there will be an excess of F ions with net oxidizing conditions

## Slide 4: Fission Products
Distribution of fission products is a central safety issue
Fission products may be gaseous, solid, or dissolved
Alkali and alkaline earth fission products form stable salts – Rb, Cs, Sr, Ba
Lanthanides and some transition metals can form stable salts
Semi-noble fission products plate out on metal surfaces – Nb, Mo, Tc
A few elements are very sensitive to redox changes
May elect to actively remove gaseous fission products
  Lowers the in-core accident source term
  Requires cooling fission product traps
  Bubble formation and collapse results in reactivity jumps

## Slide 5: Fission Product Plating
Noble metals are insoluble in the fluoride salt and can be found in helium sparge gas, on the graphite, or deposited on the metallic surfaces of the primary circuit
The deposited material contributes to the heat generation from its decay even after the reactor shutdown, decreasing the overall safety of the MSR
The deposits on the graphite specimens in the case of thermal reactors absorb neutrons during the operation and lead to lower efficiency of the reactor
One way of avoiding this detrimental precipitation is to remove the insoluble fission products by helium bubbling before they interact with the structural materials

## Slide 6: Cover Gas
The cover gas (off-gas) handling system is a key element of any MSR
Fission gases such as xenon and krypton will readily escape the salt
Acidic gases may accumulate as a result of radiolysis
Tritium is formed by neutron interactions with light elements in the salt
The cover gas system will contain the radionuclides emerging from the free surface above the fuel salt as well as any sweep or sparging gases used

## Slide 7: Tritium
Tritium production and control is an issue for Li-bearing salts
Tritium is produced by neutron reactions with lithium, beryllium, and fluorine as well as being a ternary fission product
Tritium can exist as ions or as TF, depending on redox conditions
Above 300C tritium will diffuse through structural materials

## Slide 8: Radiolytic Stability
Radiolysis is the dissociation of molecules by ionizing radiation
Molten salts are highly radiolytically stable
Salts are combinations of strongly electronegative elements with strongly electropositive metals with very high bond energies
Formation energy of salts is more negative than metal fluorides
MSRE graphite and Hastelloy N exposed to coolant salt was clean after ~3 years of operation

## Slide 9: Three principal corrosion processes
Reactions due to oxides on the metal
Reactions with dissolved impurities
Reactions with necessary constituents of the melt

## Slide 10: Protective coatings?
It is not useful to apply a protective coating of, for example, an oxide layer on the structural material for the two following reasons:
  although some oxides are relatively insoluble in the fluoride melt, most are readily dissolved
  all oxides rapidly recrystallize
Oxide films on the surface of the alloy can be attacked by the fluoride melt
The formed oxides (BeO below) typically don’t matter as long as they do not contain fissile elements
The formed fluorides are more important as they will act as oxidants of Cr in the alloy

## Slide 11: Oxides and Impurities
Oxide films on the metal are dissolved, leading to cladding constituent fluorides
Other corrosion reactions are possible with solvent components
Such reactions can lead to rapid initial corrosion
These impurity reactions can be minimized by maintaining low impurity concentrations in the salt and on the alloy surfaces

## Slide 12: Dissolved Impurities
In addition to impurities generated by reactions with oxides, impurities may result from incomplete removal of HF or of easily reducible fluorides during the salt purification
This is done by successive reactions with HF–H2 and H2

## Slide 13: Graphite Compatibility
Graphite does not react with molten fluoride mixtures of the type to be used in the MSR concepts
After carbon, borides and nitrides appear to be the most compatible nonmetallic materials
Thermodynamic data suggest that the most likely reaction is:
but this should come to equilibrium at very low CF4 pressures
CF4 concentrations over graphite–salt systems maintained for long periods at elevated temperatures have been shown to be below the limit of detection

## Slide 14: Constituents of the Melt
The oxidation reaction of alloy components with UF4 has been suggested to play an important role in corrosion
The equation will define/buffer the electrochemical potential of the salt via the UF4/UF3 ratio
Based on reasonable estimations of the activity coefficients for the above reaction, the equilibrium concentration of CrF2 is of the order of 130–300 ppm for a fuel with 1% UF3 contained in Hastelloy-N

## Slide 15: Tellerium
When Te is present in the metallic form in the fuel, it corrodes Ni-based alloys and embrittles its surface grain boundaries
Embrittlement is a vital issue to consider because it can result in cracking of the structural materials
This intergranular embrittlement produced in Hastelloy-N can be significantly reduced by adding 1–2 wt% of niobium into the Hastelloy-N
Another way to suppress the corrosion rate is by increasing the reducing conditions of the fuel, which is done by the increasing the UF3/UF4 ratio
This allows Te to be present as Te-2 rather than in an ‘oxidized’ metallic form, and this is less aggressive against the nickel-based alloys

## Slide 16: Materials for MSR systems
The materials required fall into three main categories: (1) metallic components for primary and secondary circuits, (2) graphite (or other structural steels) in the core, and (3) materials for molten-salt fuel reprocessing systems
The metallic material used in constructing the primary circuit of an MSR will operate at temperatures up to 700–750C
Nitrogen can oxidize the outside of the material due to exposure to air
Operating lifetime of 30-50 yrs, with fluences of up to 8x1021 n/cm2
The metal must have moderate oxidation resistance, must resist corrosion by the salt, and must not be subject to severe embrittlement by neutrons
The material must shapeable, with wall thicknesses from >1cm to less than 1mm, and weldable

## Slide 17: Metallic Materials for MSR systems
Fairly extensive literature exists on corrosion of metal alloys by molten fluorides in convection or forced flow loops
Limited experimental efforts on irradiation-combined corrosion effects
Nickel-based and austenitic stainless steels were primarily investigated
General knowledge:
Corrosion is associated with outward diffusion of Cr through the alloy
Corrosion rate is marked by initial rapid attack associated with dissolution of Cr and is largely driven by impurities in the salt
This is followed by a linear corrosion rate which is controlled by mass transfer

## Slide 18: Metallic Materials for MSR systems
General knowledge:
Minor impurities in the salt can enhance corrosion by several orders of magnitude
Dissolution can be mitigated by a chemical control of the redox conditions in the salts
Stainless steels, Inconel 600, Hastelloy-B, and Hastelloy-W were explored, but either excessively corroded or had poor aging properties
Hastelloy N was developed with a composition of Ni–16%Mo–7%Cr–5%Fe–0.05%C
Limited Cr is included to impart moderate oxidation resistance in air, but not high enough to lead to high corrosion rates in salt
Hastelloy N has excellent corrosion resistance to molten fluoride salts at temperatures considerably above those expected in MSR service

## Slide 19: Metallic Materials for MSR systems
Problems with Hastelloy-N
Is subject to irradiation hardening due to accumulation of He at grain boundaries
This is potentially mitigated through alloys with fine carbide precipitates to trap He
Tiny cracks formed on the inside surface of Hastelloy-N piping for the MSRE
Intergranular cracks were due to Te, which can likely be controlled with appropriate redox conditions
Additions of Ti can aide in fine carbide precipitates, and additions of Nb can limit Te cracking
No alloys with both additions have been studied, but it is supposed to additions of 1% Ti and 1% Nb can sufficiently solve both problems

## Slide 20: Materials for MSR systems
Focus on graphite core
Graphite is the principal material other than salt in the core of the reference breeder reactor design with a thermal spectrum, or used as a reflector in fast designs
The graphite structures will operate in a fuel salt environment over a range of temperatures from 500 up to 800C
There are two main requirements in the graphite in MSRs: that both molten salt and xenon be excluded from open pore volume
Significant penetration of the graphite by the fuel salt would generate a local spot, leading to enhanced radiation damage to the graphite and perhaps local boiling of the salt

## Slide 21: Graphite for MSR systems
Extensive experimental work has demonstrated the compatibility of graphite with molten salts
Graphite undergoes the same shrinkage/turnaround processes during irradiation
For molten salts, post-turnaround graphite is of concern, due to the increased porosity allowing for salt ingress
This puts a cap on fast neutron fluence in graphite for salt systems at about 3E22 n/cm2, which translates into about 3-4 years as a moderator in the MSBR
Graphite needs to be surface-sealed to prevent Xe penetration
135Xe can diffuse into the graphite and function as a neutron poison
Pyrocarbon sealing was explored, but led to more rapid turnaround

## Slide 22: Materials for MSR systems
Reprocessing materials
The key operations in fuel reprocessing are (1) removal of uranium from the fuel stream for immediate return to the reactor, and (2) removal fission products from the fuel solvent
One severe corrosive environment in this process includes salt at 550C with F2 and UF6, and so that an average valence of 4.5 exists
Other severe corrosive environment is at 650C with salt containing molten alloys of Bi, Li, Th, etc. with HF-F2 gases
The environment must be an inert gas or a vacuum to prevent deterioration of the reactive species of structural material to ensure long-term service
Typically, Ni or Ni-based alloys have been used for containment

## Slide 23: Other Salt Reactor Concepts
AHTR: TRISO particles in graphite compact prismatic core with molten salt coolant
LSFR: solid fueled fast reactor with molten salt coolant
SSR: liquid fueled, non-flowing
Secondary Coolant Loop: may use nitrate, chloride, or fluoroborate salts, with different corrosion
Materials for these systems either experience higher temperatures or higher flux/fluence requirements, and thus Hastelloy-N type materials may not be applicable
Potential options are 9Cr-1MoV coated in Ni, ODS Ni alloys, Ni-based superalloys, ODS Fe alloys, and Mo alloys
Stainless steels can be options for secondary loop

## Slide 24: Chloride Salt Corrosion
Very little corrosion data is present for chloride salt systems
The existing data does not conform to expected trends
The effect of chromium content in the alloy does not seem to be an important factor, and the effect of temperature is not clear
These corrosion rates are comparable to fluoride salts with stainless steel, and are considerably higher than corrosion rates with Hastelloy-N

## Slide 25: Na(ha)-Pu(ha)3

## Slide 26: Na(ha)-U(ha)3

## Slide 27: Summary
Distribution of fission products is a central safety issue, and fission products may be gaseous, solid, or dissolved
Gaseous species can be collected in the cover gas or sparge gas
The materials required fall into three main categories: (1) metallic components for primary and secondary circuits, (2) graphite (or other structural steels) in the core, and (3) materials for molten-salt fuel reprocessing systems
Primary focus on Ni-based alloys for a wide variety of salt-facing components
Graphite can be readily used and has experience in the core
Corrosion challenges change depending upon the reactor type/design
We still know relatively little about molten salts, especially regarding their fundamental thermophysical properties and their long-term corrosion behavior under irradiation