## Slide 1: NE 591: Advanced Reactor Materials
Fall 2021
Dr. Benjamin Beeler

## Slide 2: Last Time

## Slide 3: Research reactors

## Slide 4: USi interaction with Al
U3Si, U3Si2, and USi react with Al to form a single intermetallic compound, U(AlSi)3
The solubility of Al in the USi phases is very low
U(AlSi)3 has a composition intermediate between UAl3 and USi3, both of which are mutually soluble
The amount of Si in the interaction layer is highest for U3Si

## Slide 5: USi interaction with Al
Interaction layer growth is an interdiffusion controlled process, and can be investigated in out of pile experiments
Out-of-pile tests are typically performed at high temperatures (600C) and have shown that interdiffusion is the rate-controlling process in IL growth of silicide–Al dispersion
Fuel temperatures of typical in-pile tests are much lower (<200C) than the out-of-pile tests
Simple extrapolations to the low temperature regime of the IL growth correlations for out-of-pile tests yield orders of magnitude smaller IL thickness values than observed
This implies that thermally activated diffusion must be augmented by fission enhanced diffusion during irradiation

## Slide 6: USi interaction with Al
The compositions in the interaction layer deviate from the exact stoichiometry of U(AlSi)3
This indicates that the reaction products become amorphous during irradiation, which has been observed in in-pile tests
Since the IL is amorphous, U, Al, and Si atoms exist in a mixture without crystalline restriction of stoichiometry
The formation of gas bubbles in the ILs is important because of its potential effects on the IL growth rate
The gas bubbles in the IL, on one hand, reduce the effective diffusion area and thereby reduce the IL growth rate.
On the other hand, they increase the IL volume itself, which results in a higher measured IL growth rate

## Slide 7: Micrographs of irradiated LEU U3Si–Al and U3Si2–Al
The ILs of both fuels are generally uniform in thickness and free of visible fission gas bubbles
The gas bubbles in the unreacted fuel serve as a boundary between the unreacted fuel and the ILs
U3Si has dramatically higher swelling than U3Si2
Both samples have similar burnup and temperature
U3Si–Al
U3Si2–Al

## Slide 8: Micrographs of irradiated HEU U3Si–Al and U3Si2–Al
Gas bubbles are found in ILs of high-burnup HEU USi fuels
These images are from ultra high burnup samples, ~4.5X the previous slide
Thus, likely the formation of fission gas bubbles in the IL is dependent upon fission density
Bubbles in the IL of U3Si2 appear later than in U3Si
U3Si–Al
U3Si2–Al

## Slide 9: Blister Testing
A unique measure for sound fuel performance considered in research and test reactors is ‘blister threshold temperature’ testing with irradiated plates
Because there is neither a gap nor a plenum, no fission gas release is possible outside of the fueled zone
Fission gas and any gas included during fabrication remain in the fueled zone; in particular, fission gases are contained in pores or fission gas bubbles
Gas pressure in large pores and fission gas bubbles, which may be insufficient to cause detrimental creep or yielding of fuel, could instead result in blistering of a fuel plate when the plate is heated to a certain temperature
Two types of mechanisms can be considered for blistering: pore (or void) connection, and pressure rupture of fission gas bubbles

## Slide 10: Blister Testing
In the typical blister test, the sample plate is held at a specified temperature for 30–60 min during each annealing step
The temperature at which blisters form is termed the ‘blister temperature’
Images of a U3Si2–Al dispersion fuel plate after a postirradiation blister test at 450C

## Slide 11: USi Blistering
For typical fuel particle loadings, miniature scale plates of U3Si2 and U3Si were blistered in the range of 515–530C
An increase in fuel loading dropped the blister temperature by about 75C
When boron is added, the blister threshold temperature decreases by about 100C, similar to that observed in UAlx fuels
Boron is added as a burnable absorber in certain research reactor fuel designs as a means of flux/temperature balancing to avoid hot spots
The blister threshold temperature for U–Si intermetallic dispersion fuels is less sensitive both to burnup and to fuel volume loading than UAlx–Al dispersion fuels

## Slide 12: USi Summary
U3Si2 is presently considered the best qualified fuel in terms of uranium loading and performance for research and test reactors
U3Si is unsuitable for a plate-type geometry because of unstable swelling, it is still applicable for fuel rods
The ILs in U3Si2/Al are free of porosity formation at reasonable burnups and the IL growth is considered reasonably slow
Both U3Si and U3Si2 are amorphized under irradiation, but have inherent differences in fission gas bubble growth
U3Si has excessive breakaway swelling, whereas U3Si2 has stable, albeit still large, swelling

## Slide 13: RERTR to UMo
Failure to convert high-power research reactors using HEU to LEU U3Si2 resulted from the need for fuels of even higher uranium density
The fuel development effort has shifted to uranium–molybdenum alloys with Mo content ranging 6–10wt%, in both monolithic and dispersion fuel forms
Since 1997, the U–Mo alloys have been irradiation-tested, driven by US leadership
This program is now called the United States High Performance Research Reactor (USHPRR) Program
Similar programs work in conjuction with the USHPRR in Argentina, Canada, France, South Korea, and Russia

## Slide 14: UMo
It was recognized early on in the development of fast reactor fuels that molybdenum is one of the strongest gamma-stabilizers of the transition-metal elements, even stronger than Zr, and that it enables alloys with U to have relatively high U density
A disadvantage of Mo as an alloying element is that it has higher neutron absorption cross sections than Si and Al, but not sufficiently significant to be problematic
The solubility of Mo extends to 22 wt% (or 41 at.%) in the gamma-phase, but it is limited to a few percent in the alpha and beta-phases.

## Slide 15: UMo Phases
The gamma-phase undergoes a eutectoidal decomposition at 565C, transforming to the dual-phase mixture of the orthorhombic alpha-phase and the ordered tetragonal gamma’-phase which has the nominal stoichiometry of U2Mo
This transformation is slow when the molybdenum content is more than about 6 wt%, so a gamma-phase metastable U–Mo alloy with 6–12 wt% Mo can be obtained by quenching the alloy melt into the gamma-phase

## Slide 16: Gamma Stability
The radiation stability of UMo depends on its ability to retain the gamma phase
At research reactor temperatures, the gamma phase wants to transform into the alpha/gamma’ two phase system
Radiation counteracts the driving thermodynamics by disordering the gamma’ phase, retaining the gamma phase
The critical fission rate is the rate at which the minimum number of displacements that maintain the gamma-phase are in balance with the thermodynamic tendency to transform to the alpha/gamma’-phases

## Slide 17: UMo Fabrication
Dispersion fabrication is unique from monolithic fabrication
UMo dispersion fuels are fabricated in a similar manner to USi dispersion fuels
Both comminution and atomization processes can be applied
The UMo alloy is quite ductile, which poses problems for the comminution process
Alloys can be lightly oxidized to assist in comminution
The comminuted powders have more equiaxially shaped grains and a more homogeneous distribution of grains than the atomized powder fuel because there is no thermal process involved during fabrication
However, they are heavily cold-worked and contain a high concentration of dislocations which can polygonize and serve as nucleation sites for gas bubbles

## Slide 18: UMo Fabrication
The microstructure of the atomized powder consists of a ‘cellular’ solidification structure which is commonly found in rapidly cooled alloys that have a pronounced solidus–liquidus gap
Mo-rich phases solidify first upon cooling
As the cooling progresses, the solid phase volume increases, while, simultaneously, the Mo content in the solid phase decreases
If cooling is too rapid, Mo rich islands will form inside a network of a Mo lean matrix

## Slide 19: UMo Fabrication
The U–Mo fuel uses the same plate fabrication method as other U intermetallic fuels
However, the hot rolling procedure can have significant effects on the performance of the fuel
The thermal process changes particle characteristics and can enhance the interaction between the particles and the matrix

## Slide 20: Fuel Swelling
Fuel swelling by solid fission products is also applicable for U-Mo fuels
The fuel swelling due to fission gases is unique in the UMo system
U–Mo swelling, specifically, swelling by gas bubble growth, is known to have two distinct rates: slow at low burnup and much faster at high burnup
The phenomenon underlying the transition is grain refinement or ‘recrystallization’ of the gamma-phase U–Mo
After this transition, gas bubble agglomeration accelerates, resulting in faster swelling

## Slide 21: Recrystallization + Swelling
The evolution of fuel microstructure by fission gas bubble formation and growth is shown with three different burnups
In an SEM, fission gas bubbles first appear along grain boundaries, with no large bubbles in the fuel
35% BU
65% BU
80% BU

## Slide 22: Fission Gas Superlattice
TEM analysis has identified in the low BU regime a fission gas superlattice of 2nm sizes bubbles
As the bubbles are small, even though their number density is large, these bubbles are too small to produce much fuel volume increase
The Young-Laplace equation denotes a force balance, and the ideal gas law gives an approximation of the pressure
Thus, these small bubbles are highly pressurized and contain large amounts of gas

## Slide 23: Recrystallization + Swelling
As burnup increases (2.5–3.5E27 fissions/m3), the bubble population increases in the grain boundaries and additional bubbles progressively appear at newly formed grain boundaries as grain refinement continues
At this stage, the average bubble size also increases with fission density as the number density increases, both of which increase the fuel swelling rate
35% BU
65% BU
80% BU

## Slide 24: Recrystallization + Swelling
At higher burnup, large bubbles uniformly span the entire fuel cross section as the grain refinement is nearing completion
35% BU
65% BU
80% BU

## Slide 25: UMo Gaseous Swelling
Total swelling of U–Mo fuel is obtained from plate thickness changes before and after irradiation
The gas bubble swelling is obtained by subtracting the solid fission product swelling
The data can be fit to a linear function at low fission density, and a quadratic function at higher fission density

## Slide 27: UMo-Al Interaction
A major complication in U–Mo alloy dispersion in Al is the reaction between U–Mo and Al
Under certain irradiation conditions, fission gas bubble growth in this reaction product is sufficient to cause fuel plate failure
A small amount of silicon added to the matrix aluminum has been found to be a promising remedy to this problem
The U–Mo monolithic fuel, in which a U–Mo thin foil is sandwiched between cladding and directly bonded to cladding, is currently under development and has the advantage of providing higher U density than the dispersion form while essentially eliminating the problem related to reaction products between the fuel and matrix