## Slide 1: Fuel Types
NE 591

## Slide 2: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator

## Slide 3: Fuel is limited to select elements
A fissionable nuclide is capable of undergoing fission (even with a low probability) after capturing a high energy neutron
A fissile nuclide is capable of sustaining a nuclear fission chain reaction with neutrons of any energy
A fertile material is a material that, although not itself fissionable, can be converted into a fissile nuclide by neutron absorption and subsequent nuclei conversions.
The Ronen fissile rule states that for a heavy element with 90 ≤ Z ≤ 100, its isotopes with neutrons (A-Z) = 2 × Z – N, where N = 43 ±2 are fissile (with some exceptions)

## Slide 4: Potential fuel candidates
The heavy elements with 90 ≤ Z ≤ 100
  Thorium (Th), Protactinium (Pa), Uranium (U), Neptunium (Np), Plutonium (Pu), Americium (Am), Curium (Cm), Berkelium (Bk), Californium (Cf), Einsteinium (Es) and Fermium (Fm)
Lets apply the fissile rule to U (2 × Z – N)
  (A-Z) = 2 Z – (43 ± 2)
  (A-Z) = 2 × 92 – [41, 42, 43, 44, 45] = [143, 142, 141, 140, 139] neutrons
  So, U-231 through U-235 should be fissile

## Slide 5: There are only four fissile nuclides that are practical for nuclear fuel
U-235
  Naturally occurs in uranium in small amounts (0.7%). Can be enriched
Pu-239
  Bred from U-238 by neutron capture
Pu-241
  Bred from Pu-240 (which comes from Pu-239) by neutron capture
U-233
  Bred from Th-232 by neutron capture

## Slide 6: Why not use pure uranium metal?
Pure uranium has three phases
  α-phase is orthorhombic
  β-phase is tetragonal
  g-phase is body-centered cubic
  During thermal cycling, pure uranium dramatically swells
  Alpha U has both anisotropic thermal expansion and anisotropic irradiation growth

## Slide 7: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  Mixed oxide (MOX)
  Accident tolerant/Advanced Technology Fuel (ATF)
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
UN – Lead Cooled Fast Reactors

## Slide 8: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients that lead to deleterious behavior
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 9: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes

## Slide 10: Uranium Dioxide (UO2)
Good!
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant
    no amorphization
    Can incorporate a large number of fission products as substitutional defects

## Slide 11: Uranium Dioxide (UO2)
Bad!
  Brittle
    thermal stress fractures, fragmentation
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling
  Higher stored thermal energy than other fuel materials

## Slide 12: Uranium Dioxide (UO2)
Critical Phenomena
  Thermal conductivity (and degradation)
  Fission gas release, leading to pressure increase inside the cladding
  Fuel fragmentation and relocation under transients
  Bambooing creating stress concentrations
All 98 operational reactors in US utilize UO2

## Slide 13: Mixed Oxides (MOX)
Can be combined with PuO2 for a mixed oxide (MOX) fuel for use in fast reactors
Allows to burn excess weapons grad plutonium
About 30 reactors in Europe currently utilize a partial MOX core
Similar behavior to UO2, but different neutronics, fission gas release, thermal conductivity, etc.
Less common is inclusion of minor actinides in MOX to burn waste

## Slide 14: Accident Tolerant Fuel/Advanced Technology Fuel
Kept the acronym, changed the concept
USi fuels (U3Si2)
  A metal-ish compound, with higher thermal conductivity, higher uranium density
  Complex crystal structure (10 atoms unit cell) with effectively two sub-lattices
  Amorphizes at low temperatures
  Poor oxidation resistance
  Will require improved cladding, liners/coatings or fuel dopants

## Slide 15: Accident Tolerant Fuel/Advanced Technology Fuel
Cr-doped UO2
  Larger grain size, theoretically reduced fission gas release
  Cr changes the O potential present within the fuel, changing defect concentrations and mobilities
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 16: Uranium-Zirconium (UZr)
Utilized in sodium cooled fast reactors (SFRs)
  EBR I, EBR II
Varied crystal structure and compositional environment
Easily alloyed with Pu, minor actinides (MA)
Can function as a breeder/burner fuel
Sodium coolant
Fe-based cladding

## Slide 17: Uranium-Zirconium (UZr)
Alloy metallic U with Zr to increase the melting point and to stabilize the high temperature body-centered cubic phase
Interesting phenomena
  30-50% swelling
  Constituent redistribution
  Alpha tearing
  FCCI

## Slide 18: Uranium-Zirconium (UZr)
Good!
  High thermal conductivity
  Stability to high burnups (> 20%)
  Flexible composition
  Inherent safety- negative reactivity feedback
  Good compatibility with Na coolant
Bad!
  Low melting point
  Dramatic fuel swelling that must be accounted for
  Incredibly complex microstructures/unpredictable behavior
  Fuel-Clad Chemical Interaction
  Very easily oxidized

## Slide 19: Uranium-Molybdenum (UMo)
New fuel being qualified for research reactors
Fuel foil, with Zr diffusion barrier, Al cladding
Will be utilized in ATR, NBSR, MITR, MURR

## Slide 20: Uranium-Molybdenum (UMo)
Microstructural phenomena of interest:
  Decomposition
  Fission Gas Superlattice
  Recrystallization
  Inter-diffusion region
  Carbides

## Slide 21: UC/UCO TRISO Fuels
TRISO: TRistructural ISOtropic particle fuel
Layered fuel in mm-sized particles
Layers:
  Fuel Kernel
  Buffer
  Inner Pyrolitic Carbon (IPyC)
  SiC
  Outer Pyrolitic Carbon (OPyC)

## Slide 22: UC/UCO TRISO Fuels
Can appear as UC, U2C3, or UC2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Rapidly corrodes in water
  Reacts with some cladding

## Slide 23: UC/UCO TRISO Fuels
High temperature gas reactors (HTGR) or molten salt reactors (MSRs)
Pebble bed and prismatic types
Particles are agglomerated with graphite into a larger pebble, or into a cylindrical block
Current designs utilize UCO, which is a heterogeneous mixture of UO2 and UC fuel
Helium cooled gas or molten salt cooled

## Slide 24: UC/UCO TRISO Fuels
Each individual pebble acts as its own containment, and allows fuels to go to much higher burnups and higher temperatures than UO2
Highly reliant on accurate fabrication processes that create high integrity, uniform layers and spherical particles
Integrity of the SiC is key for fission product retention