## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2025

## Slide 2: Last Time
Solid mechanics predicts the deformation of a body from its applied load
Elastic deformation and plastic deformation
Concepts of stress and strain
Elastic moduli and Elastic constants
Work hardening/strain hardening
Toughness, ductility, DBTT, etc.

## Slide 3: Mechanics

## Slide 4: Develop constitutive relations for thick-walled
We assume small strains, so the strain is defined with respect to displacement: u
We assume isotropic material response:

## Slide 5: Small strain theory
In continuum mechanics, the infinitesimal strain theory is a mathematical approach to the description of the deformation of a solid body in which the displacements of the material particles are assumed to be much smaller than any relevant dimension of the body so that its geometry and the constitutive properties of the material at each point of space can be assumed to be unchanged by the deformation
With this assumption, the equations of continuum mechanics are considerably simplified
The small strain theory is commonly adopted in civil and mechanical engineering for the stress analysis of structures built from relatively stiff elastic materials

## Slide 6: Stress within a pressurized cylinder that has thick walls (radius/thickness<20)
The cylinder as an inner radius Ri and an outer Radius Ro
We assume there is no shear stress, so σrz = 0
We will begin with the r equation
Now we need our constitutive law
We combine these equations to get

## Slide 7: Develop equations for the stress within a pressurized cylinder with thick walls
We need one more relationship from the definition of the strain
From the previous slide, we have
If we combine these, we get
Again, from the previous slide
We end up with

## Slide 8: We now have an ODE so we can solve to get the stress
Our boundary conditions are σrr(Ri) = -p and σrr(Ro) = 0
After integrating twice, we get
From σrr, we can get σθθ from
From the end condition, we determine σzz
(a)
(b)
(c)

## Slide 9: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  Ri = 0.52, Ro = 0.58 cm, σy = 381 MPa
Which stress is the largest?
  σθθ
At what position r will the hoop stress be the largest?
  r = Ri = 0.52 cm
What is the stress at p = 5 MPa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 46.0 MPa
What is the stress at p = 9 Mpa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 82.7 Mpa
Again, we don’t even get close to yielding

## Slide 10: We’ve now solved this same problem assuming thin and thick-walled cylinders

## Slide 11: THERMO-Mechanics

## Slide 12: Thermal Expansion
As the temperature increases, atoms have larger vibrations, causing the material to expand
This expansion doesn’t raise the energy of the material when unrestrained
This expansion can be treated as a strain, but as one that doesn’t cause stress

## Slide 13: Thermal Expansion
In isotropic materials, thermal expansion happens equally in all directions and is linear with temperature
In this equation
  T is the current temperature
  T0 is the temperature the original size was measured
  α is the linear thermal expansion coefficient
  I is the identity tensor

## Slide 14: Thermal Expansion
Though thermal expansion doesn’t directly cause stress, it can still lead to thermal stress

## Slide 15: What is the stress in a thin constrained rod of length L when it is heated to ΔT?
The rod has a Young’s modulus of E and an expansion coefficient of α

## Slide 16: The large temperature gradient within a fuel pellet results in large thermal stresses

## Slide 17: Consider the constitutive relations plus T
We assume small strains, so the strain is defined as
We assume isotropic material response, so

## Slide 18: Consider a cylinder with thermal expansion but not pressure
Similar to the equations we worked through before
Solving this ODE:

## Slide 19: What is the hoop stress in the cladding?
r
Ri
Rf

## Slide 20: Where is hoop stress equal to zero?

## Slide 21: The linear temperature gradient across the cladding causes axial thermal stresses

## Slide 22: Same approach to the thermal stress in a fuel pellet
The thermal stress is due to the temperature gradient

## Slide 23: Solve this stress ODE
The boundary conditions are:
Once we solve it, we obtain
Then we can solve the hoop stress
The axial stress is more complicated to obtain, but you end up with

## Slide 24: The fuel temperature gradient causes large thermal stresses

## Slide 25: Example

## Slide 26: How far do fuel cracks extend?
E = 200 GPa, ν = 0.345, α = 11.0e-6 1/K, σfr = 130 MPa, ΔT = 550 K
Solve for η
  – σfr / σ* = 1 – 3 η2
  3 η2 = 1 + σfr / σ*
  η = ( (1 + σfr / σ*)/3 )½
σ* = 11.0e-6*200*550/(4*(1 – 0.345) ) = 461.8 MPa
η = sqrt( (1 + 130/461.8)/3 ) = 0.65

## Slide 27: Summary
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin-walled cylinder
  Thick-walled cylinder
Increases in temperature cause most materials to expand
We call this thermal expansion, which is a strain that doesn’t inherently cause stress
Thermal expansion can cause stress when
  Deformation is constrained
  There are gradients in the expansion coefficient
  There is a temperature gradient
We developed analytical equations for thermal stresses
  in the cladding
  in the fuel