## Slide 1: Overview and Introduction
NE 533: Nuclear Fuel Performance
Spring 2025
Dr. Benjamin Beeler

## Slide 2: Overview

## Slide 3: Access to Course Resources
Everything will be hosted on Moodle, classes conducted in-person and via Zoom
To access Moodle courses, log on to WolfWare with your Unity ID and password
Lecture recordings will be available via Panopto
Lecture PDFs will be uploaded to Moodle after each class
Office hours will be held in my office on Wednesdays 9-10 am
Additional office hours (in person or virtual) can be scheduled via email
I encourage all to reach out to me with any questions or concerns
Have invited everyone to a Slack channel for ease of communication

## Slide 4: Syllabus
Course Overview
In this course we will study the basic role of fuel in reactor operation and understand how the fuel impacts heat generation and transport to the coolant. The course will begin with an overview of different fuels and the fabrication processes required to construct nuclear fuel. This will include various fuel types and geometries, with a focus on light water reactor fuel and cladding. Thermal transport, mechanics, and thermomechanics affecting fuel behavior will be introduced, and methods to solve the governing equations numerically and analytically will be developed. Subsequently, changes in the fuel and cladding material that degrade the performance of the fuel will be examined. Finally, the knowledge gained throughout the course will be utilized to conduct fuel performance simulations with MOOSE.
Learning Outcomes
By the end of this course, the student should be able to:
Summarize the basics of fuel fabrication
Evaluate traditional and alternative nuclear fuel types and their application
Determine the rate at which heat is transported to the coolant from the fuel
Determine the stress state within both the fuel and the cladding
Describe the most important microstructural changes that take place in the fuel and cladding and how they impact fuel performance
Critically analyze existing literature in fuel performance modeling
Use an existing fuel performance code

## Slide 5: Topical Outline
Module 1: Fuels, Systems, Heat Conduction Equation, and Numerical Discretization
Module 2: Mechanics, Thermomechanics, and Intro to MOOSE
Module 3: Fission Products, Swelling, and Pellet Cladding Interactions
Module 4: Corrosion, Accidents, and Advanced Fuels
Modules contain 4-5 lectures, with an exam at the end of the module
Graded Exercises
  Four exams (64%)
  One paper presentation project (16%)
  One MOOSE-based project (in three parts) (20%)
Please note: the course schedule is subject to change.

## Slide 6: Exams, Projects, Grading
Using the standard NCSU +/- grading system
Four exams will be conducted closed book (with cheat sheet) and held during normal class hours
Will work with distance students to schedule exams
Will do problem session lecture prior to exam periods
Project presentations will be via PPT and conducted during normal class hours
No final exam

## Slide 7: Paper Project
Will assign a paper related to the course
Will deliver a 15-minute presentation providing a critical review of the paper
This is basically a mini QE Part 1, without the report
If you have a topic that you want the paper to address, I will do my best to accommodate that
Will occur around the midpoint of the semester
Accounts for 16% of your grade

## Slide 8: MOOSE Project
Computational project will be via MOOSE, where code (inputs/outputs) will be submitted in addition to a writeup
Project is split into 3 parts, each with a submission
The submissions are building upon each other
  Submission 1 = Part 1; Submission 2 = Part 1+ Part 2; Submission 3 = All three parts
  Grading is performed on the entirety of each submission
  Thus, you need to fix mistakes made in Part 1 for subsequent submissions
  MOOSE project is 20% of your grade, with Submission 1 = 5%; Submission 2 = 5%; Submission 3 = 10%
I am being this granular because some of this has been unclear previously

## Slide 9: Feedback
No course is static, and I need your feedback to modify/update the course to meet the needs of the students
I will be reaching out for feedback periodically throughout the semester
Completion of feedback will gain extra credit (+5) on exams

## Slide 10: Miscellaneous
My exams are known to be time-consuming but not hard, so be familiar with the material and don’t overly rely on your cheat sheet
My slides are generally information-dense, so if I am going too fast, stop me
Always ask questions, I don’t know if you aren’t getting it unless you tell me
I want to help you succeed in this class, so get help if you need it
Finally, I have two speech impediments and a southern accent
I stutter and will struggle through some lectures; bear with me and ask me to repeat something if it is unintelligible

## Slide 11: Brief Bio/Background
Computational Nuclear Materials Scientist
Expertise in advanced nuclear fuels
Ph.D. in Nuclear Engineering from Georgia Tech
Previously a staff scientist at Idaho National Laboratory in Fuel Modeling and Simulation Group
Atomistic simulations: density functional theory and molecular dynamics

## Slide 12: My viewpoint/approach
Scientifically informed engineering is a multiscale problem
Critical phenomena need to be identified from the macroscale, and informed from the lower length scales
Perform good science, sometimes for science’s sake, but often to address a key engineering problem or need

## Slide 13: tell me about yourself
Name, including how to pronounce it ‘properly’
Where you’re from
PhD/Masters/ABM
Advisor and research topic (if applicable)
Anything else???

## Slide 14: Introduction

## Slide 15: Complete nuclear fuel cycle

## Slide 16: Emphasis on In-Reactor Behavior of Fuel
The full reactor system is complex and substantial, and there are separate NE courses covering this area
Although the fuel is a relatively small part of a reactor system, it determines thermal power, which drives electric power generation
The performance of the fuel is measured by:
  How much heat is delivered to the coolant
  The length of time it operates without any problems
  How well it performs during an accident

## Slide 17: How much heat is delivered to the coolant?
Heat generated by fuel
Heat transport is related to thermal conductivity
In single crystal, pristine materials, thermal conductivity is reasonably straightforward
In dynamic, radiation environments, thermal conductivity degrades, fission gas bubbles form, grain boundaries are generated and destroyed, changing geometries, evolving chemical compositions, etc.
How does thermal conductivity vary?

## Slide 18: The length of time fuel operates without any problems
There are 94 operating nuclear reactors in the US, producing ~20% of the electricity
The net capacity factor is the ratio of an actual electrical energy output to the maximum possible electrical energy output over a period of time
Nuclear reactor capacity factor is ~92% over the past decade
The ability to maintain a high capacity factor, largely by limiting shutdown time, is key in making nuclear power economical
Fuel is the primary component forcing reactor downtime

## Slide 19: Fuel behavior during accidents
In addition to normal operating conditions, the behavior of the fuel during accidents is of critical importance
Predictable, and hopefully stable, behavior is desired during a variety of accident scenarios
Even low impact accidents are detrimental to public opinion surrounding nuclear energy
Fukushima

## Slide 20: All of these factors together represent what we call “fuel performance”
Fuel Performance
Heat generation
Fuel problems causing unscheduled outages
Fuel behavior during an accident

## Slide 21: Fuel types

## Slide 22: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator

## Slide 23: Fuel is limited to select elements
A fissionable nuclide is capable of undergoing fission (even with a low probability) after capturing a high energy neutron
A fissile nuclide is capable of sustaining a nuclear fission chain reaction with neutrons of any energy
A fertile material is a material that, although not itself fissionable, can be converted into a fissile nuclide by neutron absorption and subsequent nuclei conversions.
The Ronen fissile rule states that for a heavy element with 90 ≤ Z ≤ 100, its isotopes with neutrons (A-Z) = 2 × Z – N, where N = 43 ±2 are fissile (with some exceptions)

## Slide 24: Potential fuel candidates
The heavy elements with 90 ≤ Z ≤ 100
  Thorium (Th), Protactinium (Pa), Uranium (U), Neptunium (Np), Plutonium (Pu), Americium (Am), Curium (Cm), Berkelium (Bk), Californium (Cf), Einsteinium (Es) and Fermium (Fm)
Let’s apply the fissile rule to U (2 × Z – N)
  (A-Z) = 2 Z – (43 ± 2)
  (A-Z) = 2 × 92 – [41, 42, 43, 44, 45] = [143, 142, 141, 140, 139] neutrons
  So, U-231 through U-235 should be fissile

## Slide 25: There are only four fissile nuclides that are practical for nuclear fuel
U-235
  Naturally occurs in uranium in small amounts (0.7%). Can be enriched
Pu-239
  Bred from U-238 by neutron capture
Pu-241
  Bred from Pu-240 (which comes from Pu-239) by neutron capture
U-233
  Bred from Th-232 by neutron capture

## Slide 26: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients that lead to deleterious behavior
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 27: Why not use pure uranium metal?
Pure uranium has three phases
  α-phase is orthorhombic
  β-phase is tetragonal
  g-phase is body-centered cubic
  During thermal cycling, pure uranium dramatically swells
  Alpha U has both anisotropic thermal expansion and anisotropic irradiation growth

## Slide 28: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  Mixed oxide (MOX)
  Accident tolerant/Advanced Technology Fuel (ATF)
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
UN – Lead Cooled Fast Reactors
Other

## Slide 29: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes