## Slide 1: Development of a grain growth model for U3Si2 using experimental data, phase field simulation and molecular dynamics
Yuqing Huang
NE 591

## Slide 2: Grain growth
Assuming the only driving force is curvature and there is no significant resistive pressure.
K =
is average grain size
K is kinetic parameter
is geometric constant
is average grain boundary mobility
is average grain boundary energy

## Slide 3: Cataloge
Determination of the average grain boundary energy
Determination of the kinetic parameter
Determination of the mobility

## Slide 4: Determination of the average grain boundary energy

## Slide 5: Determination of the average grain boundary energy
Average grain boundary energy is obtained from existing molecular dynamics data

## Slide 6: Determination of the average grain boundary energy
The average grain boundary energy results from the sum of the enthalpy of formation per unit area and entropy of formation per unit area

## Slide 7: Determination of the kinetic parameter

## Slide 8: Determination of the kinetic parameter
Kinetic parameter follows an Arrhenius expression
is prefactor
Q is activation energy

## Slide 9: Determination of the kinetic parameter
Isothermal annealing was carried out at one lamella(U3Si2) at 673K to measure the average grain size at 8 times to up to 86 min and then obtain the kinetic parameter at 673K by equation below.

## Slide 10: Determination of the kinetic parameter
Other two samples of lamella(U3Si2) were annealed at a given temperature until it crystallized and initial image was taken
The sampled was heated and maintained at that temperature for a set amount of time to allow some grain growth, before taking another image.

## Slide 11: Determination of the kinetic parameter
Varying the values of activation energy to obtain
With determined and Q to obtain average grain size
The minimum error was found to occur when Q = 0.33 eV and then

## Slide 12: Uncertainty

## Slide 13: Determination of the mobility

## Slide 14: The phase field model
The phase field grain growth model uses phase field variables to describe grain

## Slide 15: The phase field model
The evolution of these variables depends on the change in Gibbs free energy
Where is the phase mobility
Where m is scalar multiplier, K is gradient energy coefficient

## Slide 16: Simulation details
Domain size:
Initial number of grains: between 500 and 600
Algorithm: Grain Tracker Algorithm
Boundary: zero flux condition
Boundary width: 3nm
Element size: to
Time steps: 100 s ~ 1600s
Temperature: 673K
Mobility:

## Slide 17: Determination of shape factor
For each different initial grain configuration

## Slide 18: Comparison surface data and volume data

## Slide 19: Determination of the grain boundary mobility
The average mobility can be expressed as an Arrhenius expression

## Slide 20: Uncertainty
Notes: The uncertainty for M0 is from uncertainty in the values of K, 𝛼,𝛾 ̅ and Q. Generated 100000 random values from each random variable and resultant is shown in the figure on the left side. The dash line in the left figure is only consider Q is random variable. Ae we can see that the distribution do not have significant change, which means that the Q is dominates source of uncertainty.

## Slide 21: Comparison with UO2

## Slide 22: Conclusion and future work
Conclusion
Developed a model for normal grain growth in U3Si2
Average grain boundary energy obtained from creating a fit to temperature of values calculated using MD simulation
Activation energy estimated by comparing model predictions with the measured values
Shape factor determined using 3D phase field grain growth simulation
Future work
The resistive pressure should be considered
Other drive force can be considered
More data from simulations and experiments should be used

## Slide 23
Thank you!