## Slide 1: Nuclear Fuel Performance
NE-591-010
Spring 2021

## Slide 2: Mechanics

## Slide 3: Determine the stress and strain throughout a body

## Slide 4: The stress divergence equation derivation
Generalized momentum conservation:
Considering a cubic element, surface forces act on the walls of the cube
Force on a wall is the product of the stress and the surface area
  For wall at dx, approximate stress via Taylor expansion

## Slide 5: Simplified Cauchy for our typical system
Assumption 1: We have a static body
Assumption 2: Gravity is negligible
Assumption 3: The problem is axisymmetric
r
q
z

## Slide 6: Consider the material response of the axisymmetric body
We assume small strains (elasticity), so the strain is defined as
We assume isotropic material response, so

## Slide 7: Solve for the stress throughout a pressurized cylinder (cladding tube) with thin walls
Because our cylinder has such thin walls (δ = thickness), we can simplify everything to simple force balance
The hoop stress is the force exerted circumferentially in both directions on every particle in the cylinder wall
First, we need the Force per unit length due to the pressure
Utilize force to hoop stress relation:
Then we equate the forces and solve for the hoop stress

## Slide 8: Find the other two stresses for a thin walled cylinder
To find the stress in the z-direction we do another force balance
Again, we equate the forces and solve for the stress
Last, the stress on the inside of the wall is –p and on the outside is zero, so the average
Ftop
Fwall

## Slide 9: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  R = 0.55 cm, δ = 0.05 cm, σy = 381 MPa
The largest stress will be the hoop stress
The hoop stress is P*(0.55/.05)
  For 5 MPa, σθ = 55 Mpa
  For 9 MPa, σθ = 99 Mpa
With these pressures, we don’t come even close to the yield stress of the cladding

## Slide 10: Stress within a pressurized cylinder that has thick walls (radius/thickness<20)
The cylinder as an inner radius Ri and an outer Radius Ro
We assume there is no shear stress, so σrz = 0
We will begin with the r equation
Now we need our constitutive law
We combine these equations to get

## Slide 11: Develop equations for the stress within a pressurized cylinder with thick walls
We need one more relationship from the definition of the strain
From the previous slide, we have
If we combine these, we get
Again, from the previous slide
We end up with

## Slide 12: We now have an ODE so we can solve to get the stress
Our boundary conditions are σrr(Ri) = -p and σrr(Ro) = 0
After integrating twice, we get
From σrr, we can get σθθ from
From the end condition, we determine σzz
(a)
(b)
(c)

## Slide 13: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  Ri = 0.52, Ro = 0.58 cm, σy = 381 MPa
Which stress is the largest?
  σθθ
At what position r will the hoop stress be the largest?
  r = Ri = 0.52 cm
What is the stress at p = 5 MPa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 46.0 MPa
What is the stress at p = 9 Mpa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 82.7 Mpa
Again, we don’t even get close to yielding

## Slide 14: We’ve now solved this same problem assuming thin and thick walled cylinders

## Slide 15: THERMO-Mechanics

## Slide 16: Thermal Expansion
As the temperature increases, atoms have larger vibrations, causing the material to expand
This expansion doesn’t raise the energy of the material when unrestrained
This expansion can be treated as a strain, but as one that doesn’t cause stress

## Slide 17: Thermal Expansion
In isotropic materials, thermal expansion happens equally in all directions and is linear with temperature
In this equation
  T is the current temperature
  T0 is the temperature the original size was measured
  α is the linear thermal expansion coefficient
  I is the identity tensor

## Slide 18: Thermal Expansion
Though thermal expansion doesn’t directly cause stress, it can still lead to thermal stress

## Slide 19: What is the stress in a thin constrained rod of length L when it is heated to ΔT?
The rod has a Young’s modulus of E and an expansion coefficient of α

## Slide 20: The large temperature gradient within a fuel pellet results in large thermal stresses

## Slide 21: Consider the material response of the axisymmetric body
We assume small strains, so the strain is defined as
We assume isotropic material response, so

## Slide 22: Consider a cylinder with thermal expansion but not pressure
Similar to the equations we worked through before
Solving this ODE:

## Slide 23: What is the hoop stress in the cladding?
r
Ri
Rf

## Slide 24: Where is hoop stress equal to zero?

## Slide 25: The linear temperature gradient across the cladding causes axial thermal stresses

## Slide 26: Same approach to the thermal stress in a fuel pellet
The thermal stress is due to the temperature gradient

## Slide 27: Solve this stress ODE
The boundary conditions are:
Once we solve it, we obtain
Then we can solve the hoop stress
The axial stress is more complicated to obtain, but you end up with

## Slide 28: The fuel temperature gradient causes large thermal stresses

## Slide 29: How far do fuel cracks extend?
E = 200 GPa, ν = 0.345, α = 11.0e-6 1/K, σfr = 130 MPa, ΔT = 550 K
Solve for η
  – σfr / σ* = 1 – 3 η2
  3 η2 = 1 + σfr / σ*
  η = ( (1 + σfr / σ*)/3 )½
σ* = 11.0e-6*200*550/(4*(1 – 0.345) ) = 461.8 MPa
η = sqrt( (1 + 130/461.8)/3 ) = 0.65

## Slide 30: Summary
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin walled cylinder
  Thick walled cylinder
Increases in temperature cause most materials to expand
We call this thermal expansion, which is a strain that doesn’t inherently cause stress
Thermal expansion can cause stress when
  Deformation is constrained
  There are gradients in the expansion coefficient
  There is a temperature gradient
We have analytical equations for thermal stresses in the cladding and in the fuel