## Slide 1: Nuclear Fuels
NE 201 Fall 2022
Dr. Benjamin Beeler

## Slide 2: Fuel is the Heat Source
Although the fuel is a relatively small part of a reactor system, it determines thermal power, which drives electric power generation
The performance of the fuel is measured by:
  How much heat is delivered to the coolant
  The length of time it operates without any problems
  How well it performs during an accident

## Slide 3: How much heat is delivered to the coolant?
Heat transport is related to thermal conductivity
In single crystal, pristine materials, thermal conductivity is reasonably straightforward
In dynamic, radiation environments, thermal conductivity degrades, fission gas bubbles form, grain boundaries are generated and destroyed
How does thermal conductivity vary?

## Slide 4: The length of time fuel operates without any problems
There are 98 operating nuclear reactors in the US, producing 20% of the electricity
The net capacity factor is the ratio of an actual electrical energy output to the maximum possible electrical energy output over a period of time
Nuclear reactor capacity factor is ~92% over the past decade
The ability to maintain high capacity factor, limit shutdown time, is key in making nuclear power economical
Fuel is the primary component forcing reactor downtime

## Slide 5: Fuel behavior during accidents
In addition to normal operating conditions, the behavior of the fuel during accidents is of critical importance
Predictable, and hopefully stable, behavior is desired during a variety of accident scenarios
Even low impact accidents are detrimental to public opinion surrounding nuclear energy
Fukushima

## Slide 6: All of these factors together represent what we call “fuel performance”
Fuel Performance
Heat generation
Fuel problems causing unscheduled outages
Fuel behavior during an accident

## Slide 7: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients that lead to deleterious behavior
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 8: Why not use pure uranium metal?
Pure uranium has three phases
  α-phase is orthorhombic
  β-phase is tetragonal
  g-phase is body-centered cubic
  During thermal cycling, pure uranium dramatically swells
  Alpha U has both anisotropic thermal expansion and anisotropic irradiation growth

## Slide 9: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  Mixed oxide (MOX)
  Accident tolerant/Advanced Technology Fuel (ATF)
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
UN – Lead Cooled Fast Reactors
Other

## Slide 10: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes

## Slide 11: Uranium Dioxide (UO2)
Good Characteristics
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant
    no amorphization
    Can incorporate a large number of fission products as substitutional defects

## Slide 12: Uranium Dioxide (UO2)
Bad Characteristics
  Brittle (thermal stress fractures, fragmentation)
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling
  Higher stored thermal energy than other fuel materials

## Slide 13: Uranium Dioxide (UO2)
Critical Phenomena
  Thermal conductivity (and degradation)
  Fission gas release, leading to pressure increase inside the cladding
  Fuel fragmentation and relocation under transients
  Bambooing creating stress concentrations
All 98 operational reactors in US utilize UO2

## Slide 14: Mixed Oxides (MOX)
Can be combined with PuO2 for a mixed oxide (MOX) fuel for use in fast reactors
Allows to burn excess weapons grade plutonium
About 30 reactors in Europe currently utilize a partial MOX core
Similar behavior to UO2, but different neutronics, fission gas release, thermal conductivity, etc.
Less common is inclusion of minor actinides in MOX to burn waste

## Slide 15: Accident Tolerant Fuel
Cr-doped UO2
  Larger grain size, theoretically reduced fission gas release
  Cr changes the O potential present within the fuel, changing defect concentrations and mobilities
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 16: Uranium-Zirconium (UZr)
Utilized in sodium cooled fast reactors (SFRs)
  EBR I, EBR II
Varied crystal structure and compositional environment
Easily alloyed with Pu, minor actinides (MA)
Can function as a breeder/burner fuel
Sodium coolant
Fe-based cladding

## Slide 17: Uranium-Zirconium (UZr)
Alloy metallic U with Zr to increase the melting point and to stabilize the high temperature body-centered cubic phase
Interesting phenomena
  30-50% swelling
  Constituent redistribution
  Alpha tearing
  FCCI

## Slide 18: Uranium-Zirconium (UZr)
Good Characteristics
  High thermal conductivity
  Stability to high burnups (> 20%)
  Flexible composition
  Inherent safety- negative reactivity feedback
  Good compatibility with Na coolant
Bad Characteristics
  Low melting point
  Dramatic fuel swelling that must be accounted for
  Incredibly complex microstructures/unpredictable behavior
  Fuel-Clad Chemical Interaction
  Very easily oxidized

## Slide 19: Uranium-Molybdenum (UMo)
New fuel being qualified for research reactors
Fuel foil, with Zr diffusion barrier, Al cladding
Will be utilized in ATR, NBSR, MITR, MURR

## Slide 20: Uranium-Molybdenum (UMo)
Microstructural phenomena of interest:
  Decomposition
  Fission Gas Superlattice
  Recrystallization
  Inter-diffusion region
  Carbides

## Slide 21: UC/UCO TRISO Fuels
TRISO: TRistructural ISOtropic particle fuel
Layered fuel in mm-sized particles
Layers:
  Fuel Kernel
  Buffer
  Inner Pyrolitic Carbon (IPyC)
  SiC
  Outer Pyrolitic Carbon (OPyC)

## Slide 22: UC/UCO TRISO Fuels
Can appear as UC, U2C3, or UC2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Rapidly corrodes in water
  Reacts with some cladding

## Slide 23: UC/UCO TRISO Fuels
High temperature gas reactors (HTGR) or molten salt reactors (MSRs)
Pebble bed and prismatic types
Particles are agglomerated with graphite into a larger pebble, or into a cylindrical block
Current designs utilize UCO, which is a heterogeneous mixture of UO2 and UC fuel
Helium cooled gas or molten salt cooled

## Slide 24: UC/UCO TRISO Fuels
Each individual pebble acts as its own containment, and allows fuels to go to much higher burnups and higher temperatures than UO2
Highly reliant on accurate fabrication processes that create high integrity, uniform layers and spherical particles
Integrity of the SiC is key for fission product retention

## Slide 25: Molten Salt Reactors
Molten Salt Reactor
  Utilizes flowing fuel salt (i.e., UF4-ZrF4-KF) with a secondary molten salt coolant loop (FLiBe)
  MSRE at ORNL, some modern designs
Stable Salt Reactor
  Utilizes fuel that is dissolved in molten salts (NaCl-(U/Pu)Cl3), contained in rods
  Molten salt coolant (NaF-ZrF, FLiBe, FLiNaK, etc.)
Can mix other actinides into the fuel in order to burn waste
Designed to be inherently safe (passive)
Molten salt corrosion is a big problem, as well as the lack of information on thermophysical properties of complex salt

## Slide 26: CANDU Reactors
Canada Deuterium Uranium: pressurized heavy water reactor
Natural uranium, as UO2, as the fuel source
Heavy water is the coolant, has a lower absorption of neutrons
Fuel pins are horizontal, as opposed to vertical
CANDU can be refueled online
Removes costs associated with enrichment

## Slide 27: UN – Lead Cooled Reactors
Fuel can appear as UN, U2N3, or UN2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Corrodes in water
  Reacts with some cladding
  Difficult to manufacture
  Requires N-enrichment
Pb or Pb-Bi metal coolant
Operates in a fast spectrum

## Slide 28: Unique Fuel Designs
Lightbridge
  High Zr content UZr alloy
  Cruciform geometry fuel rods, combined into fuel elements
Kairos
  TRISO particle compacts with low density core
  Float in molten salt coolant for online refueling
NASA/LANL
  UMo fuel for space reactors: KRUSTY

## Slide 29: Fuel Summary Table
Property | UZr | UO2 | UC | UN | U3Si2
Corrosion resistance in water | Very poor | Excellent | Very poor | Poor | Very Poor
Compatibility with clad materials | Reacts with normal clad | Excellent | Variable | Variable | Variable
Thermal stability | Phase change at 665 and 770 °C | Good | Good | Good | Good
Uranium (metal) density (g/cm3) | 19.04 | 9.65 | 12.97 | 13.52 | 11.31
Melting point (°C) | 1132 | 2865 | 2850 | 2860 | 1665
Thermal conductivity (W/m-K) | 38 at 430 °C | 3 at 1000°C | 25 at 500°C | 20 at 750°C | 23 at 773°C

## Slide 30: Fuel Types Summary
There exist a number of nuclear fuels in different stages of utilization and development
Uranium is combined with O, C, N, transition metals for a variety of fuel types
UO2: ceramic, commercial reactor fuel, light water reactors
Each reactor design or application has individual needs, and no one fuel is one size fits all
Need to balance safety, performance (normal, off-normal, extended), manufacturability, processing, waste, etc.

## Slide 31: Questions?