## Slide 1: Fuel Fabrication
NE 591

## Slide 2: Fabrication Process

## Slide 3: Global Uranium Resources

## Slide 4: Uranium deposit types
There are mainly three types of uranium deposits
  Sedimentary
    Often found in sandstone; common in Canada and western US
  Igneous/hydrothermal
    Vein-type uranium ores from geothermal activity; Greenland and Namibia
  Breccial
    found in rocks that have been broken due to tectonic fracturing, or weathering; common in India, Australia and the US
Less common means of uranium mining include seawater recovery, where U concentrations is 3.3 micrograms per liter

## Slide 5: Uranium mining/processing
Uranium ores are normally processed by grinding the ore materials to a uniform particle size and then treating the ore to extract the uranium by chemical leaching
The milling process commonly yields dry powder-form material consisting of “yellowcake”, which is U3O8

## Slide 6: Conversion
Uranium enrichment requires uranium as uranium hexafluoride, which is obtained from converting uranium oxide to UF6
Uranium oxide can be reduced by hydrogen to produce UO2
  U3O8 + 2H2 ===> 3UO2 + 2H2O
The oxide is then reacted with hydrogen fluoride to form uranium tetrafluoride (UF4)
  UO2 + 4HF ===> UF4 + 2H2O
The tetrafluoride is then fed into a fluidised bed reactor with gaseous fluorine to produce uranium hexafluoride, UF6
  UF4 + F2 ===> UF6

## Slide 7: Enrichment
Natural uranium only contains 0.7% U-235, and therefore must be enriched to obtain suitable fissile material for fuel (for most reactors)
The difference in mass between U-235 and U-238 allows the isotopes to be separated and makes it possible to enrich the percentage of U-235
Two main enrichment processes
  Gaseous diffusion: 2500 kWh per SWU
  Centrifuge: 50 kWh per SWU
The capacity of enrichment plants is measured in terms of 'separative work units' or SWU

## Slide 8: Enrichment
One ton of natural uranium feedstock might end up: as 120-130 kg of uranium for power reactor fuel, as 26 kg of typical research reactor fuel, or conceivably as 5.6 kg of weapons-grade material
The curve flattens out so much because the mass of material being enriched progressively diminishes, so requires less effort relative to what has already been applied to progress a lot further in percentage enrichment

## Slide 9: Enrichment
Enrichment accounts for almost half of the cost of nuclear fuel and about 5% of the total cost of the electricity generated
It is also the main greenhouse gas impact from the nuclear fuel cycle where the electricity used for enrichment is typically generated from coal or natural gas
However, it still only amounts to 0.1% of the carbon dioxide from equivalent coal-fired electricity generation if modern gas centrifuge plants are used

## Slide 10: Fabrication Process

## Slide 11: Powder Processing
Uranium arrives at a fuel manufacturing plant in one of two forms, uranium hexafluoride (UF6) and it needs to be converted to uranium dioxide (UO2) prior to pellet fabrication
An example conversion process injects UF6 into water to form a UO2F2 particulate slurry, ammonia (NH3) is added to this mixture and the UO2F2 reacts to produce ammonium diuranate (ADU, (NH3)2U2O7), after which the slurry is filtered, dried and heated in a reducing atmosphere to pure UO2
  A reducing atmosphere is one in which oxidation is prevented by removal of oxygen and other oxidizing gases, and which may contain actively reducing gases such as hydrogen

## Slide 12: Powder/Pellet Processing
The UO2 powder may need further processing or conditioning before it can be formed into pellets:
  Homogenization: powders may need to be blended to ensure uniformity in terms of particle size distribution and specific surface area
  Additives: U3O8 may be added to ensure satisfactory microstructure and density for the pellets and other fuel ingredients, such as lubricants, burnable absorbers (e.g. gadolinium) and pore-formers may also need to be added
UO2 powder is fed into dies and pressed biaxially into cylindrical pellet form using a load of several hundred MPa
Pellets are then sintered in a heating furnace
  Sintering is the process of compacting and forming a solid mass of material by heat or pressure

## Slide 13: Sintering Process
During sintering, atoms in the materials diffuse across the boundaries of the particles, fusing the particles together and creating one solid piece
The final fuel pellets are nearly fully dense with a uniform microstructure: grain size ~ 10 μm; pore size ~ 3 μm; density ~ 95 - 99%
A single pellet in a typical reactor yields about the same amount of energy as one ton of coal

## Slide 14: Fuel strictly manufactured to be UO2
Fuel fabricated to be nearly stoichiometric; i.e., UO2.00±
  Structure stable to Tmelt
  Maximum Tmelt
O/M ratio varies slightly during irradiation
Large deviations from stoichiometry relevant to
  Fabrication
  Defected fuel behavior
  Reprocessing
  Accident conditions during dry storage or shipment of used nuclear fuel

## Slide 15: Rods and Assemblies
The fuel pellets are assembled in fuel rods and then put together in fuel assemblies
Designs dictate that the pellet-filled rods have a precise physical arrangement in terms of their lattice pitch (spacing), and their relation to other features such as water (moderator) channels and control-rod channels
Physical structures for holding the fuel rods are therefore engineered with extremely tight tolerances and are largely constructed of steel and zirconium alloys

## Slide 16: Global Fuel Fabrication
Uranium is mined and converted into fuel in a number of countries
USA, Russia, Kazakhstan and France are leaders
Is a growing need for HALEU
  High assay low enriched uranium
  Uranium with 19.7% enrichment

## Slide 17: Fuel Fabrication Summary
Mining -> Processing -> Conversion -> Enrichment -> Powder -> Compaction/Sintering -> Rod/Assembly
U3O8 must be converted to UF6 for enrichment, which is then converted to UO2 powder for pellet manufacture
For different fuel types, enriched UF6 follows a different path

## Slide 18: Heat Transport

## Slide 19: Heat transport route
Heat is produced in the fuel, transports through the cladding and gap, and into the coolant
Important quantities include
  Volumetric heat generation rate Q (W/cm3)
  Fuel Centerline temperature T0
  Surface temperature of the fuel TS
  Inner cladding temperature TCI
  Outer cladding temperature TCO
  Coolant temperature Tcool
  Pellet radius rF
  Gap thickness tG
  Cladding thickness tc

## Slide 20: Heat can be transported in three ways
Convection
  Heat transfer through mass movement of liquid or gas
Radiation
  Heat transfer by means of photons in electromagnetic waves
Conduction
  Heat transfer by molecular or atomic motion

## Slide 21: Heat transfer mode in fuel systems?
How is heat transported through the fuel?
  Conduction
How is the heat transported through the gap?
  Mostly conduction, some convection
How is heat transported through the cladding?
  Conduction
How is heat transported to the coolant?
  Convection

## Slide 22: Heat conduction equation
ρ is the density, cp is the specific heat, T is the temperature, t is the time, and k is the thermal conductivity
It is a partial differential equation in time and space
We are solving for the T as a function of space and time
  T(x, t), where x is a vector defining the position in space
What do we need to know to solve this equation?
The geometry of our problem
The initial condition of T
The boundary conditions of T
Is each parameter is a function of T
If they aren’t a function of T, do they vary in space and time for some other reason?

## Slide 23: What is our geometry for the problem?
Reactor geometry depends on reactor type
The ideal geometry of each fuel rod is axisymmetric, but in reality it is 3D
Fuel pellet defects cause 3D geometry
The stacked pellets may not be stacked perfectly, causing their center axis to not be aligned, also causing 3D geometry

## Slide 24: The initial condition of T
The initial condition of T is set by the state of the reactor directly before startup
What is the initial temperature profile of the fuel?
The initial temperature is uniform throughout the fuel
It is equal to the initial coolant temperature
T(x, 0) = Tcool(0)

## Slide 25: Boundary conditions?
The boundary conditions on T is set by the coolant flow
The temperature of the coolant Tcool is complicated
  It varies along the length of the fuel rod (axially)
  It various around the circumference of the fuel rod

## Slide 26: Fuel properties
Density varies as a function of T (thermal expansion)
  Also varies as a function of composition (thus as a function of burnup/time)
Thermal conductivity also varies with temperature

## Slide 27: The heat capacity is a function of temperature
θ = 548.68,
C2 = 2.285 × 10-3
C3 = 2.360 × 107
Ea = 18531.7

## Slide 28: The heat generation rate is a function of the thermal neutron flux, which varies in time and space
Q = Ef Nf σf ϕth

## Slide 29: Summary
General heat transport
Heat is produced in the fuel, transports through the cladding and gap, and into the coolant
The geometry of our problem
The initial condition of T
The boundary conditions of T
Is each parameter is a function of T
  Thermal conductivity, heat capacity
Function of space/time?
  Heat generation, dependent upon flux