## Slide 1: Thermo-Mechanics
NE 591

## Slide 2: Last Time
Solid mechanics predicts the deformation of a body from its applied load
  The strain defines the deformation
  The stress defines the material’s internal response to the strain
Materials can have recoverable and permanent deformation
  Elastic deformation is recoverable and occurs due to the stretching of the atomic lattice
  Plastic deformation is permanent and results form the breaking of bonds during dislocation (line defect) migration
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin walled cylinder
  Any size wall

## Slide 3: Thermal Expansion
As the temperature increases, atoms have larger vibrations, causing the material to expand
This expansion doesn’t raise the energy of the material when unrestrained
This expansion can be treated as a strain, but as one that doesn’t cause stress

## Slide 4: Thermal Expansion
In isotropic materials, thermal expansion happens equally in all directions and is linear with temperature
In this equation
  T is the current temperature
  T0 is the temperature the original size was measured
  α is the linear thermal expansion coefficient
  I is the identity tensor

## Slide 5: Thermal Expansion
Though thermal expansion doesn’t directly cause stress, it can still lead to thermal stress

## Slide 6: What is the stress in a thin constrained rod of length L when it is heated to ΔT?
The rod has a Young’s modulus of E and an expansion coefficient of α

## Slide 7: The large temperature gradient within a fuel pellet results in large thermal stresses

## Slide 8: Consider the material response of the axisymmetric body
We assume small strains, so the strain is defined as
We assume isotropic material response, so

## Slide 9: Consider a cylinder with thermal expansion but not pressure
Similar to the equations we worked through last time
Solving this ODE:

## Slide 10: What is the hoop stress in the cladding?

## Slide 11: Where is hoop stress equal to zero?

## Slide 12: The linear temperature gradient across the cladding causes axial thermal stresses

## Slide 15: Stress/Strain Regions
Once the stress reaches the yield stress, it plastically deforms
σy is the yield stress
σU is the ultimate tensile stress
The final stress before rupture is called the fracture stress

## Slide 16: Permanent Strain
After plastic deformation, if you unload the sample, it still has the permanent strain
After unloading, the strain hardening has changed the material
Thus, if you reload, the yield strain is often higher than it was previously

## Slide 17: The hardening behavior changes for different materials

## Slide 18: Ductile materials plastically deform significantly, brittle materials do not

## Slide 19: Dislocation motion
Plastic deformation occurs due to dislocation motion
A dislocation is a line defect
  Edge and screw type
When it moves, only a small number of bonds are broken at a time

## Slide 20: Dislocation are produced during deformation

## Slide 21: Dislocation motion causes plastic deformation, dislocation pileup causes hardening

## Slide 22: As the dislocation density increases, dislocations cannot move freely, raising the yield stress

## Slide 23: As the strength increases due to dislocation pile-up, the ductility decreases

## Slide 24: We need to determine the stress and strain throughout a body

## Slide 25: Cauchy momentum equation
In this equation, u is the displacement vector, ρ is the density, σ is the stress, and g is the acceleration of gravity.
Often, we are determining the stress and strain in a static body. So the equation becomes:
Finally, we can simplify things more by making our first assumption: the impact of gravity is negligible

## Slide 26: The stress divergence equation is really just a force balance

## Slide 27: Consider an axisymmetric body
Assumption 1: We have a static body
Assumption 2: Gravity is negligible
Assumption 3: The problem is axisymmetric

## Slide 28: Consider the material response of the axisymmetric body
We assume small strains, so the strain is defined as
We assume isotropic material response, so

## Slide 29: Solve for the stress throughout a pressurized cylinder (cladding tube) with thin walls
Because our cylinder has such thin walls (δ = thickness), we can simplify everything to simple force balance
First, we need the Force per unit length due to the pressure
Then we equate the forces and solve for the hoop stress
Fstress

## Slide 30: Find the other two stresses for a thin walled cylinder
To find the stress in the z-direction we do another force balance
Again, we equate the forces and solve for the stress
Last, the stress on the inside of the wall is –p and on the outside is zero, so the average
Ftop
Fwall

## Slide 31: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  R = 0.55, δ = 0.06 cm, σy = 381 MPa
The largest stress will be the hoop stress
The hoop stress is P*(0.55/.06)
  For 5 MPa, σθ = 45.8 Mpa
  For 9 MPa, σθ = 82.5 Mpa
With these pressures, we don’t come even close to the yield stress of the cladding

## Slide 32: Develop equations for the stress within a cylinder under pressure that has thicker walls
The cylinder as an inner radius Ri and an outer Radius Ro
We assume there is no shear stress, so σrz = 0
We will begin with the r equation
Now we need our constitutive law
We combine these equations to get

## Slide 33: Develop equations for the stress within a cylinder under pressure that has thicker walls
We need one more relationship from the definition of the strain
From the previous slide, we have
If we combine these, we get
Again, from the previous slide
We end up with

## Slide 34: We now have an ODE so we can solve to get the stress
Our boundary conditions are σrr(Ri) = -p and σrr(Ro) = 0
After integrating twice, we get
From σrr, we can get σθθ from
From the end condition, we determine σzz
(a)
(b)
(c)

## Slide 35: Stresses vary over the thickness of the cladding tube

## Slide 36: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  Ri = 0.52, Ro = 0.58 cm, σy = 381 MPa
Which stress is the largest?
  σθθ
At what position r will the hoop stress be the largest?
  r = Ri = 0.52 cm
What is the stress at p = 5 MPa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 46.0 MPa
What is the stress at p = 9 Mpa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 82.7 Mpa
Again, we don’t even get close to yielding

## Slide 37: We’ve now solved this same problem assuming thin and thick walled cylinders

## Slide 38: Summary
Solid mechanics predicts the deformation of a body from its applied load
  The strain defines the deformation
  The stress defines the material’s internal response to the strain
Materials can have recoverable and permanent deformation
  Elastic deformation is recoverable and occurs due to the stretching of the atomic lattice
  Plastic deformation is permanent and results form the breaking of bonds during dislocation (line defect) migration
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin walled cylinder
  Any size wall