## Slide 1: Metallic Fuel Microstructural Phenomena
NE 591

## Slide 2: Last time
Corrosion is the environmental degradation of materials
Cladding oxidizes, forming ZrO2
The limiting step for oxidation is the oxygen transport through the oxide layer
  It begins being controlled by diffusion
  Then, a protective layer forms that slows oxidation
  Once transition occurs, it loses its protectiveness and speeds up again
Hydrogen released by oxidation enters the cladding
Due to low solubility (that is a function of temperature), hydrides form
Hydrides are brittle, and so reduce the ductility of the cladding

## Slide 3: Why metallic fuel?
It has demonstrated a high burnup capability beyond 20%
Metal fuel also has superior off-normal performance characteristics, in particular for the run-beyond-cladding-breach conditions due to the compatibility of metal fuel with sodium coolant
the inherent passive safety potential where metal fuel is far superior to other fuel types
Metal fuel also allows a very simple injection-casting fabrication technique and electrorefining-based fuel cycle closure, which promises simpler waste management, proliferation-resistance, and much improved economics

## Slide 4: Why do we alloy?
Unalloyed swelling can reach >150% at target burnups
Anisotropic swelling of alpha U
  thermal expansion
  irradiation growth
Cavitation swelling is characterized by large irregular cavities that form by mechanical tearing at grain and sub-grain boundaries, resulting in a very deformed “swirled” microstructure

## Slide 5: U-Zr (U-Pu-Zr)
Alloying with Zr increases melting point and stabilizes the high temperature bcc phase
Temperature range for fuel is ~800-1100 K
Typically 10 weight percent Zr (23 atomic percent)
Directly in multiphase region
  find bcc, beta, alpha U, delta UZr2, alternate bcc phases

## Slide 6: Fuel Redistribution

## Slide 7: alpha U Tearing

## Slide 8: Swelling of Metallic Fuel

## Slide 9: Fission Gas Release

## Slide 10: Cladding Strain

## Slide 11: Fission Gas Bubble Morphology in gamma U

## Slide 12: alpha U-Zr Bubble Morpology

## Slide 13: Radially Varying Bubble Morphologies

## Slide 14: Axial Varying Microstructure

## Slide 15: Fuel-Clad Chemical Interaction

## Slide 16: Chemical Species Interaction