## Slide 1: Fission Products
NE 591

## Slide 2: Fission Product Generation
Fission releases around 200 MeV
  The fission fragments have 169 MeV of kinetic energy
  2 to 3 neutrons with an average energy of 2 MeV
  7 MeV of prompt gamma ray photons
  The remaining energy is released by beta decay
Every fission product that is produced is now in the crystal lattice of the fuel, changing the microstructure

## Slide 3: There are various types of fission products that form in the fuel
Noble gases (Xe, Kr)
Essentially insoluble in the fuel matrix
Form either intragranular (within grain) voids or bubbles or intergranular (grain boundary) bubbles
Volatiles (Br, Rb, Te, I and Cs)
Exist as gases at high temperatures of the pellet interior
Also exist as solids at the cooler pellet exterior
Metals (Mo, Ru, Pd, and Tc)
Form metallic precipitates
Insoluble oxides (Zr, Ba and Sr)
Form insoluble oxides in the fluorite lattice
Soluble oxides (Y, La and the rare earths)
Dissolved in the cation sublattice

## Slide 4: All of the fission products impact the behavior of the fuel

## Slide 5: Fission Gas Release
Fission gases (Xe, Kr) are released in a process composed of three stages in UO2
Stage 1: Gas atoms are produced throughout the fuel due to fission and diffuse towards grain boundaries
Small intragranular bubbles form within the grains, but never get larger than a few nm radius due to resolution from energized particles
Gas atoms that don’t get trapped within the intragranular bubbles migrate to grain boundaries
Atoms forming a vacancy cluster

## Slide 6: Fission Gas Release
Stage 2: Gas bubbles nucleate on grain boundaries, growing and interconnecting
Stage 3: Gas travels through interconnected bubbles to a free surface

## Slide 7: Fission Gas Release
Fission gas release also occurs due to mechanisms that don’t depend on diffusion
Release can occur to particle recoil and knockout at low temperature
It can occur due to fracture during rapid transients

## Slide 8: Fission Gas Release
Released fission gas enters the gap and plenum, causing various problems
Xe and Kr have very low thermal conductivities, reducing the gap conductance
The plenum pressure increases
The volatile fission gases corrode the cladding
They are also radioactive and hazardous, causing problems when the cladding is breached
Fission gas release experiments:
  Post irradiation annealing
    Fuel is irradiated at low temperature
    Fuel is then placed into a furnace and heated
    Gas atom release is then measured
  In-pile release
    Gas release is measured during reactor operation
    It is much more difficult than post-irradiation annealing
    Total amount released is measured by puncturing cladding after irradiation
    Release with time can be estimated using a pressure transducer inside an instrumented fuel rod

## Slide 9: Fission Gas Release
Fission gas release models attempt to predict the rate at which gas is released from the fuel
To model fission gas release, ideally we must model all three stages of gas release
  Diffusion of gas atoms to grain boundaries
  Growth and interconnection of grain boundary bubbles
  Transport of gas atoms through interconnected bubbles to free surfaces
The earliest models only considered Stage 1
Most models now consider stage 1 and 2
There are no models that consider all three stages

## Slide 11: Summary
Fission products change the fuel behavior
Fission gas is released in three stages
  Fission gas production and diffusion to grain boundaries
  Grain boundary bubble nucleation, growth, and interconnection
  Gas transport through interconnected bubbles to free surfaces
Fission gas release is measured using post-irradiation annealing and in pile experiments