## Slide 1: Nuclear Fuel Performance
NE 533 Spring 2024

## Slide 2: Last Time
Intro to fuel performance as a three-pronged concept:
  heat generation and delivery to coolant; fuel operation without problems; fuel behavior during accidents
Uranium is combined with O, C, N, transition metals for a variety of fuel types
UO2: ceramic, commercial reactor fuel, light water reactors
Good characteristics:
  high melting point, single phase, cladding compatibility, radiation resistance, stability in water
Bad characteristics:
  brittle, low thermal conductivity, limited power density, high burnup swelling

## Slide 3: Reactor systems

## Slide 4: Heat removal systems
Now we touch on how heat is removed from the fuel
Primary mechanism to remove heat directly from fuel is a coolant
Various coolant types, most common is water

## Slide 5: Heat removal systems
Primary loop water runs through the core, transporting heat generated by the fuel, to a steam generator in a secondary water loop
Steam drives a turbine, generating electricity
A tertiary water loop helps to condense residual steam from the secondary loop via cooling towers and a water reservoir

## Slide 6: Light Water Reactor Core Design
An LWR core is comprised of fuel assemblies
Each assembly contains a grid of fuel pins
  In typical commercial LWR fuel designs, a 17x17 grid
  Some pins are replaced by control rods
Water flows from bottom to top

## Slide 7: LWR Fuel Pins
LWR fuel pins are comprised of a hollow Zircaloy tube
  This is the cladding
  Zircaloy is a type of Zr alloy
Inside the cladding are stacked UO2 pellets
Each pellet is a cylinder about 1 cm in diameter and 1.5 cm in height

## Slide 8: Most fuel designs employ some type of cladding
The primary focus of the cladding is to separate the fuel from the coolant
  Fuel contains radioactive fission products
  Avoids corrosion of the fuel by the coolant
  Keeps the fuel together, not blocking coolant flow
The cladding should be thin and have a high thermal conductivity, so it doesn’t trap any of the heat produced by the fuel
Cladding should also be neutron transparent

## Slide 9: Fuel/Cladding Gap
Fuel swells during reactor operation and the cladding creeps down around the fuel
To avoid/limit both chemical and mechanical interaction, the pellet radius is smaller that the inner radius of the cladding
In LWRs, the gap is filled with He gas, significantly impacting the heat transport
In metal fuels, the gap is filled with liquid sodium, so there is little impact on the heat transport

## Slide 10: Smear Density
Smear density is the ratio of fuel volume to total internal volume of the fuel element
Cylinder volume =
Smear density = /
Smear density = /
Typical smear density > 90%
r1
r2
h

## Slide 11: Cladding material selection
Cladding must be compatible with the coolant, reasonably compatible with the fuel, have good thermal conductivity and reasonable radiation resistance
Zirconium is used because of its
  Low neutron cross section
  Corrosion resistance in 300 C water
  Resistance to void swelling
  Adequate mechanical properties
  Good thermal conductivity
  Affordable cost
  Available in large quantities
Other cladding materials in use include
  Stainless steel
  Silicon Carbide
  Ferritic-Martensitic steels like Fe-Cr and Fe-Cr-Al
  Oxide dispersion strengthened (ODS) ferritic steels

## Slide 12: Reactor Systems Wrap-up
All reactors have basic requirements they must meet
  An approach to remove the heat from the fuel, a method to convert heat to electricity, an approach to prevent radioactive products from leaving the fuel, a method to cycle the fuel, containment in case something goes very wrong
Typically, the “fuel system” is thought to consist of the fuel itself, the gap, the cladding
  primary coolant can also be included, or at least impacts of the coolant
Cladding is the primary containment, and its integrity maintains safe operation
LWRs have fuel pellets, a He gap (bond), and Zircaloy cladding

## Slide 13: fuel fabrication

## Slide 14: Fabrication Process

## Slide 15: Global Uranium Resources
world-nuclear.org

## Slide 16: Uranium mining/processing
Uranium ores are normally processed by grinding the ore materials to a uniform particle size and then treating the ore to extract the uranium by chemical leaching
The milling process commonly yields dry powder-form material consisting of “yellowcake”, which was historically referred to as U3O8
Most modern uranium recovery facilities produce a yellowish compound comprised mostly of uranyl peroxide dihydrate

## Slide 17: Conversion
Uranium enrichment requires uranium as uranium hexafluoride (gaseous state), which is obtained from converting uranium oxide to UF6
Uranium oxide can be reduced by hydrogen to produce UO2
  U3O8 + 2H2 ===> 3UO2 + 2H2O
The oxide is then reacted with hydrogen fluoride to form uranium tetrafluoride (UF4)
  UO2 + 4HF ===> UF4 + 2H2O
The tetrafluoride is then fed into a fluidized bed reactor with gaseous fluorine to produce uranium hexafluoride, UF6
  UF4 + F2 ===> UF6

## Slide 18: Enrichment
Natural uranium only contains 0.7% U-235, and therefore must be enriched to obtain suitable fissile material for fuel (for most reactors)
The difference in mass between U-235 and U-238 allows the isotopes to be separated and makes it possible to enrich the percentage of U-235
The capacity of enrichment plants is measured in terms of 'separative work units' or SWU
Two main enrichment processes
  Gaseous diffusion: 2500 kWh per SWU
  Centrifuge: 50 kWh per SWU

## Slide 19: Enrichment
  Gaseous diffusion
    Pushes UF6 through porous membrane
    U235-F6 travels slightly faster
    First Gen. technology, historical, but now outdated
  Centrifuge
    gas is placed in a gas centrifuge cylinder and rotated at a high speed
    strong centrifugal force, heavier gas molecules move towards the outside of the cylinder

## Slide 20: SWUs
The work WSWU necessary to separate a mass F of feed of assay xf into a mass P of product assay xp and tails of mass T and assay xt is given by:
V is the value function:
The feed to product ratio (F/P) is given by the expression
The tails to product ratio (T/P) is given by the expression
The same amount of separative work will require different
  amounts of energy depending on the efficiency of the separation technology

## Slide 21: High Enriched Uranium
One ton of natural uranium feedstock might end up: as 120-130 kg of uranium for power reactor fuel, as 26 kg of typical research reactor fuel, or conceivably as 5.6 kg of weapons-grade material
The curve flattens out so much because the mass of material being enriched progressively diminishes, so requires less effort relative to what has already been applied to progress a lot further in percentage enrichment

## Slide 22: Enrichment
Enrichment accounts for almost half of the cost of nuclear fuel and about 5% of the total cost of the electricity generated
It is also the main greenhouse gas impact from the nuclear fuel cycle where the electricity used for enrichment is typically generated from coal or natural gas
However, it still only amounts to 0.1% of the carbon dioxide from equivalent coal-fired electricity generation if modern gas centrifuge plants are used

## Slide 23: Fabrication Process

## Slide 24: Powder Processing
Uranium typically arrives at a fuel manufacturing plant as uranium hexafluoride (UF6) and needs to be converted to uranium dioxide (UO2) prior to pellet fabrication
An example conversion process injects UF6 into water to form a UO2F2 particulate slurry, ammonia (NH3) is added to this mixture and the UO2F2 reacts to produce ammonium diuranate (ADU, (NH4)2U2O7), after which the slurry is filtered, dried and heated in a reducing atmosphere to pure UO2
  A reducing atmosphere is one in which oxidation is prevented by removal of oxygen and other oxidizing gases, and which may contain actively reducing gases such as hydrogen

## Slide 25: Powder/Pellet Processing
The UO2 powder may need further processing or conditioning before it can be formed into pellets:
  Homogenization: powders may need to be blended to ensure uniformity in terms of particle size distribution and specific surface area
  Additives: U3O8 may be added to ensure satisfactory microstructure and density for the pellets and other fuel ingredients, such as lubricants, burnable absorbers (e.g., gadolinium) and pore-formers may also need to be added
UO2 powder is fed into dies and pressed biaxially into cylindrical pellet form using a load of several hundred MPa
Pellets are then sintered in a heating furnace
  Sintering is the process of compacting and forming a solid mass of material by heat or pressure

## Slide 26: Sintering Process
During sintering, atoms in the materials diffuse across the boundaries of the particles, fusing the particles together and creating one solid piece
The final fuel pellets are nearly fully dense with a uniform microstructure: grain size ~ 10 μm; pore size ~ 3 μm; density ~ 95 - 99%
The sintered microstructure (grain size and porosity) has a strong impact on the fuel evolution, and this processing stage can be tailored to meet microstructural needs

## Slide 27: Fuel strictly manufactured to be UO2
Fuel fabricated to be nearly stoichiometric; i.e., UO2.00±
  Structure stable to Tmelt
  Maximum Tmelt
O/M ratio varies slightly during irradiation
Large deviations from stoichiometry relevant to
  Fabrication
  Defected fuel behavior
  Reprocessing
  Accident conditions during dry storage or shipment of used nuclear fuel

## Slide 28: Rods and Assemblies
The fuel pellets are assembled in fuel rods and then put together in fuel assemblies
Designs dictate that the pellet-filled rods have a precise physical arrangement in terms of their lattice pitch (spacing), and their relation to other features such as water (moderator) channels and control-rod channels
Physical structures for holding the fuel rods are therefore engineered with extremely tight tolerances and are largely constructed of steel and zirconium alloys

## Slide 29: Global Fuel Fabrication
LWR fuel pellets and rods/assemblies are manufactured in a number of countries
USA, Russia, Kazakhstan and France are leaders
There is a growing need for HALEU
  High assay low enriched uranium
  Uranium with 19.7% enrichment

## Slide 30: Fuel Fabrication Summary
Mining -> Processing -> Conversion -> Enrichment -> Powder -> Compaction/Sintering -> Rod/Assembly
U3O8 must be converted to UF6 for enrichment, which is then converted to UO2 powder for pellet manufacture
UO2 microstructure from fabrication strongly impacts fuel performance

## Slide 31: Heat Generation

## Slide 32: Fission basics
Impinging neutron of a given energy
  Neutron energy determines cross section which determines probability of fission event
Neutron + Target Nucleus -> Two fission products, 2-3 neutrons
Fission releases around 210 MeV of energy
  170 MeV to fission fragments
  2 MeV per neutron
  7 MeV gamma rays
  Balance radioactive decay

## Slide 33: Energy release with different nuclei
Energy release is effectively agnostic with regards to the fissioning species
Comparing U-235 with Pu-239 on the right
  Pu releases about 9 MeV more usable energy per fission
  Less than a 5% difference
Partition of energy is largely identical as well

## Slide 34: Fission product yield
Regardless of fissioning isotope, fission product yields are effectively the same, in this double hump distribution
One broad peak centered around A=95, the other around A=135
Examples:
  Mo (Z=42, A=96)
  Cs (Z=55, A=133)

## Slide 35: Fission Product Yields

## Slide 36: Calculating heat generation rate for a given fuel
We know about 200 MeV of energy is available due to a fission (210 MeV minus neutrinos)
We know the fission cross section of the target nuclide (tabulated)
We can calculate the fission atom density
The heat generation rate, Q is given by:
  Q = Ef x Nf x sf x f
  Where Ef is the fission energy, Nf is the fission atom density, sf is the fission cross section, and f is the neutron flux
  Units: J/fission x atoms/cm3 x (fission/neutron)*(cm2/atom) x (neutron/cm2-s) = J/cm3-s = W/cm3

## Slide 37: Calculating heat generation rate for a given fuel
Cross sections:
  ENDF database: Nuclear Data Sheets 148 (2018) 1–142
  Thermal neutron (E=0.025 eV) U235 fission cross section: ~586.8 barns
    1 barn = 10-24 cm2
Fission atom density
  Atom density of U-235 = UO2 density x 1/molar mass x Avogadro's number x atom fraction x enrichment

## Slide 38: Example