## Slide 1: Fuel Swelling
NE 591

## Slide 2: Last time
Fission products change the fuel behavior
Fission gas is released in three stages
  Fission gas production and diffusion to grain boundaries
  Grain boundary bubble nucleation, growth, and interconnection
  Gas transport through interconnected bubbles to free surfaces
Fission gas release is measured using post-irradiation annealing and in pile experiments
Fission gas release models are used to understand fission gas experiments and to predict gas release for fuel performance codes
Spherical grain models predict a fraction of gas release for post-irradiation annealing or for in-pile gas release
Fission gas diffusivity behavior changes with temperature and fission rate

## Slide 3: Fuel changes size and shape under reactor operation

## Slide 4: Densification
Densification takes place during initial 5 - 10 MWd/kgU
  Small, as-built pores close due to effects of fission spikes and vacancy diffusion
  Large pores stable (in absence of large hydrostatic stress)
Empirical correlation for densification is a function of
  β - Burnup (in FIMA)
  Δρ0 – Total densification that can occur (a common value is 0.01)
  βD – Burnup at which densification stops ( a common value is 5 MWD/kgU)
  CD = 7.235 − 0.0086 (T(°C) − 25) for T < 750°C and CD = 1 for T ≥ 750 °C
[Maier et al, 1988]

## Slide 5: Fission product induced swelling
Fission product swelling results from three changes in the fuel microstructure
  Solid swelling: Accumulation of soluble and insoluble fission products in fuel matrix
  Gaseous swelling: Accumulation of gaseous and volatile fission products in intragranular and intergranular pores
  High burnup swelling: Restructuring of pellet rim with the accumulation of fission gas in a large number of small pores
after Garzarolli in [Rudling et al, 2007]

## Slide 6: Solid fission product swelling
The solid fission product swelling model is a function of:
  Β – Burnup (in FIMA)
  ρ – Initial UO2 density (g/cm3)

## Slide 7: Gaseous fission product swelling
Gaseous swelling varies strongly with temperature, fission rate and stress
T < 1000K
  Fission gas atoms remain in fuel matrix or collect in small, isolated, intragranular pores (<1 nm)
  Intragranular pore size limited by fission spikes that drive gas back into fuel matrix
  Gaseous swelling constrained by fission gas release
T = 1000 to 1700 K
  Swelling takes place at hot interior of pellet
  Gas atoms in fuel matrix diffuse to grain boundaries and collect in pores
  Gas pressure causes bubbles to increase in size and to coalesce into larger pores
  Gaseous swelling opposed by applied stress (opposite of hot pressing)
  Gaseous swelling also constrained by fission gas release

## Slide 8: Total change in volume
The total change in volume is found by adding all components of dimensional change
  εtot = εth + εD + εsfp + εgfp
Example:
  fission rate = 2.5e13 f/(cm3 s)
  temperature = 1400 K
  Tref = 300 K
  For densification: Δρ0 = 0.01 and βD = 5 MWD/kgU
  Total time: 2 weeks

## Slide 9: Change in Volume Example
First, we need to calculate the burnup,
  NU = Na δU/MU = 6.022e23*9.65/238 = 2.44e22 atoms of U/cm3
  β = 2.5e13*3600*24*7*2/2.44e22 = 0.0012 FIMA
Next, we need to determine the strain from thermal expansion
  εth = αΔT = 11e-6*(1400 – 300) = 0.0121
Then, we consider densification,
  We need to calculate CD, but because we are higher than 750 °C, CD = 1
  We need to convert the burnup to FIMA, βD = 5 MWD/kgU/950 = 0.0053 FIMA
  εD = 0.01*(exp(0.0012*log(0.01)/(1*0.0053)) – 1) = -0.0065

## Slide 10: Change in Volume Example
For solid fission product swelling,
  For the density of UO2, ρ = 10.97 g/cm3
  εsfp = 5.577e-2*10.97*0.0012 = 7.34e-4
Finally, gaseous fission product swelling
  εgfp = 1.96e-28*10.97*0.0012*(2800 – 1400)^11.73* exp(-0.0162*(2800 – 1400))*exp(-17.8*10.97*0.0012) = 0.0023
Total:
  εtot = εth + εD + εsfp + εgfp = 0.0121 – 0.0065 + 7.34e-4 + 0.0023 = 0.0086

## Slide 11: The overall swelling behavior depends on temperature

## Slide 12: Creep
Creep is a general mechanism for plastic deformation that occurs over time when σ < σy
Consider a heated metal beam so it expands some distance dx
We then fix it between two walls and let it cool down
Because σ < σy, that stress remains constant
In creep, defect diffusion is induced by the stress to cause permanent deformation and reduce the stress
Therefore, creep
  Occurs over time
  Increases with increasing number of diffusing defects
    High temperature (thermal creep)
    Irradiation (irradiation creep)
x+dx
x
σ = E ε

## Slide 13: Creep
General creep equation:
Creep can be caused by various microstructural mechanisms
Bulk Diffusion (Nabarro-Herring creep)
  Atoms diffuse (high T), causing grains to elongate along the stress axis
  Q = Q(self diffusion), m = 1, and b = 2
Grain boundary diffusion (Coble creep)
  Atoms diffuse along grain boundaries to elongate the grains along the stress axis
  Q = Q(grain boundary diffusion), m = 1, and b = 3
Dislocation creep
  Dislocations glide under a high stress
  Dislocations climb due to defects to avoid obstacles
  Q = Q(self diffusion), m = 4–6, and b = 0

## Slide 14: Different creep mechanisms are active for different combinations of stress and temperature

## Slide 15: The behavior of creep changes in irradiated materials

## Slide 16: Irradiation and Creep
Irradiation accelerates creep, causing it to be significant at lower temperatures
Irradiation has little effect on diffusional creep, but it accelerates dislocation creep in cubic materials
The dislocation creep rate can be written as
  ρdm is the density of mobile dislocations
  b is the burgers vector
  vd is the dislocation velocity
Gliding dislocations quickly get pinned by obstacles
As the dislocations absorb defects created by irradiation, they climb to different slip planes to avoid the obstacles
More interstitials are absorbed than vacancies due to the higher sink strength for interstitials

## Slide 17: Fuel Creep
Like other materials, the fuel also undergoes creep
The fuel creep (In UO2) is a combination of diffusion creep and irradiation creep
It is expected that fuel creep plays a major role in dimensional change in metallic fuels, large via N-H creep, but still unproven experimentally and no good creep models exist for metallic fuels

## Slide 18: Fracture
UO2 pellets fracture during changes in temperature due to large thermal stresses
Fracture results in:
  Increased gap reduction
  Reduced thermal conductivity
  Increased avenues for fission gas release
Fracture has been typically modeled in two ways:
  Empirical relocation model that is a function of burnup
  Semi-empirical smeared cracking model
Modern methods provide means of modeling discrete cracks
Radial cracks partially penetrate the pellet during temperature increase
Full cracking occurs when the temperature decreases

## Slide 19: Fracture
The fracture behavior of the fuel is fairly complicated
Fracture strength varies with grain size (G)
  frac = G-mfrac, ref, m = 0.04 – 0.05 (vs. m ~ 0.5 for metal)
  Increasing grain size from 10 m to 100 m reduces frac by ~10%
Ductility transition temperature is lower in-reactor than in thermal tests
Fracture strength is ~10× higher in compression than in tension
Load-deformation behavior strongly affected by creep under in-reactor conditions

## Slide 20: High Burnup Structure
At the hottest regions of the fuel, defects and fission products cluster or segregate to interfaces
In the cool regions of the fuel, the diffusion is too slow for defects to arrive at the interfaces
30 GWd/t
69 GWd/t

## Slide 21: High Burnup Structure
In order to annihilate the defects, the structure changes to have small grains and many larger pores
This is referred to as the high burnup structure (HBS), sometimes called the rim structure
HBS

## Slide 22: High Burnup Structure
The mechanism for the formation of HBS is still up for debate
One theory is that dislocation networks cause grain subdivision
Another is that dislocation networks cause polygonization
In UO2, their appears to be a burnup and temperature threshold for this restructuring
The formation of high burnup structure is not unique to UO2, but occurs in all fuel types at high burnup and lower temperature
Grain subdivision in U3Si2 under ion irradiation

## Slide 23: High Burnup Structure
Originally it was assumed that HBS hurt fuel performance, but recent research shows it has a positive effect
Efficiently retains fission gas
Increased toughness and softness
Increased thermal conductivity

## Slide 24: Summary
Many materials models for fuel are empirical and correlated to burnup
Fuel pellets change shape due to
  Thermal expansion (increase in volume)
  Densification (decrease in volume)
  Swelling (increase in volume)
  Creep (volume stays the same)
Fracture also decreases the gap, as fractures pieces shift outward
At high burnup but mid to low temperature the fuel restructures to have a small grain size and large bubbles
  The structure is called High Burnup Structures (HBS)
  HBS may actually improve many fuel properties