## Slide 1: Introduction and Overview
NE 591: Advanced Reactor Materials
Fall 2021
Dr. Benjamin Beeler

## Slide 2: Office Hours
Have generated a survey monkey to set a time for office hours
Right now, tentatively set for Wednesday’s 10-11 am, subject to change pending survey results

## Slide 3: Syllabus
Course Overview
In this course we will study the basic role of fuel in reactor operation and understand how the fuel impacts heat generation and transport to the coolant. The course will begin with an overview of different fuels and the fabrication processes required to construct nuclear fuel. We will also study various fuel types and geometries, with a focus on light water reactor fuel and cladding. We will then study changes in the fuel and cladding material that degrade the performance of the fuel. Finally, student will apply knowledge gained to conduct fuel performance simulations.
Topical Outline
  Advanced Reactor Systems, Advanced Fuel types
  TRISO particles
  U-Zr (U-Pu-Zr) metallic fuel
  Molten salts
  U-Mo and U-Si
  Advanced Reactor Cladding

## Slide 4: Exams, Projects, Grading
Using the standard NCSU +/- grading system, as broken down in the syllabus
Three exams will be conducted open book, timed, and held during normal class hours, with added buffer time – 20% each
Will do problem session lecture prior to exam periods
Project presentations will be via PPT and conducted during normal class hours – 15%
Final project will be via MOOSE, where code will be submitted in addition to a writeup (possibly writeup + presentation) – 25%
No final exam

## Slide 5: Feedback
This is a new course, and I want to make sure that this class is able to meet the needs of the students, provides relevant information, and is taught at a level commensurate with the abilities of the students, and I need your feedback to do that
I will be reaching out for feedback periodically throughout the semester
Completion of feedback will gain extra credit on exams

## Slide 6: Brief Bio/Background
Computational Nuclear Materials Scientist
Expertise in advanced nuclear fuels
Ph.D. in Nuclear Engineering from Georgia Tech
Previously a staff scientist at Idaho National Laboratory in Fuel Modeling and Simulation Group
Atomistic simulations: density functional theory and molecular dynamics

## Slide 7: Advanced reactor systems

## Slide 8: What do I mean by advanced reactors?
Several generations of reactors can be distinguished
Generation I reactors were developed in 1950-60s, and are no longer operational
Generation II reactors are the present US and French fleets and most in operation elsewhere

## Slide 9: What do I mean by advanced reactors?
Generation III or III+ have been constructed and typically have:
  A more standardized design for each type to expedite licensing, reduce capital cost and reduce construction time.
  A simpler and more rugged design, making them easier to operate and less vulnerable to operational upsets.
  Higher availability and longer operating life – typically 60 years.
  Further reduced possibility of core melt accidents
  Stronger reinforcement against aircraft impact than earlier designs, to resist radiological release.
  Higher burn-up to use fuel more fully and efficiently, and reduce the amount of waste.
  Greater use of burnable absorbers ('poisons') to extend fuel life.

## Slide 10: Generation III Reactors
The greatest departure from Gen II reactors is the incorporation passive of safety features
Construction is often modular, allowing for offsite manufacturing and onsite assembly
Examples include AP1000, EPR, ABWR

## Slide 11: What do I mean by advanced reactors?
Generation IV
  designs are still conceptual
  typically incorporates six reactor designs
  four of these types are fast reactors
  all operate at higher temperatures
  all six systems represent advances in sustainability, economics, safety, reliability and proliferation-resistance

## Slide 12: What do I mean by advanced reactors?
Small Nuclear Reactors
  Small Modular Reactors (SMRs)
  Micro-Reactors
Reduces the cost associated with building 1000 MW scale reactors, and can provide power away from large grid system
SMRs are 300 MWe or less, designed with modular technology using module factory fabrication, pursuing economies of series production and short construction times
Microreactors (or very small modular reactors vSMRs) are up to 25 MWe

## Slide 13: What do I mean by advanced reactors?
Small Nuclear Reactors
  Small Modular Reactors (SMRs)
  Micro-Reactors
Reduces the cost associated with building 1000 MW scale reactors, and can provide power away from large grid system
SMRs are 300 MWe or less, designed with modular technology using module factory fabrication, pursuing economies of series production and short construction times
Microreactors (or very small modular reactors vSMRs) are up to 25 MWe

## Slide 14: Small Nuclear Reactors

## Slide 15: Fuel types

## Slide 16: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator

## Slide 17: Fuel is limited to select elements
A fissionable nuclide is capable of undergoing fission (even with a low probability) after capturing a high energy neutron
A fissile nuclide is capable of sustaining a nuclear fission chain reaction with neutrons of any energy
A fertile material is a material that, although not itself fissionable, can be converted into a fissile nuclide by neutron absorption and subsequent nuclei conversions.
The Ronen fissile rule states that for a heavy element with 90 ≤ Z ≤ 100, its isotopes with neutrons (A-Z) = 2 × Z – N, where N = 43 ±2 are fissile (with some exceptions)

## Slide 18: Potential fuel candidates
The heavy elements with 90 ≤ Z ≤ 100
  Thorium (Th), Protactinium (Pa), Uranium (U), Neptunium (Np), Plutonium (Pu), Americium (Am), Curium (Cm), Berkelium (Bk), Californium (Cf), Einsteinium (Es) and Fermium (Fm)
Lets apply the fissile rule to U (2 × Z – N)
  (A-Z) = 2 Z – (43 ± 2)
  (A-Z) = 2 × 92 – [41, 42, 43, 44, 45] = [143, 142, 141, 140, 139] neutrons
  So, U-231 through U-235 should be fissile

## Slide 19: There are only four fissile nuclides that are practical for nuclear fuel
U-235
  Naturally occurs in uranium in small amounts (0.7%). Can be enriched
Pu-239
  Bred from U-238 by neutron capture
Pu-241
  Bred from Pu-240 (which comes from Pu-239) by neutron capture
U-233
  Bred from Th-232 by neutron capture

## Slide 20: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients that lead to deleterious behavior
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 21: Why not use pure uranium metal?
Pure uranium has three phases
  α-phase is orthorhombic
  β-phase is tetragonal
  g-phase is body-centered cubic
  During thermal cycling, pure uranium dramatically swells
  Alpha U has both anisotropic thermal expansion and anisotropic irradiation growth

## Slide 22: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  Mixed oxide (MOX)
  Accident tolerant/Advanced Technology Fuel (ATF)
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
UN – Lead Cooled Fast Reactors
Other

## Slide 23: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes

## Slide 24: Uranium Dioxide (UO2)
Good Characteristics
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant
    no amorphization
    Can incorporate a large number of fission products as substitutional defects

## Slide 25: Uranium Dioxide (UO2)
Bad Characteristics
  Brittle (thermal stress fractures, fragmentation)
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling
  Higher stored thermal energy than other fuel materials

## Slide 26: Uranium Dioxide (UO2)
Critical Phenomena
  Thermal conductivity (and degradation)
  Fission gas release, leading to pressure increase inside the cladding
  Fuel fragmentation and relocation under transients
  Bambooing creating stress concentrations
All 98 operational reactors in US utilize UO2

## Slide 27: Questions?