## Slide 1: Nuclear Fuels
Dr. Benjamin Beeler
Asst. Prof. in Nuclear Engineering
NE 201

## Slide 2: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator

## Slide 3: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 4: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Other fuel/reactor types

## Slide 5: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Other fuel/reactor types

## Slide 6: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes

## Slide 7: UO2
Good Features
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant
    no amorphization
    Can incorporate a large number of fission products as substitutional defects

## Slide 8: UO2
Bad Features
  Brittle
    thermal stress fractures, fragmentation
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling

## Slide 9: UO2
Critical Phenomena
  Thermal conductivity (and degradation)
  Fission gas release, leading to pressure increase inside the cladding
  Fuel fragmentation and relocation under transients
  Bambooing creating stress concentrations
All 98 operational reactors in US utilize UO2

## Slide 10: UO2-mixed oxides
Can be combined with PuO2 for a mixed oxide (MOX) fuel for use in fast reactors
Allows to burn excess weapons grad plutonium
About 30 reactors in Europe currently utilize a partial MOX core
Similar behavior to UO2, but different neutronics, fission gas release, thermal conductivity, etc.
Less common is inclusion of minor actinides in MOX to burn waste

## Slide 11: Accident Tolerant Fuel
USi fuels (U3Si2)
  Higher thermal conductivity, higher uranium density
Cr-doped UO2
  Larger grain size, reduced fission gas release
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 12: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Other fuel/reactor types

## Slide 13: UZr
Utilized in sodium cooled fast reactors (SFRs)
  EBR I, EBR II
Varied crystal structure and compositional environment
Easily alloyed with Pu, minor actinides (MA)
Can function as a breeder/burner fuel
Sodium coolant
Fe-based cladding

## Slide 14: UZr
Alloy metallic U with Zr to increase the melting point and to stabilize the high temperature body-centered cubic phase
Interesting phenomena
  30-50% swelling
  Constituent redistribution
  Alpha tearing
  FCCI

## Slide 15: UZr
Good
  High thermal conductivity
  Stability to high burnups (> 20%)
  Flexible composition
  Inherent safety- negative reactivity feedback
  Good compatibility with Na coolant
Bad
  Low melting point
  Dramatic fuel swelling that must be accounted for
  Incredibly complex microstructures/unpredictable behavior
  Fuel-Clad Chemical Interaction
  Very easily oxidized

## Slide 16: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX and USi
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Other fuel/reactor types

## Slide 17: UMo
New fuel being qualified for research reactors
Fuel foil, with Zr diffusion barrier, Al cladding
Will be utilized in ATR, NBSR, MITR, MURR

## Slide 18: UMo
Decomposition
Fission Gas Superlattice
Recrystallization
Interdiffusion region
Carbides

## Slide 19: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX and USi
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Other fuel/reactor types

## Slide 20: UC/UCO TRISO
TRISO: TRistructural ISOtropic particle fuel
Layered fuel in mm-sized particles
Layers:
  Fuel Kernel
  Buffer
  Inner Pyrolitic Carbon (IPyC)
  SiC
  Outer Pyrolitic Carbon (OPyC)

## Slide 21: UC/UCO TRISO
High temperature gas reactors (HTGR) or molten salt reactors (MSRs)
Pebble bed and prismatic types
Particles are agglomerated with graphite into a larger pebble, or into a cylindrical block
Current designs utilize UCO, which is a heterogeneous mixture of UO2 and UC fuel
Helium cooled gas or molten salt cooled

## Slide 22: UC/UCO TRISO
Each individual pebble acts as its own containment, and allows fuels to go to much higher burnups and higher temperatures than UO2
Highly reliant on accurate fabrication processes that create high integrity, uniform layers and spherical particles
Integrity of the SiC is key for fission product retention

## Slide 23: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX and USi
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Other fuel/reactor types

## Slide 24: UN
Potential fuel for gas cooled reactors, compacts or TRISO kernels, as well as lead cooled reactors
High fissile density, high thermal conductivity, and chemical stability with cladding
Very difficult to manufacture, poor oxidation resistance, requires N-enrichment

## Slide 25: Unique Fuel Designs
Lightbridge
  High Zr content UZr alloy
  Cruciform geometry fuel rods, combined into fuel elements
Kairos
  TRISO particle compacts with low density core
  Float in molten salt coolant for online refueling

## Slide 26: Unique Fuel Designs
NASA/LANL
  UMo fuel for space reactors: KRUSTY
Stable Salt Reactor (SSR)
  Dissolved molten salt fuel
  NaCl-U-Pu-stuff

## Slide 27: Summary
There exist a number of nuclear fuels in different stages of utilization and development
The more established ones are the less interesting ones…
Active research on existing, underutilized, and developmental fuel designs
Each reactor design or application has individual needs, and no one fuel is one size fits all
Need to balance safety, performance (normal, off-normal, extended), manufacture, processing, waste, etc.

## Slide 28: How do we model advanced fuels?

## Slide 29: Atomistic Modeler’s Toolkit
Density Functional Theory (DFT)
  is a computational quantum mechanical modelling method used to investigate the electronic structure of many-body systems, in particular atoms, molecules, and the condensed phases
Molecular Dynamics (MD)
  is a computer simulation method for analyzing the physical movements of atoms and molecules, determined by numerically solving Newton's equations of motion for a system of interacting particles
Yashima, https://doi.org/10.1039/C0CC00573H
Sand, https://doi.org/10.1016/j.jnucmat.2018.08.049

## Slide 30: Atomistic Modeler’s Toolkit
ab initio Molecular Dynamics (AIMD)
  is a computer simulation method in which finite temperature molecular dynamics (MD) trajectories are generated with forces obtained from accurate 'on the fly' electronic structure calculations
  hybrid mixing between the accuracy of electronic structure calculations, while allowing for real temperature effects to be considered
Schnappinger, https://doi.org/10.1039/C7CP05061E
Yazyev, https://doi.org/10.1007/s00214-005-0052-6

## Slide 31: Integration into Fuel Performance Models
BISON is the multiphysics MOOSE-based fuel performance code developed under NEAMS and includes thermal transport, stress, and underlying material evolution, etc.
BISON requires models for material properties and how they evolve during operation
A lot of these fundamental properties are unknown, and too difficult to obtain experimentally
Lower Length Scale Modeling!