## Slide 1: Fuel Thermal Conductivity
NE 591

## Slide 2: Housekeeping
You all should have received graded exams in your email
Exam 2 key is posted on moodle site
Any questions, please let me know via email or during office hours tomorrow
3rd and final exam tentatively scheduled for April 23
  Will be open book and timed via moodle
Go into moodle, there is a an example assignment called “Upload test”
Upload a document into this Upload test assignment so that we can all make sure we are capable of using the moodle system

## Slide 3: Last time
Many materials models for fuel are empirical and correlated to burnup
Fuel pellets change shape due to
  Thermal expansion
  Densification
  Swelling
  Creep
Fracture also decreases the gap, as fractures pieces shift outward
At high burnup but mid to low temperature the fuel restructures to have a small grain size and large bubbles
  The structure is called High Burnup Structures (HBS)
  HBS may actually improve many fuel properties

## Slide 4: UO2 Thermal Conductivity
We have established correlations for thermal conductivity of fresh UO2 fuel as a function of temperature
  Where t = T/1000
  The first part of the equation describes the phonon interactions
  The second part describes electronic transport which becomes significant at high temperature

## Slide 5: UO2 Thermal Conductivity
UO2 thermal conductivity is low and decreases more during reactor operation
The thermal conductivity has been collected after various amounts of burnup to make empirical fits

## Slide 6: UO2 Thermal Conductivity
The primary empirical model used in BISON is the NFIR model
The model is a function of the temperature T (in C) and the burnup β (in MWD/kgU

## Slide 7: UO2 Thermal Conductivity
The Rf function switches between two kph functions

## Slide 8: UO2 Thermal Conductivity Example
What is the thermal conductivity of a fuel predicted by the NFIR model at a temperature of 1200 K and a burnup of 5% FIMA?
First, we need to convert T to C and burnup to MWD/kgU
  T = 1200 K – 273.15 = 926.85 C, β = 0.05 FIMA*950 = 47.5 MWD/kgU
Next, we need to calculate Rf
  Rf = 0.5*(1 + tanh((926.86 – 900)/150)) = 0.5886
Now, we need kph1
  kph1 = 1/(9.592e-2 + 6.14e-3*47.5 – 1.4e-5*47.5^2 + (2.5e-4 – 1.81e-6*47.5)*926.85) = 1.9685 W/(m K)
Then, kph2
  kph2 = 1/(9.592e-2 + 2.6e-3*47.5 + (2.5e-4 – 2.7e-7*47.5)*926.85) = 2.2766 W/(m K)
Finally, kel
  kel = 1.32e-2*exp(1.88e-3*926.85) = 0.0754 W/(m K)
Then, we put it all together
  k = (1 – 0.5886)*1.9685 + 0.5886*2.2766 + 0.0754 = 2.23 W/(m K)

## Slide 9: Going beyond burnup…
Operating Conditions
Variables
Elasticity tensor
Fracture stress
Melting temperature
Fuel Property values
Dimensional change
Thermal conductivity
Elasticity tensor
Thermal conductivity
Failure criteria
Cladding
Property values
Dimensional change
Yield stress
Gap conductance
Gap pressure
Diffusion constants
Neutron flux
Temperature
Displacement
Coolant T&P
Burn-up
Fuel performance codes historically rely on materials models correlated to temperature and burn-up
Development has begun on models based on microstructure rather than burn-up

## Slide 10: Microstructure-based fuel performance modeling
Operating Conditions
Neutron flux
Variables
Temperature
Displacement
Stoichiometry
Coolant T&P
Fuel
Microstructure variables
Average grain size
Dislocation density
U defect concentrations
Pu concentration
Fission product precipitate fractions
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Crack parameter
Cladding
Microstructure variables
Average grain size
Dislocation density
H concentration
Hydride fraction
Point defect concentrations
Loop density
2nd phase particle fraction
Gap variable
Gap fission gas concentration
Grain growth
Defect prod. & transport
Fission gas behavior
Densification
Microstructure evolution models
Plasticity
Grain growth
Defect prod. & transport
Hydrogen transport
Microstructure evolution models
Loop evolution
Plasticity
Fracture
Structure/property relationships connect the microstructure variables to the property values
Elasticity tensor
Thermal conductivity
Failure criteria
Dimensional change
Yield stress
Cladding
Property values
Elasticity tensor
Fracture stress
Melting temperature
Dimensional change
Thermal conductivity
Diffusion constants
Fuel Property values

## Slide 11: Example: fission gas behavior in the fuel
Take into account a finite set of variables to describe the state of the material
Utilize a mechanistic model of fission gas behavior to predict the evolution of the microstructure
Utilize this updated microstructure to inform a number of structure/property relationships
Model of fission gas behavior
Variables
Temperature
Displacement
Stoichiometry
Structure/property relationships
Elasticity tensor
Fracture stress
Dimensional change
Thermal conductivity
Gap conductance
Gap pressure
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Gap fission gas concentration

## Slide 12: Multiscale separate effects experiments and simulations inform the development of the models
nm
μm
mm

## Slide 13: Microstructure-based models
Can provide a structure/property relationship to replace the existing burnup dependent model
For example, thermal conductivity, taking into account microstructural features and their evolution
Bulk conductivity
Fission gas
Intragranular porosity
Grain boundary and bubbles
κpr
Precipitated fission products
Vacancies and interstitials

## Slide 14: Parametrizing the mechanistic model
We employ multiscale modeling and simulation to determine the various parameters for the model
MD simulations conducted at LANL have been used to determine the coefficients for various point defects
MD simulations have shown that phonon scattering must be accounted for to accurately represent small bubbles
Mesoscale simulations have shown that GB bubbles have a larger impact on the thermal conductivity
Maxwell-Eucken (no phonon scattering)

## Slide 15: Parametrizing the mechanistic model
A thermal resistor model is created to describe the impact of GB bubbles on the thermal conductivity
MARMOT simulations are currently being used to inform the development of the precipitate multiplier

## Slide 16: Parametrizing the mechanistic model
Each term in the expression must be coupled to a corresponding state variable
The full model calculates the thermal conductivity as a function of:
  Temperature
  Point defect concentrations
  Intragranular bubble density and average radius
  Fractional coverage of bubbles on GBs and average radius
  Precipitate volume fractions and average sizes
Currently effects of precipitates fission products and individual point defects are neglected in the model, as they are not tracked or predicted in BISON

## Slide 17: Comparing with experiments…
The model under-predicts the temperature in most cases, but not all
Thus, the model is neglecting some resistive effects from the microstructure
But generally performs as well, and in some cases better, than the burnup based model
RISO-3 AN3
RISO-3 AN4
RISO II-3
US PWR TSQ0002

## Slide 18: Summary
The fuel thermal conductivity decreases with burnup
The NFIR model is a fairly accurate empirical model of the fuel thermal conductivity
Researchers are working to develop materials models for the fuel and cladding that are mechanistic rather than empirical and that are based on the evolution of the microstructure rather than the burnup.

## Slide 19: MOOSE Project
We will be utilizing MOOSE for a project and we need to find a way to get it working for all
Go to this site: https://www.mooseframework.org/getting_started/ and try to download and install MOOSE on your own/local machine
Also, I am working on getting a functional MOOSE build on rdfmg cluster such that we don’t require individual students to have sufficient computing capacity
Once we all have MOOSE, we will do 1-2 lectures of training and examples

## Slide 20: Presentation Project
Vedant: https://doi.org/10.1016/j.jnucmat.2019.151965
Yuqing: https://doi.org/10.1016/j.jnucmat.2020.152069
Khadija: https://doi.org/10.1016/j.jnucmat.2020.152050
Presentations will be conducted on ZOOM, Thursday, April 9
Article overview, background, motivation, brief methods, results summary, critical analysis, potential future work

## Slide 21: Zirconium Cladding

## Slide 22: Cladding
The purpose of the cladding is to
  Hold the pellets together so that coolant can freely flow past
  Transport heat from fuel to the coolant
  Contain fission products
  Contain fuel fragments
We would also prefer if the cladding had little to no impact on the neutron transport in the reactor

## Slide 23: Why Zirconium alloys?
Benefits
Low neutron cross section
Corrosion resistance in 300°C water
Resistance to void swelling
Adequate mechanical properties
Good thermal conductivity
Affordable cost
Available in large quantities
Problems?
Corrosion under high temperature steam
Hydride embrittlement
Anisotropic characteristics lead to creep and growth

## Slide 24: Zirconium
Pure zirconium was not acceptable due to its oxidation behavior
Oxygen with water reacted to form an oxide layer
The oxide layer is brittle and flakes off, allowing more oxidation to occur
Zr alloys were developed to reduce corrosion resistance

## Slide 25: Commercial Zr Alloys in PWRs
Alloy | Sn % | Nb % | Fe % | Cr % | Ni % | O % | Fuel Vendor
PWRs (structural components and fuel rods) |  |  |  |  |  |  | 
Zircaloy-4 (SRA) | 1.2-1.7 | - | 0.18-0.24 | 0.07-0.13 | - | 0.1-0.14 | 
ZIRLO (SRA) | 1 | 1 | 0.1 | - | - | 0.12 | W
Optimized ZIRLO (pRXA) | 0.7 | 1 | 0.1 | - | - | 0.12 | W
M5 (RXA) | - | 0.8-1.2 | 0.015-0.06 | - | - | 0.09-0.12 | AREVA
HPA-45 (SRA/RXA) | 0.6 | - | Fe+V | - | - | 0.12 | AREVA
NDA (SRA) | 1 | 0.1 | 0.3 | 0.2 |  | 0.12 | NFI
MDA (SRA) | 0.8 | 0.5 | 0.2 | 0.1 |  | 0.12 | MHI/MNF

## Slide 26: Summary
Zirconium alloys used as cladding
Zirconium fabricated into an alloy to increase corrosion resistance
There are a number of Zr alloys utilized in PWRs as cladding and structural materials