## Slide 1: Nuclear Fuel Concepts
Benjamin Beeler
Assistant Professor
Department of Nuclear Engineering
North Carolina State University

## Slide 2: My viewpoint/approach
Scientifically informed engineering is a multiscale problem
Critical phenomena need to be identified from the macroscale, and informed from the lower length scales
Perform good science, sometimes for science’s sake, but often to address a key engineering problem or need

## Slide 3: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator
While the fuel must meet neutronic requirements, limiting possible options of materials choice, the lifetime of the fuel is governed by material constraints

## Slide 4: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients that lead to deleterious behavior
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 5: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  Mixed oxide (MOX)
  Accident tolerant fuel (ATF)
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
UN – Lead Cooled Fast Reactors
NaCl-UCl3 – Molten Salt Reactors

## Slide 6: Why not use pure uranium metal?
Pure uranium has three phases
  α-phase is orthorhombic
  β-phase is tetragonal
  g-phase is body-centered cubic
  During thermal cycling, pure uranium dramatically swells
  Alpha U has both anisotropic thermal expansion and anisotropic irradiation growth

## Slide 7: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes
Good behaviors
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant (no amorphization can incorporate a large number of fission products as substitutional defects)

## Slide 8: Uranium Dioxide (UO2)
Bad behaviors
  Brittle (thermal stress fractures, fragmentation)
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling
  Higher stored thermal energy than other fuel material

## Slide 9: Uranium Dioxide (UO2)
Critical Phenomena
  Thermal conductivity (and degradation)
  Fission gas release, leading to pressure increase inside the cladding
  Fuel fragmentation and relocation under transients
  Bambooing creating stress concentrations
All 98 operational reactors in US utilize UO2

## Slide 10: Mixed Oxides
UO2 can be combined with PuO2 for a mixed oxide (MOX) fuel for use in fast reactors
Allows to burn excess weapons grade plutonium
About 30 reactors in Europe currently utilize a partial MOX core
Similar behavior to UO2, but different neutronics, fission gas release, thermal conductivity, etc.
Less common is inclusion of minor actinides in MOX to burn waste

## Slide 11: Accident Tolerant Fuel/Advanced Technology Fuel
USi fuels (U3Si2)
  A metal-ish compound, with higher thermal conductivity, higher uranium density
Cr-doped UO2
  Larger grain size, theoretically reduced fission gas release
  Cr changes the O potential present within the fuel, changing defect concentrations and mobilities
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 12: Uranium-Zirconium (UZr)
Utilized in sodium cooled fast reactors (SFRs) - EBR I, EBR II
Varied crystal structure and compositional environment
Easily alloyed with Pu, minor actinides (MA)
Can function as a breeder/burner fuel
Sodium coolant
Fe-based cladding
Alloy with Zr to increase the melting point and to stabilize the high temperature body-centered cubic phase

## Slide 13: Uranium-Zirconium (UZr)
Phenomena of interest
  30-50% swelling
  Constituent redistribution
  Alpha tearing
  FCCI
Good: High thermal conductivity; Stability to high burnups (> 20%); Flexible composition; Inherent safety- negative reactivity feedback, etc.
Bad: Low melting point; Dramatic fuel swelling that must be accounted for; Incredibly complex microstructures; Fuel-Clad Chemical Interaction, Easily oxidized, etc.

## Slide 14: Uranium-Molybdenum (UMo)
New fuel being qualified for research reactors
Fuel foil, with Zr diffusion barrier, Al cladding
Will be utilized in ATR, NBSR, MITR, MURR
Phenomena: Decomposition; Fission Gas Superlattice; Recrystallization; Interdiffusion region; Carbides

## Slide 15: TRISO Particle Reactors
High temperature gas reactors (HTGRs) or molten salt reactors (MSRs) can utilize TRISO particles as the fuel source
Pebble bed and prismatic types of HTGRs
Particles are agglomerated with graphite into a larger pebble, or into a cylindrical block
Current designs utilize UCO (in the US), which is a heterogeneous mixture of UO2 and UC fuel
Helium cooled gas or molten salt cooled

## Slide 16: UC/UCO TRISO Fuels
TRISO: TRistructural ISOtropic particle fuel
Layered fuel in mm-sized particles
Layers:
  Fuel Kernel
  Buffer
  Inner Pyrolitic Carbon (IPyC)
  SiC
  Outer Pyrolitic Carbon (OPyC)
Can appear as UC, U2C3, or UC2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Rapidly corrodes in water
  Reacts with some cladding

## Slide 17: Uranium Nitride
Potential fuel for gas cooled reactors, compacts or TRISO kernels, as well as lead cooled reactors
Pb-cooled reactors are similar in concept to SFRs, pool-type
High fissile density, high thermal conductivity, and chemical stability with cladding
Very difficult to manufacture, poor oxidation resistance, requires N-enrichment
Also being explored as a potential accident tolerant fuel for LWRs

## Slide 18: Unique Fuel Designs
KRUSTY
LightBridge
Kairos
SSR

## Slide 19: Summary
There exist a number of nuclear fuels in different stages of utilization and development
The more established ones are the less interesting ones…
Active research on existing, underutilized, and developmental fuel designs
Each reactor design or application has individual needs, and no one fuel is one size fits all
Need to balance safety, performance (normal, off-normal, extended), manufacture, processing, waste, etc.

## Slide 20: How do we model advanced fuels?

## Slide 21: Atomistic Modeler’s Toolkit
Density Functional Theory (DFT)
  is a computational quantum mechanical modelling method used to investigate the electronic structure of many-body systems, in particular atoms, molecules, and the condensed phases
Molecular Dynamics (MD)
  is a computer simulation method for analyzing the physical movements of atoms and molecules, determined by numerically solving Newton's equations of motion for a system of interacting particles
Yashima, https://doi.org/10.1039/C0CC00573H
Sand, https://doi.org/10.1016/j.jnucmat.2018.08.049

## Slide 22: Atomistic Modeler’s Toolkit
ab initio Molecular Dynamics (AIMD)
  is a computer simulation method in which finite temperature molecular dynamics (MD) trajectories are generated with forces obtained from accurate 'on the fly' electronic structure calculations
  hybrid mixing between the accuracy of electronic structure calculations, while allowing for real temperature effects to be considered
Schnappinger, https://doi.org/10.1039/C7CP05061E
Yazyev, https://doi.org/10.1007/s00214-005-0052-6

## Slide 23: DFT applied to Nuclear Fuels
Since we are dealing with the electronic structure, these calculations are very computationally expensive and limited to a few hundred atoms
Typically employed to calculate lattice constants, elastic constants, point defects, electronic densities, phonon DOS, etc.
DFT on advanced nuclear fuels has really only existed for about 15 years

## Slide 24: DFT applied to Nuclear Fuels

## Slide 25: MD applied to Nuclear Fuels
MD can span longer time scales and larger length scales, up to millions of atoms and nanoseconds
These simulations require interatomic potentials capable of accurately predicting a number of properties
No interatomic potentials for advanced nuclear fuels existed prior to about 15 years ago
Potential development is still a major area for research

## Slide 26: MD applied to Nuclear Fuels

## Slide 27: AIMD applied to Nuclear Fuels
BCC U
Alpha U with int
Eutectic LiCl-KCl

## Slide 28: Integration into Fuel Performance Models

## Slide 29: Integration into Fuel Performance Models
BISON is the multiphysics MOOSE-based fuel performance code developed under NEAMS and includes thermal transport, stress, and underlying material evolution, etc.
BISON requires models for material properties and how they evolve during operation
A lot of these fundamental properties are unknown, and too difficult to obtain experimentally
Lower Length Scale Modeling!

## Slide 30: Integration into Fuel Performance Models
Example of U-Zr fission gas swelling

## Slide 31: Molten Salts
Applications of molten salts: Catalysis; Metal production; Solar power; Thermal energy storage; Pyroprocessing; Molten salt reactors
There is a gap in the fundamental properties of molten salts
These properties are difficult to collect experimentally due to high temperatures, corrosivity, toxicity, etc.
Computational methods are used to supplement the experimental data

## Slide 32: What do we do?
Work with experimentalists to target specific salt pseudo-binaries and ternaries and validate computationally determined properties, then expand beyond the experimental data
Apply AIMD to determine density, compressibility, thermal expansion, heat capacity, enthalpy of mixing, etc.
Utilize these calculations to determine transport properties: diffusivity, viscosity, thermal conductivity, etc.

## Slide 33: NaCl-MgCl2 Density
Great agreement with the literature
Identified a temperature transition
Fit with first order Redlich-Kister expansion (n=2)
1100 K

## Slide 34: Summary
Scientifically informed engineering is a multiscale problem
There exist a number of scientific knowledge gaps for advanced nuclear fuels
Atomistic methods (DFT, MD, AIMD) are a rapidly growing area that can fill in a number of these gaps
Atomistic data can be implemented into higher length scale methodologies to increase fidelity of fuel performance simulations