## Slide 1: Mechanics
NE 591

## Slide 2: Last Time
Solid mechanics predicts the deformation of a body from its applied load
The strain defines the deformation
The stress defines the material’s response to the strain
Materials can have recoverable and permanent deformation
  Elastic deformation is recoverable and occurs due to the stretching of the atomic lattice
  Plastic deformation is permanent and results form the breaking of bonds

## Slide 3: Stress/Strain Regions
Once the stress reaches the yield stress, it plastically deforms
σy is the yield stress
σU is the ultimate tensile stress
The final stress before rupture is called the fracture stress

## Slide 4: Permanent Strain
After plastic deformation, if you unload the sample, it still has the permanent strain
After unloading, the strain hardening has changed the material
Thus, if you reload, the yield strain is often higher than it was previously

## Slide 5: The hardening behavior changes for different materials

## Slide 6: Ductile materials plastically deform significantly, brittle materials do not

## Slide 7: Dislocation motion
Plastic deformation occurs due to dislocation motion
A dislocation is a line defect
  Edge and screw type
When it moves, only a small number of bonds are broken at a time

## Slide 8: Dislocation are produced during deformation

## Slide 9: Dislocation motion causes plastic deformation, dislocation pileup causes hardening

## Slide 10: As the dislocation density increases, dislocations cannot move freely, raising the yield stress

## Slide 11: As the strength increases due to dislocation pile-up, the ductility decreases

## Slide 12: We need to determine the stress and strain throughout a body

## Slide 13: Cauchy momentum equation
In this equation, u is the displacement vector, ρ is the density, σ is the stress, and g is the acceleration of gravity.
Often, we are determining the stress and strain in a static body. So the equation becomes:
Finally, we can simplify things more by making our first assumption: the impact of gravity is negligible

## Slide 14: The stress divergence equation is really just a force balance