## Slide 1: Nuclear Fuels
Dr. Benjamin Beeler
Asst. Prof. in Nuclear Engineering
NE 201

## Slide 2: Brief Bio/Background
Computational Nuclear Materials Scientist
Expertise in advanced nuclear fuels
Ph.D. in Nuclear Engineering from Georgia Tech
Previously a staff scientist at Idaho National Laboratory in Fuel Modeling and Simulation Group
Atomistic simulations: density functional theory and molecular dynamics

## Slide 3: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator

## Slide 4: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 5: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Others…

## Slide 6: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Others…

## Slide 7: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes

## Slide 8: UO2
Good!
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant
    no amorphization
    Can incorporate a large number of fission products as substitutional defects

## Slide 9: UO2
Bad!
  Brittle
    thermal stress fractures, fragmentation
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling

## Slide 10: UO2
Critical Phenomena
  Thermal conductivity (and degradation)
  Fission gas release, leading to pressure increase inside the cladding
  Fuel fragmentation and relocation under transients
  Bambooing creating stress concentrations
All 98 operational reactors in US utilize UO2

## Slide 11: UO2-mixed oxides
Can be combined with PuO2 for a mixed oxide (MOX) fuel for use in fast reactors
Allows to burn excess weapons grad plutonium
About 30 reactors in Europe currently utilize a partial MOX core
Similar behavior to UO2, but different neutronics, fission gas release, thermal conductivity, etc.
Less common is inclusion of minor actinides in MOX to burn waste

## Slide 12: Accident Tolerant Fuel
USi fuels (U3Si2)
  Higher thermal conductivity, higher uranium density
Cr-doped UO2
  Larger grain size, reduced fission gas release
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 13: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Others…

## Slide 14: Uranium-Zirconium
Utilized in sodium cooled fast reactors (SFRs)
  EBR I, EBR II
Varied crystal structure and compositional environment
Easily alloyed with Pu, minor actinides (MA)
Can function as a breeder/burner fuel
Sodium coolant
Fe-based cladding

## Slide 15: UZr
Alloy metallic U with Zr to increase the melting point and to stabilize the high temperature body-centered cubic phase
Interesting phenomena
  30-50% swelling
  Constituent redistribution
  Alpha tearing
  FCCI

## Slide 16: UZr
Good!
  High thermal conductivity
  Stability to high burnups (> 20%)
  Flexible composition
  Inherent safety- negative reactivity feedback
  Good compatibility with Na coolant
Bad!
  Low melting point
  Dramatic fuel swelling that must be accounted for
  Incredibly complex microstructures/unpredictable behavior
  Fuel-Clad Chemical Interaction
  Very easily oxidized

## Slide 17: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Others…

## Slide 18: Uranium-Molybdenum
New fuel being qualified for research reactors
Fuel foil, with Zr diffusion barrier, Al cladding
Will be utilized in ATR, NBSR, MITR, MURR

## Slide 19: UMo
Decomposition
Fission Gas Superlattice
Recrystallization
Interdiffusion region
Carbides

## Slide 20: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Others…

## Slide 21: UC/UCO TRISO
TRISO: TRistructural ISOtropic particle fuel
Layered fuel in mm-sized particles
Layers:
  Fuel Kernel
  Buffer
  Inner Pyrolytic Carbon (IPyC)
  SiC
  Outer Pyrolytic Carbon (OPyC)

## Slide 22: UC/UCO TRISO
High temperature gas reactors (HTGR) or molten salt reactors (MSRs)
Pebble bed and prismatic types
Particles are agglomerated with graphite into a larger pebble, or into a cylindrical block
Current designs utilize UCO, which is a heterogeneous mixture of UO2 and UC fuel
Helium cooled gas or molten salt cooled

## Slide 23: UC/UCO TRISO
Each individual pebble acts as its own containment, and allows fuels to go to much higher burnups and higher temperatures than UO2
Highly reliant on accurate fabrication processes that create high integrity, uniform layers and spherical particles
Integrity of the SiC is key for fission product retention

## Slide 24: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
Others…

## Slide 25: UN – Lead Cooled Reactor
Potential fuel for gas cooled reactors, compacts or TRISO kernels, as well as lead cooled reactors
High fissile density, high thermal conductivity, and chemical stability with cladding
Very difficult to manufacture, poor oxidation resistance, requires N-enrichment

## Slide 26: Unique Fuel Designs
Lightbridge
  High Zr content UZr alloy
  Cruciform geometry fuel rods, combined into fuel elements
Kairos
  TRISO particle compacts with low density core
  Float in molten salt coolant for online refueling

## Slide 27: Unique Fuel Designs
NASA/LANL
  UMo fuel for space reactors: KRUSTY
Stable Salt Reactor (SSR)
  Dissolved molten salt fuel
  NaCl-U-Pu-stuff

## Slide 28: Summary
There exist a number of nuclear fuels in different stages of utilization and development
The more established ones are the less interesting ones…
Active research on existing, underutilized, and developmental fuel designs
Each reactor design or application has individual needs, and no one fuel is one size fits all
Need to balance safety, performance (normal, off-normal, extended), manufacture, processing, waste, etc.