## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2025

## Slide 2: Last Time
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin walled cylinder
  Thick walled cylinder
Thermal expansion is a strain that doesn’t inherently cause stress
Thermal expansion can cause stress when there is a temperature gradient
We have analytical equations for thermal stresses
  in the cladding
  in the fuel

## Slide 3: Paper Project
Assigned papers uploaded to moodle with your name as a prefix
This will be a critical review of the paper, similar to what we do for QE2, but much shorter
15 minute presentation that summarizes what was done in the paper, provides context on why it was done, and reviews what could or should have been done, or could be done next
All presentations will be submitted via moodle, due by end of the day on Mar. 20
Presentations will take place in-class on Mar. 21 and Mar. 26
If you have a specific paper that you would like to review and applies to this topic field, present it to me and I will consider it

## Slide 4: Material Property Evolution

## Slide 5: Dislocations are imperfections associated with a line of lattice sites (1D defect)
In a dislocation, an extra half plane of atoms is inserted into the lattice
When it moves, only a small number of bonds are broken at a time
Dislocation motion controls the plastic (permanent) deformation of crystalline materials

## Slide 6: Grain boundaries
Materials are typically composed of various regions where the crystal lattice is oriented differently. These regions are called grains
When two grains meet, there is a plane of atoms that do not follow the crystal lattice called a grain boundary
Most crystalline materials are polycrystalline, not single crystal
High-res transmission eleectron microscopy can also show individual atoms (palladium)
www.knmf.kit.edu/TEM.php
Atomistic simulation of grain boundaries in 3D

## Slide 7: Metals are often cast, and polycrystals naturally form during casting

## Slide 8: Polycrystals naturally form during casting
Solidification begins in different regions of the melt, each with a different orientation
Once the different regions meet, grain boundaries form between them

## Slide 9: Ceramic sintering
Ceramics are typically sintered, and polycrystals also naturally form from sintering
In sintering, powders are compacted at high temperature
The particles are each oriented differently, and as they fuse, grain boundaries form
The differences between the grain orientations result in the grain boundary

## Slide 10: Distribution of grain sizes
In a polycrystal, there is also a distribution of grain sizes
Therefore, we commonly refer to the grain size distribution and the average grain size
The Hillert distribution is an analytical distribution for grain size
Real materials often vary from this behavior

## Slide 11: 3D Defects
When point defects cluster, they form three dimensional defects
The energy of a point defects is reduced when several point defects cluster together
Larger clusters of vacancies are called voids
Clusters of impurity atoms are called precipitates

## Slide 12: Microstructure
Material microstructure is the structure observable with 25x magnification
The microstructure includes grain structure, secondary phases, porosity, and more
The microstructure can strongly influence physical properties such as strength, toughness, ductility, hardness, corrosion resistance, high/low temperature behavior or wear resistance.
These properties in turn govern the application of these materials in industrial practice
Annealed Stainless Steel
Cast Bronze
Sintered UO2
Co-Al-W Superalloy
Friction stir welded stainless steel

## Slide 13: Material processing
The processes we use to make a material have a huge impact on its microstructure and properties
Casting – manufacturing process in which a liquid material is poured into a mold and then allowed to solidify
  Can be used to make complex shapes
  The solidified microstructure typically has properties that are far from ideal
Sintering – Forming a solid from a powder using heat and/or pressure without melting the material
  Applicable to metals and ceramics
  Difficult to obtain a material that is fully dense
  Used to make fuel pellets
Post-fabrication processing
  heat treatment
  working

## Slide 14: Material processing
Heat treatment: heating or cooling a material to extreme temperatures to get desired microstructure and properties
  Used to control the rate of microstructure change, including diffusion, grain growth, or phase change
  Annealing
    heat and hold the material, which allows for any defects in the material to repair themselves
    The metal is then allowed to cool back to room temperature at a slow pace to produce a more ductile crystalline structure
  Quenching
    heated to a temperature that transforms its internal structure, held at that temperature, then rapidly cooled
    The quick cooling process locks in the high T structure, or forces phase transformation without the ability to relax stresses

## Slide 15: Material processing
Working: metalworking process that plastically deforms the alloy
Cold working occurs below the recrystallization temperature, hot working occurs above
By plastically deforming the material, we are increasing the number of dislocations and dislocation barriers, increasing the yield strength
Main types of working processes:
  Squeezing (rolling/extrusion/drawing)
  Bending (shaping)
  Shearing (slitting)

## Slide 16: Summary
Gap size changes due to thermal expansion, changing temperature profile
Often have displacements instead of strains, and can solve for stress via displacements
Fuel and pellet conditions change with time due to microstructure evolution
Atoms in the fuel and cladding materials are arranged in a crystal lattice
The crystal lattice is never perfect; it has defects
  Point defects, dislocations, grain boundaries, voids and precipitates
All materials have defects, radiation damage causes many more defects
Microstructure can be tailored through processing, during fabrication or post-fabrication

## Slide 17: mechanistic modeling

## Slide 18: Microstructure-based fuel performance modeling
Operating Conditions
Neutron flux
Variables
Temperature
Displacement
Stoichiometry
Coolant T&P
Fuel
Microstructure variables
Average grain size
Dislocation density
U defect concentrations
Pu concentration
Fission product precipitate fractions
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Crack parameter
Cladding
Microstructure variables
Average grain size
Dislocation density
H concentration
Hydride fraction
Point defect concentrations
Loop density
2nd phase particle fraction
Gap variable
Gap fission gas concentration
Grain growth
Defect prod. & transport
Fission gas behavior
Densification
Microstructure evolution models
Plasticity
Grain growth
Defect prod. & transport
Hydrogen transport
Microstructure evolution models
Loop evolution
Plasticity
Fracture
Structure/property relationships connect the microstructure variables to the property values
Elasticity tensor
Thermal conductivity
Failure criteria
Dimensional change
Yield stress
Cladding
Property values
Elasticity tensor
Fracture stress
Melting temperature
Dimensional change
Thermal conductivity
Diffusion constants
Fuel Property values

## Slide 19: Example: fission gas behavior in the fuel
Take into account a finite set of variables to describe the state of the material
Utilize a mechanistic model of fission gas behavior to predict the evolution of the microstructure
Utilize this updated microstructure to inform a number of structure/property relationships
Model of fission gas behavior
Variables
Temperature
Displacement
Stoichiometry
Structure/property relationships
Elasticity tensor
Fracture stress
Dimensional change
Thermal conductivity
Gap conductance
Gap pressure
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Gap fission gas concentration

## Slide 20: Multiscale separate effects experiments and simulations inform the development of the models
nm
μm
mm

## Slide 21: Microstructure-based models
Can provide a structure/property relationship to replace the existing burnup dependent model
For example, thermal conductivity, taking into account microstructural features and their evolution
Bulk conductivity
Fission gas
Intragranular porosity
Grain boundary and bubbles
κpr
Precipitated fission products
Vacancies and interstitials

## Slide 22: Parametrizing the mechanistic model
We employ multiscale modeling and simulation to determine the various parameters for the model
MD simulations conducted at LANL have been used to determine the coefficients for various point defects
MD simulations have shown that phonon scattering must be accounted for to accurately represent small bubbles
Mesoscale simulations have shown that GrB bubbles have a larger impact on the thermal conductivity
Maxwell-Eucken (no phonon scattering)

## Slide 23: Parametrizing the mechanistic model
A thermal resistor model is created to describe the impact of GrB bubbles on the thermal conductivity
MARMOT simulations are currently being used to inform the development of the precipitate multiplier

## Slide 24: Parametrizing the mechanistic model
Each term in the expression must be coupled to a corresponding state variable
The full model calculates the thermal conductivity as a function of:
  Temperature
  Point defect concentrations
  Intragranular bubble density and average radius
  Fractional coverage of bubbles on GBs and average radius
  Precipitate volume fractions and average sizes
Currently effects of precipitate fission products and individual point defects are neglected in the model, as they are not tracked or predicted in BISON

## Slide 25: Comparing with experiments…
The model under-predicts the temperature in most cases, but not all
Thus, the model is neglecting some resistive effects from the microstructure
Generally performs as well, and in some cases better, than the burnup based model
RISO-3 AN3
RISO-3 AN4
RISO II-3
US PWR TSQ0002

## Slide 26: UZr Fuel Performance Modeling
Development of a quantitative phase-field model of macroscale constituent redistribution in the U-Zr system, where model parameters were optimized, and the model validated against an independent data set
Calculation of surface tension based on molecular dynamics, which is used in the BISON gaseous metallic fuel swelling model

## Slide 27: U3Si2 Fuel Performance Modeling
Point Defect Diffusion, Fission gas swelling, thermal and irradiation creep

## Slide 28: TRISO Particle Fuel Performance Modeling
TRISO particle modeling is still under development from a mechanistic model standpoint
Imperfect data for many critical fission products through different layers
Data typically for UO2 only, not for UC or UCO fuel kernels

## Slide 29: FeCrAl
Evolution of compositional randomness (precipitation) will affect the mechanical properties of FeCrAl
Kinetic Monte Carlo simulations modeled the precipitation of alpha’ phase from bcc Fe-Cr alloys under thermal aging at various temperatures
Fe-Al alloys do not show any phase separation
Can determine critical temperatures for precipitation and the resulting microstructures to investigate potential hardening

## Slide 30: Summary
Researchers are working to develop materials models for the fuel and cladding that are mechanistic rather than empirical and that are based on the evolution of the microstructure rather than the burnup