## Slide 1: Understanding and Controlling the Crud Source Term in PWRs
Penghui Cao1, Daniel Wells2, Dennis Hussey2, Michael Short1
1 Department of Nuclear Science and Engineering, MIT, USA
2 Electric Power Research Institute (EPRI), Palo Alto, CA & Charlotte, NC, USA
LWRS Conference, Chicago, IL
August 2nd, 2016

## Slide 2: Goal: The Crud Source Term in PWRs
Crud cross section showing typical structure
Corrosion products deposit as crud on fuel rods
Crud constituent phases
Short, M. P.,et al. MRS-B 39(1):71-77 (2014)
To hot leg
To cold leg
CASL phase I scope
What about the crud source term?

## Slide 3: What Is Crud? Why Does It Matter?
Reactor fouling deposits: Causes operational problems like:
Power
Core Height
Axial downward power shift
BO3 Concentration
Crud induced power shift
“Leaker” fuel failures
Crud-induced localized corrosion
Image: D. Wells. EPRI Summer P-TAC Meeting (2013)
Image: D. Gaston et al. Ann. Nucl. Ener., doi: 10.1016/j.anucene.2014.09.060 (2014)

## Slide 4: First: An Overall System View
Where does Crud come/go in a PWR primary loop?
Cold Leg: 304SS, ~290C
Steam Generator: Alloy 600/690, 330C (Inlet) to 290C (Outlet)
Core: Contains fuel rods with sub-cooled boiling, removing particulates
Hot Leg: 304SS, ~330C

## Slide 5: Engineering Scale: What Is Missing?
Ultimate goal: Predict the Ni & Fe metal release terms
  Acts as source term for crud deposition codes (MAMBA1, BOA2)
1 Developed by CASL
2 Developed by EPRI
? ? ?

## Slide 6: Delineating Scales and Interscale Communication
Molecular Dynamics (LAMMPS, Sandia)
MOOSE Mesoscale Oxidation, Diffusion Path Analysis
E. Broitman, R. Becker et al. PRICM-8, 2013.
MOOSE MultiApps, Transfers, RELAP-7
D. Gaston et al., INL Multiphysics Group, 2013.
Pre-computed diffusivity relations
Recalculate environmental conditions
Calculate local Fe, Ni release rates

## Slide 7: Observations of Crud from PWRs
Mostly NiFe2O4 crystallites
Some NiO, Fe3O4
Source term appears to be particulate
Short, M. P.,et al. MRS-B 39(1):71-77 (2014)

## Slide 8: Observations Become Justified Assumptions
Alloy 600 corrosion
Alloy 690 corrosion
Alloy 600 oxide film
P. Combrade et al. “Oxidation Of Ni Base Alloys In PWR Water: Oxide Layers And Associated Damage To The Base Metal.” Proceedings of the 12th International Conference on Environmental Degradation of Materials in Nuclear Power System – Water Reactors – Edited by T.R. Allen, P.J. King, and L. Nelson TMS (The Minerals, Metals & Materials Society), 2005
All reactor internals create NiFe2O4 outer oxide crystals

## Slide 9: Assumption: NiFe2O4 Grows from Coolant
Data by P. Scott et al. show NiFe2O4 growth from solution
P. Scott, O. Calonne, and P. Combrade, “Study of Surface Remediation to Delay PWSCC Initiation in Alloy 600,” Unpublished EPRI project, 2007.

## Slide 10: Assumption: Only the Innermost Oxide is Protective
Multiple studies confirm only innermost oxide slows down oxidation and metal release
Two phases identified:
  Cr2O3
  (Ni,Fe)Cr2O4
Cr2O3 often observed as “islands” (more to come…)
Graphical summary of observations of oxide phases formed on Ni-based alloys in PWR conditions
Graphical schematic of oxide layers formed on A600 after tens of thousands of hours of exposure in a PWR

## Slide 11: Assumption: Water Ni/Fe Content Doesn’t Matter
BOREAL (PWR-like loop) testing shows little effect of Ni/Fe in coolant
  F. Carrette. EDF-MAI Report H-B60-2008-01951-EN, p. 13 (2008).
Saturation levels around 1-5ppb

## Slide 12: Key Assumptions: What (NOT) To Model
NiFe2O4
(Ni,Fe)(Cr,Fe)2O4
(Ni,Fe)Cr2O4
Cr2O3
Metal with (Cr,Ni) depletion zone
Base alloy
Flow, Erosion
O
Fe
Cr
Diffusion/Transport
600 | 690 | 304
600 | 690 | 304
Low Ni,Fe High Ni,Fe
in coolant in coolant
[1] T. Devine, ibid
[2] S Cisse et al. Corr. Sci., 56:209-216 (2012).
[1] [1] [1] [1] [2]
Missing diffusivity data

## Slide 13: Computing Unknown Diffusivities
D0
EA or Q

## Slide 14: Steps in Our Calculations
Choose potentials and parameters
Create unit cell with high defect density (speeds calculations)
Compute mean squared displacement (MSD) to get diffusion rates
Use nudged elastic band (NEB) method to find activation barriers (ΔHm)
Fit to experimental data (if available) to back out ΔHf at real temperatures & defect concentrations

## Slide 15: Computing Unknown Diffusivities: Cr2O3
[1] R. Grimes. Phil. Mag. A, 72(3):651-668 (1995).
[2] Minervini et al., J. Mater. Chem., 10:2349-2354 (2000).
Buckingham potential: Compensates charge loss due to ionic defects [1-2]
Model: 18x18x6 hexagonal unit cell with periodic boundary conditions, 58,320 atoms

## Slide 16: Computing Unknown Diffusivities: O in Cr2O3
In-plane diffusion
Out-of-plane
Path 1
Path 2
Path 3
Path 4
Path 5
Path | Migration barrier (eV) | Jump distance (Å) | (in-plane) | (out of plane)
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
Path | Migration barrier (eV) | Jump distance (Å) |  | 
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27

## Slide 17: Watching Oxygen Diffusion Mechanisms
Path | Migration barrier (eV) | Jump distance d (Å) | (in-plane) | (out of plane)
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
Path | Migration barrier (eV) | Jump distance d (Å) |  | 
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
What this means:
Oxygen diffuses mostly in-plane…
Atoms colored by displacement from original sites

## Slide 18: Watching Oxygen Diffusion Mechanisms
What this means:
Oxygen diffuses mostly in-plane… but out-of-plane jumps do happen.
Atoms colored by displacement from original sites
Path | Migration barrier (eV) | Jump distance d (Å) | (in-plane) | (out of plane)
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27
Path | Migration barrier (eV) | Jump distance d (Å) |  | 
1 | 0.425 | 2.63 | 2.63 | 0
2 | 2.38 | 2.99 | 2.99 | 0
3 | 1.38 | 2.74 | 1.53 | 2.27
4 | 1.63 | 2.85 | 1.72 | 2.27
5 | 5.532 | 4.13 | 3.45 | 2.27

## Slide 19: Unknown Diffusivities: Cr in Cr2O3
1
2
3
4
5
Path | Migration barrier (eV) | Jump distance d (Å) | (in-plane) | (out-of-plane)
1 | 0.971 | 2.87 | 2.84 | 0.385
2 | 8.19 | 4.96 | 4.96 | 0
3 | 7.86 | 5.74 | 5.73 | 0.385
4 | 2.67 | 2.65 | 0 | 2.65
5 | 1.23 | 6.41 | 0 | 6.41
Path | Migration barrier (eV) | Jump distance d (Å) |  | 
1 | 0.971 | 2.87 | 2.84 | 0.385
2 | 8.19 | 4.96 | 4.96 | 0
3 | 7.86 | 5.74 | 5.73 | 0.385
4 | 2.67 | 2.65 | 0 | 2.65
5 | 1.23 | 6.41 | 0 | 6.41

## Slide 20: Watching Chromium Diffusion Mechanisms
1
2
3
4
5
What does this mean?
Cations migrate out-of-plane, which is very anisotropic.

## Slide 21: Full Cr2O3 Dataset for Oxygen
Anisotropic (factor of 2)

## Slide 22: Full Cr2O3 Dataset for Chromium
Highly anisotropic (30x)

## Slide 23: Comparison to Other Systems
Charged defect anisotropy is quite common in other systems
E. Kendrick et al. Nat. Mater., 2007, 6, 871
Long-range, anisotropic diffusion by hand-to-hand tetrahedral in La1-xBa1+xGaO4x/2 by DFT
In-plane O diffusion by the vacancy mechanism, with oxygen ion density in red
A. Chroneos et al. J. Mater. Chem., 20:266-270 (2010)

## Slide 24: Diffusion Coefficients in Cr2O3
O diffusivity: x (plus doping effects)
Cr diffusivity: x
Fe diffusivity: x
Ni diffusivity: x

## Slide 25: Effects of Dopant Cations
Ni slows oxygen diffusion more than Fe for both defects
At 1800K,
Diffusivity at 1800K | Interstitial diffusion () | Vacancy diffusion ()
 | 5.82∙10-11 | 2.29∙10-10
 | 2.67∙10-10 | 2.32∙10-10
Diffusivity at 1800K |  | 
 | 5.82∙10-11 | 2.29∙10-10
 | 2.67∙10-10 | 2.32∙10-10

## Slide 26: Comparison to Recent Work
Same diffusivities studied by MD in Cr2O3, different results
J. Vaari. “Molecular dynamics simulations of vacancy diffusion in chromium(III) oxide, hematite, magnetite and chromite.” Solid State Ionics, 270:10-15 (2015).
Path | Hm (eV)
1 | 0.971

## Slide 27: Check Calculations with Experimental Data
Check computed MD Cr2O3 data with tracer diffusion experiments
EA matches to within experimental error
D0 differs by one order of magnitude (pretty good for MD)
Takeaway message: Our MD appears to be correct!
A. C. S. Sabioni et al. Mat. Sci. Eng. A, 392:254-261 (2005)
Our Fe diffusivity: x (1eV/atom = 96.85 kJ/mol)

## Slide 28: Justifying Bulk Diffusion
SIMS data of Fe diffusion through polycrystalline Cr2O3
(Our MD data)
Grain size (nm)
GB width (~1nm)
A. C. S. Sabioni et al. Mat. Sci. Eng. A, 392:254-261 (2005)

## Slide 29: The Spinel Diffusion Data, for Completeness
Key points:
Much lower activation energies, similar prefactors
Far faster diffusion predicted through spinel than Cr2O3
No tracer experiments to scale to! Major missing piece of data.
Diffusion in bulk (Ni,Fe)Cr2O4
Diffusion in bulk Cr2O3

## Slide 30: Feed Microscale into Engineering Scale
Microscale model computes Fickian flux, feeds areal release rate up to engineering scale
A600, A690, SS304
Metal
Oxide
Prescribed thickness vs. time

## Slide 31: Microscale Model Assumptions: Oxide Thickness
Used experimental data from oxidation of A600, A690, 304SS at PWR conditions (units removed for proprietary concerns)
  325-350C, 1200ppm H3BO3, 2ppm LiOH, pH ~ 7.2, 25-30 cc/kg H2
Program on Technology Innovation: Review of Oxidation and Surface Film Formation Studies
on Austenitic Alloys in Light Water Reactor Coolants. EPRI, Palo Alto, CA: 2015. 3002005478
L. Guinard, C. Gabet, T. Czerwiec, E. Riquelme, and O. Kerrec, “Effect of surface passivation of Inconel 690 on oxidation in primary circuit conditions,” presented at the
Water Chemistry of Nuclear Reactor Systems 8, BNES, vol. 1, p. 67, 2000.
A. Machet, A. Galtayries, S. Zanna, P. Jolivet, M. Foucault, P. Combrade, P. Scott, and P. Marcus, “Kinetics of passivation of a nickel-base alloy in high temperature water,” presented at the EUROCORR 2004, Nice (France), 2004.
Time
Thickness

## Slide 32: Putting it All Together
Compute local metal release rate at every location & time step
Diffusivities, oxide thicknesses are functions of space & time
  Temperature profiles prescribed along loop, also functions of space & time
Local release rate
Species i (Fe or Ni for now)
Quadrature point
Prescribed oxide thickness vs. time & type
Avogadro’s number
Atomic number density
Local wetted perimeter
Concentration of species i in local metal
Our MD diffusivities
Diffusion Flux (m2/s)

## Slide 33: WEC 4-Loop PWR, A600, Cr2O3 Assumed
Key Points:
Slightly super- parabolic release rates (exponent >0.5)
WAY too little metal released: Further points to Cr2O3 being not fully protective in its actual state on SG tubes
  “Islands” of Cr2O3 observed on Ni-based alloys are likely not fully formed, allow for fast diffusion in between
Fe
Ni

## Slide 34: WEC 4-Loop PWR, A600, Spinel Assumed
Key Points:
Super- parabolic release rates
Ni/Fe ratio roughly unity in the first fuel cycle
~20kg total metal release, correct order of magnitude
Fe
Ni

## Slide 35: WEC 4-Loop PWR, A690, Spinel Assumed
Key Points:
Almost linear release rates!
Metal release is a pure function of oxide growth rates, plant geometry, and temperature for identical oxide phases
Ni/Fe ratio roughly two in the first cycle, should increase with time
~50kg total metal release, more crud predicted than for A600 plants
  This is an artifact of the model, not reality. We can learn from it though…
Fe
Ni

## Slide 36: What Can Integrated Predictions Tell Us?
MD Cr2O3 data is likely correct (with tracer validation)
Cr2O3 is likely not fully formed, though “islands” may be more complete in A690
Ni/Fe ratios on par with plant observations
A690 plants predicted to release more crud
  Not consistent with existing measurements and data
Image: ANT International Crud in PWR/VVER coolant, p. 4-55 (2014)

## Slide 37: Major Data Gaps – Near Term Future Work
Tracer diffusion experiments for (Fe,Ni)Cr2O4 system
  Needed to find ΔHf
TEM analysis of SG tubes from autoclaves & plants
  Phase identification often done using EDX, no phase info!
SIMS data of Fe diffusion through polycrystalline Cr2O3
A. C. S. Sabioni et al. Mat. Sci. Eng. A, 392:254-261 (2005)
Z X Xia et al. Sci. Rep., 5:13027 (2015)

## Slide 38: Major Data Gaps – Near Term Future Work
Low-temperature, long-timescale MD simulations
  Search for low-T fast diffusion
  Check spinel off-stoichiometry diffusivities are representative
Crud from A690 plants
  Must wait until fuel cycle 3 to account for historical crud
R. Yang et al. J. Nucl. Sci. Technol., 43:9, 951-959 (2006)
Schematic of the parallel replica dynamics method for accelerated MD simulations. A. Voter et al., Annu. Rev. Mater. Res. 32:321–46 (2002).

## Slide 39: Thanks to Our Sponsor, Acknowledgments
This research was supported by:
P-TAC (PWR Technical Advisory Committee), contract numbers 10002739 and 10004433
Thanks to Kenny Epperson for accurate PWR segment lengths, wetted perimeters & areas