## Slide 1: Introduction and Overview
NE 591-010: Nuclear Fuel Performance
Spring 2022
Dr. Benjamin Beeler

## Slide 2: Access to Course Resources
Everything will be hosted on Moodle, classes conducted in-person and via ZOOM
To access Moodle courses, log on to WolfWare with your Unity ID and password
Record lectures available after the fact on Panopto
For distance students, should also have access to videos in Engineering Online
Office hours will be held in my office on Wednesdays 10-11 am
Additional virtual office hours can be scheduled via email
I encourage all to reach out to me with any questions or concerns

## Slide 3: Syllabus
Course Overview
In this course we will study the basic role of fuel in reactor operation and understand how the fuel impacts heat generation and transport to the coolant. The course will begin with an overview of different fuels and the fabrication processes required to construct nuclear fuel. We will also study various fuel types and geometries, with a focus on light water reactor fuel and cladding. We will then study changes in the fuel and cladding material that degrade the performance of the fuel. Finally, student will apply knowledge gained to conduct fuel performance simulations.
Learning Outcomes
By the end of this course, the student should be able to:
Understand the basics of fuel fabrication
Calculate the rate at which heat is transported to the coolant from the fuel
List the most important microstructural changes that take place in the fuel and cladding and how they impact fuel performance
Use an existing fuel performance code

## Slide 4: Topical Outline
  Introduction and Overview
  Fuel types
  Fuel fabrication
  Thermal transport
  Mechanical behavior
  Materials issues in the fuel
  Materials issues in the cladding
  Used fuel disposition
  Overview of fuel performance codes
  Utilization of fuel performance codes
Graded Exercises
  Three exams
  One paper presentation project
  One MOOSE-based final project

## Slide 5: Exams, Projects, Grading
Using the standard NCSU +/- grading system, as broken down in the syllabus
Three exams will be conducted open book, timed, and held during normal class hours, with added buffer time for online submission – 20% each
Will do problem session lecture prior to exam periods
Project presentations will be via PPT and conducted during normal class hours – 15%
Final project will be via MOOSE, where code will be submitted in addition to a writeup – 25%
No final exam

## Slide 6: Feedback
This course is still evolving, and I want to make sure that this class is able to meet the needs of the students, provides relevant information, and is taught at a level commensurate with the abilities of the students, and I need your feedback to do that
I will be reaching out for feedback periodically throughout the semester
Completion of feedback will gain extra credit on exams
Fill out the “Post to Forum: Introduce Yourself” activity on the Moodle so I can get to know everyone
Complete “Example Test #1”

## Slide 7: Brief Bio/Background
Computational Nuclear Materials Scientist
Expertise in advanced nuclear fuels
Ph.D. in Nuclear Engineering from Georgia Tech
Previously a staff scientist at Idaho National Laboratory in Fuel Modeling and Simulation Group
Atomistic simulations: density functional theory and molecular dynamics

## Slide 8: My viewpoint/approach
Scientifically informed engineering is a multiscale problem
Critical phenomena need to be identified from the macroscale, and informed from the lower length scales
Perform good science, sometimes for science’s sake, but often to address a key engineering problem or need

## Slide 9: Complete nuclear fuel cycle

## Slide 10: Emphasis on In-Reactor Behavior of Fuel
The full reactor system is complex and substantial, and there are separate NE courses covering this area
Although the fuel is a relatively small part of a reactor system, it determines thermal power, which drives electric power generation
The performance of the fuel is measured by:
  How much heat is delivered to the coolant
  The length of time it operates without any problems
  How well it performs during an accident

## Slide 11: How much heat is delivered to the coolant?
Heat transport is related to thermal conductivity
In single crystal, pristine materials, thermal conductivity is reasonably straightforward
In dynamic, radiation environments, thermal conductivity degrades, fission gas bubbles form, grain boundaries are generated and destroyed
How does thermal conductivity vary?

## Slide 12: The length of time fuel operates without any problems
There are 98 operating nuclear reactors in the US, producing 20% of the electricity
The net capacity factor is the ratio of an actual electrical energy output to the maximum possible electrical energy output over a period of time
Nuclear reactor capacity factor is ~92% over the past decade
The ability to maintain high capacity factor, limit shutdown time, is key in making nuclear power economical
Fuel is the primary component forcing reactor downtime

## Slide 13: Fuel behavior during accidents
In addition to normal operating conditions, the behavior of the fuel during accidents is of critical importance
Predictable, and hopefully stable, behavior is desired during a variety of accident scenarios
Even low impact accidents are detrimental to public opinion surrounding nuclear energy
Fukushima

## Slide 14: All of these factors together represent what we call “fuel performance”
Fuel Performance
Heat generation
Fuel problems causing unscheduled outages
Fuel behavior during an accident

## Slide 15: Fuel types

## Slide 16: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator

## Slide 17: Fuel is limited to select elements
A fissionable nuclide is capable of undergoing fission (even with a low probability) after capturing a high energy neutron
A fissile nuclide is capable of sustaining a nuclear fission chain reaction with neutrons of any energy
A fertile material is a material that, although not itself fissionable, can be converted into a fissile nuclide by neutron absorption and subsequent nuclei conversions.
The Ronen fissile rule states that for a heavy element with 90 ≤ Z ≤ 100, its isotopes with neutrons (A-Z) = 2 × Z – N, where N = 43 ±2 are fissile (with some exceptions)

## Slide 18: Potential fuel candidates
The heavy elements with 90 ≤ Z ≤ 100
  Thorium (Th), Protactinium (Pa), Uranium (U), Neptunium (Np), Plutonium (Pu), Americium (Am), Curium (Cm), Berkelium (Bk), Californium (Cf), Einsteinium (Es) and Fermium (Fm)
Lets apply the fissile rule to U (2 × Z – N)
  (A-Z) = 2 Z – (43 ± 2)
  (A-Z) = 2 × 92 – [41, 42, 43, 44, 45] = [143, 142, 141, 140, 139] neutrons
  So, U-231 through U-235 should be fissile

## Slide 19: There are only four fissile nuclides that are practical for nuclear fuel
U-235
  Naturally occurs in uranium in small amounts (0.7%). Can be enriched
Pu-239
  Bred from U-238 by neutron capture
Pu-241
  Bred from Pu-240 (which comes from Pu-239) by neutron capture
U-233
  Bred from Th-232 by neutron capture

## Slide 20: Fuel Considerations
Safety:
  Stable and predictable behavior
  No melting, no phase changes under transients that lead to deleterious behavior
Uranium density
Mechanical integrity
Cladding interactions
Swelling and fission gas release
Operating temperatures

## Slide 21: Why not use pure uranium metal?
Pure uranium has three phases
  α-phase is orthorhombic
  β-phase is tetragonal
  g-phase is body-centered cubic
  During thermal cycling, pure uranium dramatically swells
  Alpha U has both anisotropic thermal expansion and anisotropic irradiation growth

## Slide 22: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  Mixed oxide (MOX)
  Accident tolerant/Advanced Technology Fuel (ATF)
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
UN – Lead Cooled Fast Reactors
Other

## Slide 23: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes

## Slide 24: Uranium Dioxide (UO2)
Good Characteristics
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant
    no amorphization
    Can incorporate a large number of fission products as substitutional defects

## Slide 25: Uranium Dioxide (UO2)
Bad Characteristics
  Brittle (thermal stress fractures, fragmentation)
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling
  Higher stored thermal energy than other fuel materials

## Slide 26: Uranium Dioxide (UO2)
Critical Phenomena
  Thermal conductivity (and degradation)
  Fission gas release, leading to pressure increase inside the cladding
  Fuel fragmentation and relocation under transients
  Bambooing creating stress concentrations
All 98 operational reactors in US utilize UO2

## Slide 27: Mixed Oxides (MOX)
Can be combined with PuO2 for a mixed oxide (MOX) fuel for use in fast reactors
Allows to burn excess weapons grade plutonium
About 30 reactors in Europe currently utilize a partial MOX core
Similar behavior to UO2, but different neutronics, fission gas release, thermal conductivity, etc.
Less common is inclusion of minor actinides in MOX to burn waste

## Slide 28: Accident Tolerant Fuel/Advanced Technology Fuel
Kept the acronym, changed the concept
USi fuels (U3Si2)
  A metal-ish compound, with higher thermal conductivity, higher uranium density
  Complex crystal structure (10 atoms unit cell) with effectively two sub-lattices
  Amorphizes at low temperatures
  Poor oxidation resistance
  Will require improved cladding, liners/coatings or fuel dopants

## Slide 29: Accident Tolerant Fuel/Advanced Technology Fuel
Cr-doped UO2
  Larger grain size, theoretically reduced fission gas release
  Cr changes the O potential present within the fuel, changing defect concentrations and mobilities
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 30: Questions?