## Slide 1: Fuel Swelling
NE 591

## Slide 2: Last time
Many materials models for fuel are empirical and correlated to burnup
Fuel pellets change shape due to
  Thermal expansion (increase in volume)
  Densification (decrease in volume)
  Swelling (increase in volume)
  Creep (volume stays the same)
Fracture also decreases the gap, as fractures pieces shift outward
At high burnup but mid to low temperature the fuel restructures to have a small grain size and large bubbles
  The structure is called High Burnup Structures (HBS)
  HBS may actually improve many fuel properties

## Slide 3: UO2 Thermal Conductivity
We have establish correlations for thermal conductivity of fresh UO2 fuel as a function of temperature
  Where t = T/1000
  The first part of the equation describes the phonon interactions
  The second part describes electronic transport which becomes significant at high temperature

## Slide 4: UO2 Thermal Conductivity
UO2 thermal conductivity is low and decreases more during reactor operation
The thermal conductivity has been collected after various amounts of burnup to make empirical fits

## Slide 5: UO2 Thermal Conductivity
The primary empirical model used in BISON is the NFIR model
The model is a function of the temperature T (in C) and the burnup β (in MWD/kgU

## Slide 6: UO2 Thermal Conductivity
The Rf function switches between two kph functions

## Slide 7: UO2 Thermal Conductivity Example
What is the thermal conductivity of a fuel predicted by the NFIR model at a temperature of 1200 K and a burnup of 5% FIMA?
First, we need to convert T to C and burnup to MWD/kgU
  T = 1200 K – 273.15 = 926.85 C, β = 0.05 FIMA*950 = 47.5 MWD/kgU
Next, we need to calculate Rf
  Rf = 0.5*(1 + tanh((926.86 – 900)/150)) = 0.5886
Now, we need kph1
  kph1 = 1/(9.592e-2 + 6.14e-3*47.5 – 1.4e-5*47.5^2 + (2.5e-4 – 1.81e-6*47.5)*926.85) = 1.9685 W/(m K)
Then, kph2
  kph2 = 1/(9.592e-2 + 2.6e-3*47.5 + (2.5e-4 – 2.7e-7*47.5)*926.85) = 2.2766 W/(m K)
Finally, kel
  kel = 1.32e-2*exp(1.88e-3*926.85) = 0.0754 W/(m K)
Then, we put it all together
  k = (1 – 0.5886)*1.9685 + 0.5886*2.2766 + 0.0754 = 2.23 W/(m K)

## Slide 8: Going beyond burnup…
Operating Conditions
Variables
Elasticity tensor
Fracture stress
Melting temperature
Fuel Property values
Dimensional change
Thermal conductivity
Elasticity tensor
Thermal conductivity
Failure criteria
Cladding
Property values
Dimensional change
Yield stress
Gap conductance
Gap pressure
Diffusion constants
Neutron flux
Temperature
Displacement
Coolant T&P
Burn-up
Fuel performance codes historically rely on materials models correlated to temperature and burn-up
We have begun development of models based on microstructure rather than burn-up

## Slide 9: Microstructure-based fuel performance modeling
Operating Conditions
Neutron flux
Variables
Temperature
Displacement
Stoichiometry
Coolant T&P
Fuel
Microstructure variables
Average grain size
Dislocation density
U defect concentrations
Pu concentration
Fission product precipitate fractions
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Crack parameter
Cladding
Microstructure variables
Average grain size
Dislocation density
H concentration
Hydride fraction
Point defect concentrations
Loop density
2nd phase particle fraction
Gap variable
Gap fission gas concentration
Grain growth
Defect prod. & transport
Fission gas behavior
Densification
Microstructure evolution models
Plasticity
Grain growth
Defect prod. & transport
Hydrogen transport
Microstructure evolution models
Loop evolution
Plasticity
Fracture
Structure/property relationships connect the microstructure variables to the property values

## Slide 10: Example: fission gas behavior in the fuel
Take into account a finite set of variables to describe the state of the material
Utilize a mechanistic model of fission gas behavior to predict the evolution of the microstructure
Utilize this updated microstructure to inform a number of structure/property relationships
Model of fission gas behavior
Variables
Temperature
Displacement
Stoichiometry
Structure/property relationships
Elasticity tensor
Fracture stress
Dimensional change
Thermal conductivity
Gap conductance
Gap pressure
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Gap fission gas concentration

## Slide 11: Multiscale separate effects experiments and simulations inform the development of the models
nm
μm
mm

## Slide 12: Microstructure-based models
Can provide a structure/property relationship to replace the existing burnup dependent model
For example, thermal conductivity, taking into account microstructural features and their evolution
Bulk conductivity
Fission gas
Intragranular porosity
Grain boundary and bubbles
κpr
Precipitated fission products
Vacancies and interstitials

## Slide 13: Parametrizing the mechanistic model
We employ multiscale modeling and simulation to determine the various parameters for the model
MD simulations conducted at LANL have been used to determine the coefficients for various point defects
MD simulations have shown that phonon scattering must be accounted for to accurately represent small bubbles
Mesoscale simulations have shown that GB bubbles have a larger impact on the thermal conductivity
Maxwell-Eucken (no phonon scattering)

## Slide 14: Parametrizing the mechanistic model
A thermal resistor model is created to describe the impact of GB bubbles on the thermal conductivity
MARMOT simulations are currently being used to inform the development of the precipitate multiplier

## Slide 15: Parametrizing the mechanistic model
Each term in the expression must be coupled to a corresponding state variable
The full model calculates the thermal conductivity as a function of:
  Temperature
  Point defect concentrations
  Intragranular bubble density and average radius
  Fractional coverage of bubbles on GBs and average radius
  Precipitate volume fractions and average sizes
Currently effects of precipitates fission products and individual point defects are neglected in the model, as they are not tracked or predicted in BISON

## Slide 16: Comparing with experiments…
The model under-predicts the temperature in most cases, but not all
Thus, the model is neglecting some resistive effects from the microstructure
But generally performs as well, and in some cases better, than the burnup based model
RISO-3 AN3
RISO-3 AN4
RISO II-3
US PWR TSQ0002

## Slide 17: Summary
The fuel thermal conductivity decreases with burnup
The NFIR model is a fairly accurate empirical model of the fuel thermal conductivity
Researchers are working to develop materials models for the fuel and cladding that are mechanistic rather than empirical and that are based on the evolution of the microstructure rather than the burnup.

## Slide 18: MOOSE Project
We will be utilizing MOOSE for a project and we need to find a way to get it working for all
Go to this site: https://www.mooseframework.org/getting_started/ and try to download and install MOOSE on your own/local machine
Also, I am working on getting a functional MOOSE build on rdfmg cluster such that we don’t require individual students to have sufficient computing capacity
Once we all have MOOSE, we will do 1-2 lectures of training and examples

## Slide 19: Presentation Project
Vedant: https://doi.org/10.1016/j.jnucmat.2019.151965
Yuqing: https://doi.org/10.1016/j.jnucmat.2020.152069
Khadihja: https://doi.org/10.1016/j.jnucmat.2020.152050
Presentations will be conducted on ZOOM, Thursday, April 9
Article overview, background, motivation, brief methods, results summary, critical analysis, potential future work