## Slide 1: Thermo-Mechanics
NE 591

## Slide 2: Last Time
Solid mechanics predicts the deformation of a body from its applied load
  The strain defines the deformation
  The stress defines the material’s internal response to the strain
Materials can have recoverable and permanent deformation
  Elastic deformation is recoverable and occurs due to the stretching of the atomic lattice
  Plastic deformation is permanent and results form the breaking of bonds during dislocation (line defect) migration
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin walled cylinder
  Any size wall

## Slide 3: Thermal Expansion
As the temperature increases, atoms have larger vibrations, causing the material to expand
This expansion doesn’t raise the energy of the material when unrestrained
This expansion can be treated as a strain, but as one that doesn’t cause stress

## Slide 4: Thermal Expansion
In isotropic materials, thermal expansion happens equally in all directions and is linear with temperature
In this equation
  T is the current temperature
  T0 is the temperature the original size was measured
  α is the linear thermal expansion coefficient
  I is the identity tensor

## Slide 5: Thermal Expansion
Though thermal expansion doesn’t directly cause stress, it can still lead to thermal stress

## Slide 6: What is the stress in a thin constrained rod of length L when it is heated to ΔT?
The rod has a Young’s modulus of E and an expansion coefficient of α

## Slide 7: The large temperature gradient within a fuel pellet results in large thermal stresses

## Slide 8: Consider the material response of the axisymmetric body
We assume small strains, so the strain is defined as
We assume isotropic material response, so

## Slide 9: Consider a cylinder with thermal expansion but not pressure
Similar to the equations we worked through last time
Solving this ODE:

## Slide 10: What is the hoop stress in the cladding?
r
Ri
Rf

## Slide 11: Where is hoop stress equal to zero?

## Slide 12: The linear temperature gradient across the cladding causes axial thermal stresses

## Slide 13: Same approach to the thermal stress in a fuel pellet
The thermal stress is due to the temperature gradient

## Slide 14: Solve this stress ODE
The boundary conditions are:
Once we solve it, we obtain
Then we can solve the hoop stress
The axial stress is much more complicated to obtain, but you end up with

## Slide 15: The fuel temperature gradient causes large thermal stresses

## Slide 16: How far do fuel cracks extend?
E = 200 GPa, ν = 0.345, α = 11.0e-6 1/K, σfr = 130 MPa, ΔT = 550 K
Solve for η
  – σfr / σ* = 1 – 3 η2
  3 η2 = 1 + σfr / σ*
  η = ( (1 + σfr / σ*)/3 )½
σ* = 11.0e-6*200*550/(4*(1 – 0.345) ) = 461.8 MPa
η = sqrt( (1 + 130/461.8)/3 ) = 0.65

## Slide 17: Analytical Thermomechanics Summary
Increases in temperature cause most materials to expand
We call this thermal expansion, which is a strain that doesn’t inherently cause stress
Thermal expansion can cause stress when
  Deformation is constrained
  There are gradients in the expansion coefficient
  There is a temperature gradient
We have analytical equations for thermal stresses in the cladding and in the fuel

## Slide 18: The gap changes as a function of time
Both the pellet and the cladding swell
But, as the gap decreases, the temperature changes, which again makes the gap change
The solution using the analytical equations is iterative, due to the dependence of the gap size and temperature.

## Slide 19: Calculate the steady state temperature profile in the rod, including thermal expansion
LHR = 200 W/cm, δ0gap = 30 μm, Rf = 0.5, Tcool = 580 K, TEXP,0 = 373 K, kgap = 0.0026 W/cm-K, tC= 0.06 cm, αf = 11.0e-6 1/K, αC = 7.1e-6 1/K
ΔTcool = 25.5 K, ΔTclad = 22.5 K, ΔTfuel = 530.5 K
So, TIC = 580 + 25.5 + 22.5 = 628.0 K, Ts = 701.5 K, T0 = 1232.0 K
First, we will deal with expansion in the cladding
  Av(Rc) = 0.5 + 30e-4 + 0.06/2 = 0.533 cm
  Av(TC) = 580 + 25.5 + 22.5/2 = 616.75 K
  ΔRc = 0.533*7.1e-6*(616.75 – 373) = 9.22e-4 cm

## Slide 20: Calculate the steady state temperature profile in the rod, including thermal expansion
Second, we deal with the fuel
  Av(Tf) = (1232 + 701.5)/2 = 966.7 K
  ΔRf = 0.5*11e-6*(966.7 – 373) = 0.0033 cm
The total change in the gap is 9.22e-4 – 0.0033 = -0.0023
However, that means the gap is smaller and so our temperatures were wrong!

## Slide 21: This calculation is repeated until the gap width stops changing significantly
The change in the gap does NOT effect the coolant or cladding temperatures, just the gap and fuel temperatures.
We only need to repeat the calculation of the fuel and cladding temperatures and the change in the gap
Iteration | δgap (cm) | Ts (K) | T0 (K)
0 | 0.003 | 701 | 1232
1 | 0.00066 | 644 | 1174
2 | 0.00097 | 652 | 1182
3 | 0.00094 | 651 | 1181
4 | 0.00094 | 651 | 1181

## Slide 22: Next time
Solve the temperature and the displacement vector for the full thermomechanical problem