## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2023

## Slide 2: mechanistic modeling

## Slide 3: Microstructure-based fuel performance modeling
Operating Conditions
Neutron flux
Variables
Temperature
Displacement
Stoichiometry
Coolant T&P
Fuel
Microstructure variables
Average grain size
Dislocation density
U defect concentrations
Pu concentration
Fission product precipitate fractions
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Crack parameter
Cladding
Microstructure variables
Average grain size
Dislocation density
H concentration
Hydride fraction
Point defect concentrations
Loop density
2nd phase particle fraction
Gap variable
Gap fission gas concentration
Grain growth
Defect prod. & transport
Fission gas behavior
Densification
Microstructure evolution models
Plasticity
Grain growth
Defect prod. & transport
Hydrogen transport
Microstructure evolution models
Loop evolution
Plasticity
Fracture
Structure/property relationships connect the microstructure variables to the property values
Elasticity tensor
Thermal conductivity
Failure criteria
Dimensional change
Yield stress
Cladding
Property values
Elasticity tensor
Fracture stress
Melting temperature
Dimensional change
Thermal conductivity
Diffusion constants
Fuel Property values

## Slide 4: Example: fission gas behavior in the fuel
Take into account a finite set of variables to describe the state of the material
Utilize a mechanistic model of fission gas behavior to predict the evolution of the microstructure
Utilize this updated microstructure to inform a number of structure/property relationships
Model of fission gas behavior
Variables
Temperature
Displacement
Stoichiometry
Structure/property relationships
Elasticity tensor
Fracture stress
Dimensional change
Thermal conductivity
Gap conductance
Gap pressure
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Gap fission gas concentration

## Slide 5: Multiscale separate effects experiments and simulations inform the development of the models
nm
μm
mm

## Slide 6: Microstructure-based models
Can provide a structure/property relationship to replace the existing burnup dependent model
For example, thermal conductivity, taking into account microstructural features and their evolution
Bulk conductivity
Fission gas
Intragranular porosity
Grain boundary and bubbles
κpr
Precipitated fission products
Vacancies and interstitials

## Slide 7: Parametrizing the mechanistic model
We employ multiscale modeling and simulation to determine the various parameters for the model
MD simulations conducted at LANL have been used to determine the coefficients for various point defects
MD simulations have shown that phonon scattering must be accounted for to accurately represent small bubbles
Mesoscale simulations have shown that GrB bubbles have a larger impact on the thermal conductivity
Maxwell-Eucken (no phonon scattering)

## Slide 8: Parametrizing the mechanistic model
A thermal resistor model is created to describe the impact of GB bubbles on the thermal conductivity
MARMOT simulations are currently being used to inform the development of the precipitate multiplier

## Slide 9: Parametrizing the mechanistic model
Each term in the expression must be coupled to a corresponding state variable
The full model calculates the thermal conductivity as a function of:
  Temperature
  Point defect concentrations
  Intragranular bubble density and average radius
  Fractional coverage of bubbles on GBs and average radius
  Precipitate volume fractions and average sizes
Currently effects of precipitate fission products and individual point defects are neglected in the model, as they are not tracked or predicted in BISON

## Slide 10: Comparing with experiments…
The model under-predicts the temperature in most cases, but not all
Thus, the model is neglecting some resistive effects from the microstructure
Generally performs as well, and in some cases better, than the burnup based model
RISO-3 AN3
RISO-3 AN4
RISO II-3
US PWR TSQ0002

## Slide 11: UZr Fuel Performance Modeling
Development of a quantitative phase-field model of macroscale constituent redistribution in the U-Zr system, where model parameters were optimized, and the model validated against an independent data set
Calculation of surface tension based on molecular dynamics, which is used in the BISON gaseous metallic fuel swelling model

## Slide 12: U3Si2 Fuel Performance Modeling
Point Defect Diffusion, Fission gas swelling, thermal and irradiation creep

## Slide 13: TRISO Particle Fuel Performance Modeling
TRISO particle modeling is still under development from a mechanistic model standpoint
Imperfect data for many critical fission products through different layers
Data typically for UO2 only, not for UC or UCO fuel kernels

## Slide 14: FeCrAl
Evolution of compositional randomness (precipitation) will affect the mechanical properties of FeCrAl
Kinetic Monte Carlo simulations modeled the precipitation of alpha’ phase from bcc Fe-Cr alloys under thermal aging at various temperatures
Fe-Al alloys do not show any phase separation
Can determine critical temperatures for precipitation and the resulting microstructures to investigate potential hardening

## Slide 15: Summary
Researchers are working to develop materials models for the fuel and cladding that are mechanistic rather than empirical and that are based on the evolution of the microstructure rather than the burnup.

## Slide 16: Material Property Evolution

## Slide 17: Pretty much everything we have learned so far, nothing changes once the fuel and cladding reach steady state

## Slide 18: Fuel is dynamic!

## Slide 19: Property changes due to microstructure evolution during reactor operation must be considered
Mid Life
Point defect diffusion
Point defect clustering
Fission gas segregation to GB and voids
Bubble nucleation
Zinkle and Singh 2000
Late life
Fission product swelling
Bubble percolation and fission gas release
Cladding creep
Fuel creep
Brohan 2000
Insertion in reactor
Removal from reactor
Fuel Fabrication
Sintered UO2
Height 2 cm
Diameter 1 cm
~10 μm grain size
Density > 95%
From Pedro Peralta, ASU
Fuel failure
Pellet/cladding interaction
Cladding corrosion
Cladding fracture
Santana et al. 2011
Early life
Thermal expansion
Fracture
Point defect and fission gas generation
Fuel Densification

## Slide 20: The properties and performance of a material are a result of factors across various length scales
Chemical bonds
Crystal structure
Defect interactions
Microstructure
Material properties and performance

## Slide 21: The crystal structure of a material is the shape of the ordered structure of the atoms
The atoms of many materials form an organized lattice, these are called crystalline materials. All reactor materials are crystalline.
The configuration of the atoms in the lattice impacts the properties of the material (density, thermal expansion coefficient, elastic modulus, etc.)
All major light water nuclear materials are either cubic or hexagonal
(d) Hexagonal close packed

## Slide 22: Crystalline materials
In crystalline materials, the lattices are not perfect, they have defects
Defects can be 0D, 1D, 2D, 3D
The interactions between defects seriously impact material properties and how they perform

## Slide 23: Point defects
Point defects (zero-dimensional defects) are lattice imperfections related to one or two lattice sites
There are several types of point defects
  Vacancies
  Self interstitial atoms (SIA)
  Interstitial impurity atoms
  Substitutional impurity atoms
Point defects control the mobility of atoms and, therefore influence all processes that depend on diffusion

## Slide 24: Point defects
Vacancies and interstitials form naturally in materials
Extra atoms can sit on a surface, creating a vacancy, or a surface can have a missing atom, creating a self interstitial atom (SIA)
We define the number of vacancies or interstitials in terms of a concentration
There exists an equilibrium concentration of point defects

## Slide 25: Radiation damage
Ionizing radiation can introduce defects into the crystal lattice, called radiation damage
PKA collisions create a collision cascade, which results in the generation of defects (point and clusters)

## Slide 26: Dislocations are imperfections associated with a line of lattice sites (1D defect)
In a dislocation, an extra half plane of atoms is inserted into the lattice
When it moves, only a small number of bonds are broken at a time
Dislocation motion controls the plastic (permanent) deformation of crystalline materials

## Slide 27: Grain boundaries
Materials are typically composed of various regions where the crystal lattice is oriented differently. These regions are called grains
When two grains meet, there is a plane of atoms that do not follow the crystal lattice called a grain boundary
Most crystalline materials are polycrystalline, not single crystal
High-res transmission eleectron microscopy can also show individual atoms (palladium)
www.knmf.kit.edu/TEM.php
Atomistic simulation of grain boundaries in 3D

## Slide 28: Metals are often cast, and polycrystals naturally form during casting

## Slide 29: Polycrystals naturally form during casting
Solidification begins in different regions of the melt, each with a different orientation
Once the different regions meet, grain boundaries form between them

## Slide 30: Ceramic sintering
Ceramics are typically sintered, and polycrystals also naturally form from sintering
In sintering, powders are compacted at high temperature
The particles are each oriented differently, and as the fuse, grain boundaries form
The differences between the grain orientations result in the grain boundary

## Slide 31: Distribution of grain sizes
In a polycrystal, there is also a distribution of grain sizes
Therefore, we commonly refer to the grain size distribution and the average grain size
The Hillert distribution is an analytical distribution for grain size
Real materials often vary from this behavior

## Slide 32: 3D Defects
When point defects cluster, they form three dimensional defects
The energy of a point defects is reduced when several point defects cluster together
Larger clusters of vacancies are called voids
Clusters of impurity atoms are called precipitates

## Slide 33: Microstructure
Material microstructure is the structure observable with 25x magnification
The microstructure includes grain structure, secondary phases, porosity, and more
The microstructure can strongly influence physical properties such as strength, toughness, ductility, hardness, corrosion resistance, high/low temperature behavior or wear resistance.
These properties in turn govern the application of these materials in industrial practice
Annealed Stainless Steel
Cast Bronze
Sintered UO2
Co-Al-W Superalloy
Friction stir welded stainless steel

## Slide 34: Material processing
The processes we use to make a material have a huge impact on its microstructure and properties
Casting – manufacturing process in which a liquid material is poured into a mold and then allowed to solidify
  Can be used to make complex shapes
  The solidified microstructure typically has properties that are far from ideal
Sintering – Forming a solid from a powder using heat and/or pressure without melting the material
  Applicable to metals and ceramics
  Difficult to obtain a material that is fully dense
  Used to make fuel pellets
Heat treatment – heating or cooling a material to extreme temperatures to get desired microstructure and properties
  Used to control the rate of microstructure change, including diffusion, grain growth, or phase change
  Use on many types of materials (metals, ceramics, glasses)

## Slide 35: Summary
Even during steady state operation, fuel and pellet conditions change with time due to microstructure evolution
Atoms in the fuel and cladding materials are arranged in a crystal lattice
The crystal lattice is never perfect; it has defects
  Point defects include vacancies, interstitials, and impurity atoms
  Dislocations are line defects
  Grain boundaries are planar defects
  Voids and precipitates are volume defects
All materials have defects, radiation damage causes many more defects
Microstructure can be tailored through processing