## Slide 1
Michael Short
February 16, 2016
TMS-2016, Nashville, TN
Characterization and Mitigation of CRUD Growth at PWR Fuel Cladding Conditions

## Slide 2: What the Hell Is CRUD?
Chalk River Unidentified Deposits: Corrosion deposits on fuel rods
CRUD cross section showing typical structure
Corrosion products deposit as CRUD on fuel rods
CRUD constituent phases
Short, M. P.,et al. MRS-B 39(1):71-77 (2014)
To hot leg
From cold leg

## Slide 3: Who Cares About CRUD?
Chalk River Unidentified Deposits: Causes operational problems like:
Power
Core Height
Axial downward power shift
BO3 Concentration
CRUD induced power shift
“Leaker” fuel failures
CRUD-induced localized corrosion
Image: D. Wells. EPRI Summer P-TAC Meeting (2013)
Image: D. Gaston et al. Ann. Nucl. Ener., doi: 10.1016/j.anucene.2014.09.060 (2014)

## Slide 4: Overview of the MIT IHTFP* Loop
*Internally Heated Testloop for PWRs

## Slide 5: Overview of the MIT IHTFP Loop
Circulation Loop
Auxiliary Loop
Controls chemistry
Room temperature, slightly pressurized
Auxiliary Loop
At actual PWR conditions
Where the CRUD actually grows
Circulation Loop

## Slide 6: Main Circulation Loop
Pressure Control
  Increased by pressurizing pump
  Measured by pressure transmitter and gauges
  Set by back-pressure regulator
1
1
2
Temperature Control
  Increased by autoclave heating rod and pre-heater
  Measured by thermocouples in autoclave and on the loop
1
2
2
Flow Control
  Increased by circulation pump
  Measured by differential pressure transmitter
  Moderated by control valve
1
3
3
Fill Terminal
Pressurizing Pump
Pre-heater
Vacuum Terminal
To Vent
Control Valve
Thermocouple
Fill Terminal
To Auxiliary Loop
Autoclave
3
2
    Differential Pressure Sensor
Circulation Pump
Control Valve
Pressure switch
1 Inch tubing
3/4 Inch tubing
1/2 Inch tubing
1/4 Inch tubing
    Pressure Relief Valve
    Pressure Gauge
From Water Tank

## Slide 7: Where the Magic Happens: The Autoclave
Sapphire
Windows
Water out
Water in
Actual Autoclave

## Slide 8: CFD Shows Minimal Flow Disturbance
CFD analysis courtesy of Akshay Dave, Victor Petrov, Annalisa Manera of U. Michigan
Flow remains relatively uniform around heating rod

## Slide 9: Auxiliary Chemistry Control Loop
Cooler
Drain
Pressurizing pump
pressure
regulator
Small pump
Pressure transmitter
Pressure Gauge
Drain
To Circulation Loop
From Circulation Loop
Ion Exchange Resin Container
Water Tank
Small pump
Temperature Probe
Valve
Flow Sensor
Measurement equipment
pH, Dissolved O2, Conductivity

## Slide 10: Comparison of IHTFP to a PWR
 | PWR | First Sample
Pressure | 15.5 MPa | 15.5 MPa
Temperature | 287-324°C | 320°C
Reynolds Number | 5·105 | 1.62·105
Mass flux | 3500 kg/m2s | 1920 kg/m2s
Fe3O4, NiO | 13-116 ppb | 20,000 ppb

## Slide 11: Experimental Goals
CRUD Fractal Analysis
  Fractal analysis using box-counting method with ImageJ program
  Determine CRUD’s fractal characteristic in terms of:
    tortuosity dimension
    area dimension
    If CRUD is fractal
1
1
2
CRUD Mitigation through Chemical Bonding
  Prevent or mitigate CRUD growth through coating that prevent chemical bonding by particles and ions
  Pre-screening in small loop
  10 materials to be tested
1
2
2
3
CRUD Mitigation through Control of Boiling
  Hydrophobic surface bubble formation could mitigate CRUD
  Biphilic surface could control boiling and mitigate CRUD without DNB problem
1
3
2
Source: [1] Azimi, G. et. al. “Hydrophobicity of rare-earth oxide ceramics.”

## Slide 12: First CRUD Growth after One Week
Sample Ring
Flow Ring
    CRUD grown:
      Heater Temperature: 470 Celsius
      Water Temperature: 320 Celsius
      Pressure:155 bars
      7 days
Heater

## Slide 13: First CRUD Sample: SEM Images
Magnification x3,250
Magnification x7,500

## Slide 14: First CRUD Sample: SEM Cross Section
Magnification x10,000
Magnification x25,000

## Slide 15: Fractalline Analysis of CRUD
Our CRUD model assumes that CRUD is fractalline, and calculates an effective permeability 𝞳 using this assumption
Requires fractal tortuosity dimension (dT) and fractal area dimension (dN) as shown below:
dT and dN obtained by the box-counting method
ImageJ is used for image processing

## Slide 16: Fractal Analysis
Fractal Analysis of First CRUD Sample
Magnification x7500
Magnification x7500 (Binary)

## Slide 17: Fractal Analysis
Fractal Area Dimension Analysis of First CRUD Sample
Fractal area dimension dN is 1.8547 which is –slope
dN and dT that was used in Mamba was ~1.6
R2 is very close to 1 indicating that CRUD is fractal
Chart: Ln(Box Size)
| 0.69315 | 1.38629 | 2.07944 | 2.77259 | 3.46574 | 4.158879999999999 | 4.852029999999999 | 5.545179999999999 | 6.23832 | 6.93147
 | 11.5566 | 10.3425 | 9.1813 | 8.0268 | 6.7811 | 5.4116 | 4.0254 | 2.7726 | 1.3863 | 0
 | 20

## Slide 18: One Week of CRUD Growth

## Slide 19: Isolating Boiling Chimneys

## Slide 20: Isolating Boiling Chimneys

## Slide 21: Isolating Boiling Chimneys

## Slide 22: Isolating Boiling Chimneys

## Slide 23: Isolating Boiling Chimneys

## Slide 24: Isolating Boiling Chimneys

## Slide 25: Isolating Boiling Chimneys

## Slide 26: Isolating Boiling Chimneys

## Slide 27: Starting to Measure Boiling Chimney Properties, Fractalline Dimensions

## Slide 28: Images for Fractal Analysis

## Slide 29: Ongoing CRUD Characterization – One Week of CRUD Growth, Single Chimney

## Slide 30: Ongoing CRUD Characterization – One Week of CRUD Growth, Single Chimney

## Slide 31: Going Deep into Boiling Chimneys

## Slide 32: Going Deep into Boiling Chimneys

## Slide 33: Going Deep into Boiling Chimneys

## Slide 34: Looking Around Boiling Chimneys

## Slide 35: What’s Next in the MIT CRUD Loop?
LOTS more fractal analysis for statistics
Growing CRUD at different pressures (heat fluxes) to control fractal dimensions
Four week CRUD growth experiment ended last week
Development of CRUD resistant materials, biphilic coatings for CRUD mitigation and improved heat transfer