## Slide 1: Fission and heat generation
NE-591

## Slide 2: Fission basics
Impinging neutron of a given energy
  Neutron energy determines cross section which determines probability of fission event
Neutron + Target Nucleus -> Two fission products, 2-3 neutrons
Fission releases around 210 MeV of energy
  170 MeV to fission fragments
  2 MeV per neutron
  7 MeV gamma rays
  Balance radioactive decay

## Slide 3: Energy release with different nuclei
Energy release is effectively agnostic with regards to the fissioning species
Comparing U-235 with Pu-239 on the right

## Slide 4: Fission product yield
Regardless of fissioning isotope, fission product yields are effectively the same, in this double hump distribution
One broad peak centered around A=95, the other around A=135
Examples:
  Mo (Z=42, A=96)
  Cs (Z=55, A=133)

## Slide 5: Fission Product Yields

## Slide 6: Calculating heat generation rate for a given fuel
We know about 200 MeV of energy is available due to a fission (210 MeV minus neutrinos)
We know the fission cross section of the target nuclide (tabulated)
We can calculate the fission atom density
The heat generation rate, Q is given by:
  Q = Ef x Nf x sf x f
  Where Ef is the fission energy, Nf is the fission atom density, sf is the fission cross section, and f is the neutron flux
  Units: J/fission x atoms/cm3 x (fission/neutron)*(cm2/atom) x (neutron/cm2-s) = J/cm3-s

## Slide 7: Calculating heat generation rate for a given fuel
Cross sections:
  ENDF database: Nuclear Data Sheets 148 (2018) 1–142
  Thermal neutron (E=0.025 eV) U235 fission cross section: 586.8 barns
    1 barn = 10-24 cm2
Fission atom density
  Atom density of U-235 = UO2 density x 1/molar mass x Avogadros number x atom fraction x enrichment

## Slide 8: Calculating heat generation rate for a given fuel
Given a density of UO2 (10.97 g/cm3)
Enrichment of 4%
Molar mass of 3% enriched UO2
  235*0.03 + 238*0.97 + 2*16 = 269.9 g/mol
Atom density of U-235 = 10.97 x 1/269.9 x 6.022E23 x 1/3 x 0.03
  2.45E20 atoms/cm3
Given a flux of 5E12 neutrons/cm2/s
Q = Ef x Nf x sf x f
  200E6 eV x 1.602E-19 J/eV x 2.45E20 atoms/cc x 587E-24 cm2 x 5E13 n/cm2/s
Q = 230 J/s/cm2 = 230 W/cm2

## Slide 9: Some notes
Fast neutron cross section ~100x less than thermal neutron cross section
Fuels for fast neutron spectrum typically have high enrichments, 19.7% U-235
Historical research reactor fuels, such as UMo and U3Si2, have had an enrichment of 90+%
Neutron flux will vary depending on the reactor
  HFIR has a peak neutron flux of 3E15 n/cm2/s
  PULSTAR has a peak neutron flux of 1E13 n/cm2/s
Significant variability in heat generation depending on fuel type and reactor conditions

## Slide 10: Reactor Systems
NE 591

## Slide 11: Heat removal systems
Last time, worked though the heat generation rate in the fuel
Now we touch on how heat is removed from the fuel
Primary mechanism to remove heat directly from fuel is a coolant
Various coolant types, most common is water

## Slide 12: Heat removal systems
Primary loop water runs through the core, transporting heat generated by the fuel, to a steam generator in a secondary water loop
Steam drives a turbine, generating electricity
A tertiary water loop helps to condense residual steam from the secondary loop via cooling towers and a water reservoir

## Slide 13: Light Water Reactor Core Design
An LWR core is comprised of fuel assemblies
Each assembly contains a grid of fuel pins
  In typical commercial LWR fuel designs, a 17x17 grid
  Some pins are replaced by control rods
Water flows from bottom to top

## Slide 14: LWR Fuel Pins
LWR fuel pins are comprised of a hollow Zircaloy tube
  This is the cladding
  Zircaloy is a type of Zr alloy
Inside the cladding are stacked UO2 pellets
Each pellet is a cylinder about 1 cm in diameter and 1 cm in height

## Slide 15: Not only water cooled reactor designs

## Slide 16: Not all fuel is pellet-based
Metallic fuel is a solid fuel slug
  Utilized an Fe-based cladding, such as HT-9
TRISO particles are formed into spherical compacts, or can be formed into pellet compacts
UMo and USi have been used in plate fuels
Assemblies are often hex-shaped and can included reflectors

## Slide 17: ATR and HFIR Core design
HFIR combines curved plates in concentric regions
The ATR core is a unique curved design with plate type fuel

## Slide 18: Most fuel designs employ some type of cladding
The primary focus of the cladding is to separate the fuel from the coolant
  Fuel contains dangerous fission products
  Avoids corrosion of the fuel by the coolant
  Keeps the fuel together, not blocking coolant flow
The cladding should be thin and have a high thermal conductivity, so it doesn’t trap any of the heat produced by the fuel

## Slide 19: Fuel/Cladding Gap
Fuel swells during reactor operation and the cladding creeps down around the fuel
To avoid both chemical and mechanical interaction, the pellet radius is smaller that the inner radius of the cladding
In LWRs, the gap is filled with gas, significantly impacting the heat transport
In metal fuels, the gap is filled with liquid sodium, so there is little impact on the heat transport

## Slide 20: Cladding material selection
Cladding must be compatible with the coolant, reasonably compatible with the fuel, have good thermal conductivity and reasonable radiation resistance
Zirconium is used because of its
  Low neutron cross section
  Corrosion resistance in 300 C water
  Resistance to void swelling
  Adequate mechanical properties
  Good thermal conductivity
  Affordable cost
  Available in large quantities
Other cladding materials in use include
  Stainless steel
  Silicon Carbide
  Ferritic-Martensitic steels like Fe-Cr and Fe-Cr-Al
  Oxide dispersion strengthened (ODS) ferritic steels

## Slide 21: Molten Salt Reactors w/o cladding
Some MSRs plan to utilize liquid UCl3 as the fuel, flowing continuously through the core
Secondary loop comprised of coolant salt, such as LiCl-KCl