## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2025

## Slide 2: Notes
Wellness day on Tuesday 2/11
No class
  do something fun, take some time off, take care of yourself
For events, activities, support:
  https://wellness.ncsu.edu/wellness-day/
Less fun news… paper project will be assigned next week
Let me know if you prefer a specific topic area
Reminder to make progress on your MOOSE project
Exam on module 2 planned for Feb. 20

## Slide 3: Last Time
We developed analytical solutions for the stress in a pressurized cylinder with a thick wall
Increases in temperature cause most materials to expand, which is a strain that doesn’t inherently cause stress
Thermal expansion can cause stress when
  Deformation is constrained, there are gradients in the expansion coefficient, there is a temperature gradient
We developed analytical equations for thermal stresses
  in the cladding and in the fuel

## Slide 4: NUMERICAL THERMO-Mechanics

## Slide 5: Now we can solve the temperature and the displacement vector for the full thermomechanical problem
T impacts the value of u through thermal expansion
u impacts the value of T through changes in the thickness of the gap
The value for T evolves with time
The value for u also evolves with time, even though there is not time in its PDE

## Slide 6: The primary tool for solving all thermomechanics problems is the finite element method
Finite difference
  Can solve the heat conduction equation
  Can’t easily solve the mechanics equations
Finite Volume
  Can solve the heat conduction equation
  Can solve the mechanics equations
  Eqns derived from fluid dynamics
Finite Element
  Can solve the heat conduction equation
  Can solve the mechanics equations
  Can handle any geometry
  Can handle any boundary condition

## Slide 7: The 1D thermomechanics problem definition
The initial temperature is set to 273 K
We will take 50 time steps of 0.5 s
The full power of Q = 450 begins at time t = 0.
UO2 material properties are used for both the thermal and mechanics equations
r
Rf
dT/dr = 0
ur = 0
Tr = Ts
dur/dr = 0

## Slide 8: Comparison to analytical theory
If we use a constant thermal conductivity, analytical 1D model matches very well
When k is a function of temperature, there is a difference between the FEM and analytical stress

## Slide 9: There are various available tools for solving coupled thermomechanical problems with FEM
Commercial tools
  ABAQUS
  ANSYS
  COMSOL
Open source
  MOOSE
NRC-based
  FRAPCON/FRAPTRAN

## Slide 10: The purpose of a fuel performance code is to simulate and evaluate fuel rod behavior
The first fuel performance codes were developed in the mid seventies
Advanced fuel performance codes are still under development today

## Slide 11: How are fuel performance codes used?
The primary goals are to predict the fuel centerline temperature and the stress in the cladding
Fuel performance codes aren’t focused on predicting power production, but rather to predict safety margins, provide coupling to other codes

## Slide 12: A fuel performance code must be able to predict:
Fuel
Temperature profile
Volumetric change
Gap
Gap heat transport
Mechanical interaction between fuel and cladding
Gap pressure
Cladding
Temperature profile
Stress

## Slide 13: The primary focus is solving the thermomechanical problem
Gap
The handling of the gap changes the most between different codes
Fuel
Solved Numerically
Solved Numerically or analytically
Cladding
Solved Numerically or analytically
Solved Numerically

## Slide 14: Various approaches to model the fuel rod
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 15: Early fuel performance codes were made for either steady state or transient operation
Steady state codes
  Leave off the time derivative part of the heat equation
  The material properties still evolve with time as a function of burnup
  The volumetric changes in the fuel are also a function of burnup
  Creep of fuel and cladding change with time
Transient codes
  Include the time derivative
  Have similar burnup dependent models like steady state codes, but don’t include creep
  Have additional models for rapid transients

## Slide 16: Start with FRAPCON
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 17: FRAPCON Flow Chart
FRAPCON is the NRC’s steady-state fuel performance code
FRAPCON has the ability to accurately calculate the high-burnup response of light-water reactor fuel rods
FRAPCON iterates to determine fuel rod temperatures, fuel and cladding deformation
This converged data is iterated to produce gas release, void volumes and plenum pressure
Then marches forward in time

## Slide 18: FRAPTRAN
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 19: FALCON
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 20: FALCON
FALCON is a 2D fuel performance code developed by EPRI
Development of FALCON started in 1996
The beta version was released in 2003
It was developed by ANATECH for EPRI
FALCON is proprietary, owned by EPRI
It is no longer under active development in the US

## Slide 21: FALCON is a 2D transient and steady state code
Gap
Pressure is calculated using equation of state
Simplified contact model is used for gap closure
Gap heat transfer model is used
Fuel
Solved with FEM
Solved with FEM
Cladding
Solved with FEM
Solved with FEM

## Slide 22: FALCON can predict the fuel performance in axisymmetric RZ space or in Rθ space

## Slide 23: BISON
Computational cost
Accuracy
Transient, full 3D
Transient, 2D axisymmetric with discrete pellets
Transient, 2D axisymmetric with smeared pellets
Transient, multiple 1D slices (1.5D)
Transient, 1D
Steady state, 1D (analytical)
Steady, multiple 1D slices (1.5 D)

## Slide 24: BISON
The next generation fuel performance code under development in the US
It uses the MOOSE framework
Development was begun in 2008
The first paper using BISON was published in 2009 and the paper summarizing its full capabilities was published in 2012
It was developed at Idaho National Laboratory, with some support by ANATECH
BISON is available for free, but it is export controlled and requires a license agreement be signed

## Slide 25: BISON models the fuel behavior ranging from 1D to full 3D and uses FEM
Gap
Pressure is calculated using equation of state
Fully implemented implicit contact algorithm
Gap heat transfer model is used
Fuel
Solved with FEM
Solved with FEM
Cladding
Solved with FEM
Solved with FEM

## Slide 26: Can handle smeared or discrete pellets, asymmetric pellet geometry and deformation

## Slide 27: Because of its unique 3D capability, BISON can model truly 3D fuel performance problems

## Slide 28: Other countries have other fuel performance codes
http://www.materials.cea.fr/en/PDF/PLEIADES-Platform.pdf

## Slide 29: OFFBEAT – new(ish) tool
The OpenFOAM Fuel BEhavior Analysis Tool (OFFBEAT) is a multi-dimensional fuel performance code developed in Switzerland
The code can be used both for studying complex 2D or 3D local effects and for more traditional 1.5D base irradiation analyses
OFFBEAT is based on the open-source C++ library OpenFOAM, thus the governing equations are discretized with modern finite volume techniques

## Slide 30: Summary
Fuel performance codes are focused on predicting the center temperature of the pellet and the stress in the cladding
All fuel performance codes
  Numerically model the temperature in the fuel
  Numerically model the stress in the cladding
  Consider gap pressure, closure, and heat transfer
The primary US codes are
  FRAPCON – Steady state 1.5D, uses finite difference
  FRAPTRAN – Transient 1.5D, uses finite difference
  BISON – Steady or transient, 1D – 3D, uses finite element

## Slide 31: Material Property Evolution

## Slide 32: Pretty much everything we have learned so far, nothing changes once the fuel and cladding reach steady state

## Slide 33: Fuel is dynamic!

## Slide 34: Property changes due to microstructure evolution during reactor operation must be considered
Mid Life
Point defect diffusion
Point defect clustering
Fission gas segregation to GB and voids
Bubble nucleation
Zinkle and Singh 2000
Late life
Fission product swelling
Bubble percolation and fission gas release
Cladding creep
Fuel creep
Brohan 2000
Insertion in reactor
Removal from reactor
Fuel Fabrication
Sintered UO2
Height 2 cm
Diameter 1 cm
~10 μm grain size
Density > 95%
From Pedro Peralta, ASU
Fuel failure
Pellet/cladding interaction
Cladding corrosion
Cladding fracture
Santana et al. 2011
Early life
Thermal expansion
Fracture
Point defect and fission gas generation
Fuel Densification

## Slide 35: The properties and performance of a material are a result of factors across various length scales
Chemical bonds
Crystal structure
Defect interactions
Microstructure
Material properties and performance

## Slide 36: The crystal structure of a material is the shape of the ordered structure of the atoms
The atoms of many materials form an organized lattice, these are called crystalline materials. All reactor materials are crystalline.
The configuration of the atoms in the lattice impacts the properties of the material (density, thermal expansion coefficient, elastic modulus, etc.)
All major light water nuclear materials are either cubic or hexagonal
(d) Hexagonal close packed

## Slide 37: Crystalline materials
In crystalline materials, the lattices are not perfect, they have defects
Defects can be 0D, 1D, 2D, 3D
The interactions between defects seriously impact material properties and how they perform

## Slide 38: Point defects
Point defects (zero-dimensional defects) are lattice imperfections related to one or two lattice sites
There are several types of point defects
  Vacancies
  Self interstitial atoms (SIA)
  Interstitial impurity atoms
  Substitutional impurity atoms
Point defects control the mobility of atoms and, therefore influence all processes that depend on diffusion

## Slide 39: Point defects
Vacancies and interstitials form naturally in materials
Extra atoms can sit on a surface, creating a vacancy, or a surface can have a missing atom, creating a self interstitial atom (SIA)
We define the number of vacancies or interstitials in terms of a concentration
There exists an equilibrium concentration of point defects

## Slide 40: Radiation damage
Ionizing radiation can introduce defects into the crystal lattice, called radiation damage
PKA collisions create a collision cascade, which results in the generation of defects (point and clusters)