## Slide 1: NE 591: Advanced Reactor Materials
Fall 2021
Dr. Benjamin Beeler

## Slide 2: Last Time
Thermal conductivity degradation
  fission gas swelling/porosity, sodium infiltration
Fuel-cladding mechanical interaction
  fuel swelling, creep, internal pressure, etc.
Fuel-cladding chemical interaction
  phase diagrams and kinetics, low melting points, intermetallics, etc.

## Slide 3: Reprocessing
Pyroprocessing
For more than 50 years, pyrometallurgy has been studied as an alternative strategy in the reprocessing of used fuel
Pyrochemical processes rely on refining techniques at high temperature (500–900 C) depending on the molten salt eutectic used
Typically, chloride systems operate at lower temperature compared to fluoride systems, and are preferred in processing
These processes are mainly based on electrorefining or on extraction from the molten salt phase into liquid metal
Two processes-one for oxide fuel and one for metallic fuel-have been developed to near industrial scale

## Slide 4: IFR Pyroprocess
This process was developed in the US to be part of the IFR project, and can handle the treatment of transuranics
The fuel is recycled using an electrochemical process based on molten chloride salts and liquid metals
The molten salt medium for electrorefining is a solution of a certain amount of UCl3 dissolved in a LiCl–KCl eutectic

## Slide 5: IFR Pyroprocess
The fuel is electrochemically dissolved using a potential between the basket (loaded with used fuel) as anode and a stainless steel electrode in the salt as the cathode
Uranium and TRU are deposited on the anodes
Once the fuel is dissolved and most of the uranium is deposited on the solid steel, this cathode is replaced by a liquid cadmium cathode, and the remaining TRUs can be codeposited with the remaining uranium

## Slide 6: IFR Pyroprocess
The alkali, alkaline earth, rare earth, and halide FPs remain primarily dissolved in the salt phase
More than 90% of the noble metal FPs and fuel alloy material are retained in the chopped fuel cladding segments in the anode baskets
Can reduce the repository burden of radioactive waste by separating long-lived MA from spent light-water reactor fuel, burning MA in fast reactors, and decreasing the long-term radioactivity of nuclear waste

## Slide 7: Refabrication
Metal-fueled fast reactors facilitate the effective transmutation of MA because of the high-energy neutron spectrum
One of the measures to load MA into the reactor core is to add MA to the fuel alloy homogeneously
Can perform injection casting in the same manner as the fresh fuel, to form MA-bearing fuel alloys
These technologies are expected to reduce the fuel cycle cost even for small-scale fuel cycle plants because of the simplicity of the process and the compactness of the equipment
For example, in the injection casting process, composition adjustment, melting (alloying), and casting of the fuel slug can be done in a single injection-casting furnace

## Slide 8: Metallic fuel performance modeling

## Slide 9: Metallic Fuel Phenomena

## Slide 10: Constituent Redistribution Models
Constituent redistribution is driven by:
  temperature gradients in the fuel,
  solubility gradients in a phase and phase boundaries,
  additional chemical potentials applied by fuel– cladding gap and cladding
Results in three concentric zones, namely, a Zr-enriched central zone, a Zr-depleted and U-enriched intermediate zone, and a slightly Zr-enriched zone on the outer periphery
Migration quickly levels off early in life after a new distribution settles

## Slide 11: Constituent Redistribution Models
While ternary phase diagrams exist, their accuracy is suspect, and simplified pseudo-binary phase diagrams can be more easily implemented, and removes complexities associated with largely unknown phases
When applied to a fuel with different Pu content, the phase diagram must be modified accordingly

## Slide 12: Constituent Redistribution Models
Using the calculated phase fractions, the Fickian and Soret diffusion coefficient are determined
Artificial factors are used to set the diffusivity in two-phase regions and to scale diffusivities in each phase
The magnitudes of diffusivities in each phase are largely unknown, and effectively wholly unknown in two-phase regions
BISON Zr Diffusion Model

## Slide 13: Temperature Predictions
Constituent redistribution relies on accurate temperature profiles
Fuel temperature is affected by the thermal conductivity of the fuel, which in turn is changed by porosity evolution and sodium infiltration, in addition to changes in Zr concentration
BISON thermal conductivity models exist for the distinct phases/species, and account for degradation of thermal conductivity

## Slide 14: Porosity Predictions
BISON utilizes a simplified model for porosity
The mechanical force balance on an equilibrium bubble can be expressed by the Young-Laplace equation
Making assumptions for creep stress, bubble size, can calculation swelling due to fission gas
Finally, can determine porosity from the swelling
Solid fission products are a function of fission density

## Slide 15: Porosity Predictions
These porosity models don’t incorporate different phases, initial porosity, axial/radial swelling, etc.
These models have been updated slightly to improve code robustness, but still don’t incorporate these critical microstructural phenomena

## Slide 16: Mechanical Properties
Young’s Modulus
Poisson’s ratio
Creep
Cladding models for HT-9 creep and kth

## Slide 17: BISON Testing
BISON can handle binary and ternary fuel and compare reasonably well with EBR-II data
Discrepancies are due to inadequate knowledge of materials models, and underlying issues with material descriptions, and code robustness
Development is ongoing, and improvements to swelling models, for example, have been made

## Slide 18: Other Codes
LIFEMETAL
The code has evolved from the LIFE series of codes from ANL that perform steady-state and transient analyses for nuclear fuel
The original code was developed for UO2 and mixed oxide fuels for use in fast reactor systems
The code was developed in association with the IFR and has been extensively used for planning steady state and transient experiments at EBR-II

## Slide 19: Other Codes
ALFUS
JAEA code that is multiphysics in nature and focuses on the mechanical behavior of the fuel under irradiation
Both LIFE-METAL and ALFUS are capable of simulating metal fuel irradiation behavior to some extent
Both lack different swelling in different radial zone, coupling of redistribution, realistic predictions of FCCI

## Slide 20: Mixed oxide fuel

## Slide 21: MOX Introduction
Despite some disadvantages, such as its low U density, poor thermal conductivity, and its chemical reaction with sodium, MOX fuel (U,Pu)O2 is the fuel that has been used most in fast reactors
In order to avoid the dramatic swelling of metallic fuels, MOX fuels were explored in fast reactors
Behavior was observed to be satisfactory and was relatively widely implemented in SFRs

## Slide 22: MOX Fuels in SFRs
SRFs with MOX fuel will lead the MOX to run at higher temperatures than LWR fuel, and thus with different properties
Fission product phases and evolving microstructures create highly localized properties that can differ significantly from the bulk fuel
Stoichiometry and Pu content are important factors that dictate thermal properties

## Slide 23: MOX Restructuring
Oxide nuclear fuels are commonly touted for their outstanding high temperature capabilities under irradiation, but this stability comes the tradeoff of low thermal conductivity
Due to the low thermal transport, a steep temperature gradient is formed along the radius of the fuel pellet, with the hottest region at the center of the pellet and coolest near the cladding
This leads to grain growth and restructuring
Pu bearing fast reactor oxide fuels display four defining regions of a restructured pellet:
  the central void, the columnar grain growth region, the equiaxed grain growth region, and the as-sintered region
The higher temperatures and heating rates form coarse, elongated grains that grow radially toward the outer rim of the fuel

## Slide 24: MOX Restructuring
The equiaxed region consists of grains that have undergone significant growth when compared to the un-irradiated samples
Central voids have been shown to appear in irradiation times as short as 10 min, demonstrating that the appearance the central void is a result of fuel temperature and linear heating rate, not high burnup
The central void forms from the accumulation of voids and pores present in the fuel along a thermal gradient

## Slide 25: MOX Pore Formation
Heating Rate

## Slide 26: MOX Pore Formation
The smallest spherical pores are highly mobile, being able to quickly and easily move through the restructured region
Intermediate sized pores become flat and elongated as they travel towards the fuel centers, leaving streaks at the tips of the voids as they travel
These “lenticular” voids are the most readily identifiable porosity feature in the irradiated MOX fuels due to their distinct shape

## Slide 27: Redistribution of Pu
The movement of pores leads to a redistribution of plutonium

## Slide 28: Sodium coolant

## Slide 30: SFR Cladding
HT9 is the current cladding material of choice for SFRs
HT9 is a nonswelling ferritic/martensitic stainless steel
The rate of cladding strain has increased for the initially 85% fuel smeared density elements
12.5% BU

## Slide 31: Questions?