## Slide 1: NE 795: Advanced Reactor Materials
Fall 2023
Dr. Benjamin Beeler

## Slide 2: Last Time
Carbides have high fissile density and high thermal conductivity
He-bonded and Na-bonded designs for liquid metal or gas cooled reactors
Higher swelling and lower FGR than oxide fuels
Two primary phases: UC and U2C3
Three stages in burnup that affect fuel temperature
FGR dependent upon temperature, occurs <3 at% burnup
Fuel restructures into typically three zones with variable porosity
Properties dependent upon impurities and composition

## Slide 3: Carbide FCCI
FCCI in fuel pins containing carbide fuel consists of clad carburization, slight reaction with FPs, and formation of intermetallic compounds
Carbides generally present fewer compatibility problems than MOX fuels
Chemical Reactions with FPs
Very little available oxygen leads to FP-C interactions, and we have an expected decrease in C/M ratio with burnup
Significant FP-cladding interactions are generally not seen
Some Te intergranular attack, some reaction with iodine
Generally not a concern

## Slide 4: Carbide FCCI
Low melting phases
Hypostoichiometric carbide fuels can contain U/Pu metal as a second phase which can form intermetallic compounds with the cladding
Experimental compatibility tests of (U,Pu)C with cladding have shown intermetallic compounds such as (U,Pu)Fe2 or (U,Pu)Ni5 in the fuel and cladding interface
At typical fuel surface temperatures (~1000K), reaction rates should be slow to create intermetallics
However, if sufficient hypostoichiometry is present, can react to form intermetallics

## Slide 5: Cladding Carburization
Carbide fuels are designed to be hyperstoichiometric, which results in a two-phase UC/U2C3 microstructure
The presence of excess carbon prevents the formation of intermetallic phases, but carburizes the cladding
The decarburization of fuel and the carburization of cladding are governed by the dissolution of carbon atoms from the fuel and then diffusion into cladding
Cr forms very stable carbides, and carburization often takes the form of Cr23C6 precipitation

## Slide 6: Cladding Carburization
Cr23C6 precipitation starts at the grain boundaries, and then can proceed along preferred crystallographic planes
The carburization proceeds deeper into the material
The grain boundary carbides can lead to intragranular failure of the steel after only a moderate burnup
Austenitic stainless steels are very susceptible to carburization and are deemed too brittle if carbon content reaches 0.6 wt.%

## Slide 7: Cladding Carburization
Carbon activity and partial pressure of CO are important parameters responsible for clad carburization
In sodium-bonded fuel, carbon transfer from the fuel to the clad takes place by dissolution of carbon in sodium liquid
In He-bonded fuel pins, carbon transfer takes place through CO
Out-of-pile testing with Na-bonded fuel showed carburization above 1000 K, with hardening of the SS316 cladding up to 100 mm
The depth of carburization in Na-bonded fuel was greater than in the He-bonded pins

## Slide 8: Cladding Carburization
Cladding temperature plays a critical role in carburization
The temperature gradient in the fuel causes carbon to migrate to colder zones in the fuel, increasing the C/M ratio at the pellet surface
Carburization depth shows a strong dependence on cladding temperature
Carbon penetration seems to follow a diffusion process with a constant surface concentration

## Slide 9: Na Bonded Pin Performance
For the sodium-bonded fuel pin, the smear density is lower than that of He-bonded fuel
This allows for the manufacture of a denser fuel with less initial porosity
In the beginning (stage A), the fresh fuel fractures, reducing thermoelastic stresses and drastically changing temperature gradient of the fuel
There is no abrupt change in fuel temperature in this concept
The lower temperature of the sodium-bonded pin keeps the swelling rate of the fuel low
The decrease in thermal conductivity with burnup is compensated by a slow decrease in linear heating
FCMI can be avoided till end of life by proper selection of initial fuel–clad gap
Na bond acts like a medium for transfer of carbon from the fuel to clad, causing clad carburization

## Slide 10: He Bonded Pin Performance
He bonding is the most preferred bonding concept of carbide fuel, due to cost and the potential for Na bond deterioration at high burnup
The in-pile performance of the He-bonded pin depends to a large extent on the porosity of the as-fabricated fuel
The initial temperature rise is much higher at the beginning of life because of the lower thermal conductivity of the He bond compared to Na bond
The lower thermal conductivity of the He bond requires the reduction of the fuel–clad gap compared to the Na-bonded fuel
The fuel density for He bonded fuel is lower and has a fabrication porosity of about 15%
The gap closure in the early burnup period results in lowering of the fuel temperature, and free swelling changes into restrained swelling under the contact pressure developed at the clad–fuel interface

## Slide 11: Pin Failure
The mechanical properties of the fuel and clad (creep, fracture toughness) largely predict the fuel behavior after gap closure
Cladding breaches due to FCMI or FCCI can be due to loss of ductility of the clad, carburization of the clad, or fuel swelling
Clad carburization makes the clad surface hard and brittle and cracks form and propagate easily
It has been observed that the He-bonded pin can be operated safely up to 15 at.% burnup (peak burnup 20 at.%).

## Slide 12: Carbide Fabrication
Fabrication of carbide fuel on commercial scale is a difficult task and needs additional care because of its pyrophoricity, high radio toxicity, and the concern for criticality restricts the batch size
Carbide powders formed during carbothermic reduction of oxides are prone to oxidation and hydrolysis
This requires high-purity inert-gas cover in the fabrication line consisting of glove boxes

## Slide 13: Fabrication Techniques
Melting casting
In this method, UO2 or U metal chips with graphite are arc-melted and made into the form of a button
Melting casting route results in large-grained materials compared to that obtained by powder metallurgical methods
The melting casting method is, however, uneconomical due to the high cost of metal fabrication
Metal hydriding– dehydriding
This method is followed for small-scale production of high-purity carbides, where the metal hydride reacts with graphite
Actinide carbides MC and M2C3 can be prepared from a mixture of hydride and graphite
For UC, the reaction between uranium metal and a hydrocarbon gas (methane) is carried out with careful control of the hydrocarbon flow

## Slide 14: Carbothermic Reduction
Uranium monocarbide is mainly produced by carbothermic reduction of UO2 and carbon following the reaction
A mixture of UO2 and carbon is blended together and the mixture is compacted at 300–600 MPa along with an organic binder
The pellets are heated in a vacuum induction furnace and ground to a powder for compaction

## Slide 15: Carbothermic Reduction
Uranium–plutonium-mixed carbide is also prepared by carbothermic reduction of UO2–PuO2
The physical state and homogeneity of the mixture influences the reaction rate and the quality of the final product
The reaction is complicated by the uneven distribution of plutonium in the two carbide phases and the formation of CO2 and CO, especially in hyperstoichiometric feedstock
Pu can volatilize and evaporate, which needs to be controlled via increased CO partial pressure
Carbothermic reduction temperature also depends on the Pu content of the material

## Slide 16: Pressing
The conventional powder metallurgy route of carbide fuel fabrication has certain disadvantages, including pick up of O/N impurities from the cover gas and risks of pyrophoricity
Direct pressing takes the product of carbothermic reduction and presses them into a low density pellet, which can be sintered into the final product
This reduces O pickup, reduces dust and impurities, and reduces time/cost
There is an additional route that involves wet processing of nitrate-based fuels in a sol-gel technique

## Slide 17: As-fabricated microstructures
Carbide pellets are susceptible to surface defects, such as chips and cracks
As in all sintered materials, residual porosity will be present
Varying degrees of the M2C3 phase will be present and are observable via characterization
Mixed carbide fuel with (a) 70%PuC and (b) 20%PuC showing bright/white areas of sesquicarbide phase

## Slide 18: nitride fuels

## Slide 19: Nitride Fuels
Nitride fuel has been proposed as an advanced fuel for fast reactors and developed since the 1960s and tested in the BR-10, MTR, and EBR-II reactors
Nitride fuel is often a solid solution of uranium mononitride (UN) and plutonium mononitride (PuN), in which the Pu/(U+Pu) molar ratio ranges from 0.15 to 0.25
Nitride has potential applications as a fuel for space reactors, large breeder reactors, different Gen IV fast reactors, accelerator-driven systems, and small modular reactors
UN is now also being considered as an accident tolerant fuel for LWRs

## Slide 20: Nitride Fuel Benefits
Higher fissile density: 40% more uranium in UN than in UO2, leading to higher conversion ratios, and potentially higher burn-ups
Higher thermal conductivity: reduction of the fuel centerline temperature, increase in the margin for fuel melting, delay the migration of fission products and actinides
Reprocessing: readily dissolve in nitric acid (HNO3), making this fuel compatible with the PUREX process
Stability: chemically compatible with most potential cladding materials, good irradiation stability
Potential for longer fuel cycle: neutronic behavior of UN can extend cycles from 18 to 25 months, reducing costs and down time

## Slide 21: Nitride Properties
Best of both worlds fuel; with high melting point, high fissile density, and high thermal conductivity

## Slide 22: Drawbacks of Nitrides
Fabrication: the production of MA or Pu-containing nitride fuel is not straight forward and requires some difficult production steps
Oxidation resistance: the nitride pellets readily oxidize in superheated steam
Nitride powder is pyrophoric, requiring strict atmospheric controls during fabrication and handling
Fuel enrichment: the nitrogen component has to be highly enriched in 15N to increase the neutron economy and avoid the (n, p) formation of 14C from 14N, which significantly increases costs
Fuel fabrication and N enrichment have led to slower development of MN fuels than MC fuels

## Slide 23: Irradiation History of Nitrides
The experience from irradiation of nitride fuels consists of about 1400 UN rods, 300 (U,Pu)N rods, and a few inert matrix and MA-bearing rodlets
UN was used as a driver fuel for BR-10 for 18 years, and this is where the majority of the irradiation data comes from
Similar to carbides, both Na-bonded and He-bonded pins have been studied, the majority being He

## Slide 24: UN Phase Diagram
There are two main uranium nitrides, UN and U2N3; the former has an NaCl-type cubic structure, and the latter has an M2O3-type cubic structure at low temperature (alpha-U2N3) and a hexagonal structure at higher temperature (beta-U2N3)
The phase diagram of U–N is complicated since the diagram depends on nitrogen pressure
There is still uncertainty regarding the phase diagram

## Slide 25: UN Phase Diagram
Where nitrogen pressure is greater than 105 Pa, UN melts at 3123K and that UN and U2N3 have a wide range of nonstoichiometry
At lower nitrogen pressure (<2E5 Pa) UN decomposes such that UN and U2N3 have little nonstoichiometry
At low PN, the beta-U2N3 phase changes to UN2
U2N3 decomposes to UN, and UN decomposes to U and nitrogen at nitrogen pressure below 2.5 atm

## Slide 26: UN Decomposition
The decomposition of U2N3 is the last stage in the formation of UN through carbothermic reduction, thus the equilibrium nitrogen pressure of UN and U2N3 is very important from the viewpoint of their use as nuclear fuels
UN decomposes at 3073K and U2N3 decomposes 1620K at nitrogen pressure of 1 atm

## Slide 27: MN Crystal Structure
UN has same NaCl-type close-packed structure as UC
Several actinides also share this NaCl-type structure, and thus can exist as substitutional species in UN/PuN
Allows for fabrication of homogeneous mixed nitride fuels, including MA-bearing fuels

## Slide 28: Ternary U/Pu-N
The ternary system is characterized by a complete solubility of UN and PuN
The (U,Pu)N phase has a narrow composition range of the N/(U+Pu) molar ratio
Although Pu2N3 does not exist in the Pu–N system, a sesquinitride phase was identified in the U–Pu–N system at a Pu/(U+Pu) molar ratio of 0.15
In a mononitride lattice with NaCl-type structure, small nitrogen atoms are incorporated into a dense face-centered cubic packing of metal atoms

## Slide 29: Effect of Pu on U/Pu N Properties
The addition of Pu can dramatically affect thermophysical properties
Pu is more volatile than U, and has a higher vapor pressure
Pu degrades the thermal conductivity by as much as 2X
PuN is less stable than UN, and could be susceptible to radiolysis

## Slide 30: UN Irradiation Performance
The irradiation experience of nitride fuel is rather limited in comparison with the other fuels for fast reactors, such as oxide, metallic, and carbide fuels
The number of (U,Pu)N fuel pins irradiated in fast reactors so far is smaller than 200
UN pins have reached 10% FIMA in fast reactors, and greater than 15% FIMA in thermal reactors

## Slide 31: UN Pins
Similar to carbides, pin designs are either He-bonded or Na-bonded
He-bonded fuel pin is characterized by low-density pellets (80–85% of theoretical density (TD)) and a small gap
Na-bonded fuel pin is characterized by high-density pellets (>90% TD) and a large gap
Na-bonded concept has the advantage of keeping the fuel temperature relatively low due to good thermal conductivity of liquid Na
Difficulties with Na are the reactivity in air, and additional hurdles in fabrication and reprocessing

## Slide 32: UN Pins
The He-bonding concept is considered as the reference for (U,Pu)N fuel
The temperature of fuel pellets becomes high in comparison with the fuel with Na bonding, especially at an early stage of irradiation
The small gap is closed by free swelling of fuel pellets at a burnup of 2–3% FIMA

## Slide 33: Temperature with Burnup
Similar to carbides, have three stages in temperature
Stage A is the first rise of power and lasts for one to several days
Stage B has the resintering of pellets center and closure of He gap
Stage C is the quasi steady state irradiation period in which FCMI begins
The TD of the fuel is reduced to ~80% to avoid excessive strain on the cladding