## Slide 1: Nuclear Fuel Performance
NE 591

## Slide 2: Last Time
Mining -> Processing -> Conversion -> Enrichment -> Powder -> Compaction/Sintering -> Rod/Assembly
U3O8 must be converted to UF6 for enrichment, which is then converted to UO2 powder for pellet manufacture
For different fuel types, enriched UF6 follows a different path

## Slide 3: Last Time
General heat transport
Heat is produced in the fuel, transports through the gap and cladding, and into the coolant
The geometry of our problem
The initial condition of T
The boundary conditions of T
Is each parameter is a function of T
  Thermal conductivity, heat capacity
Function of space/time?
  Heat generation, dependent upon flux

## Slide 4: Analytical solve of heat conduction

## Slide 5: The most accurate solution is numerical, in 3D, requires modeling the entire core, and is multi-physics
Solution is 3D and changes in time
All the properties are functions of temperature
The boundary conditions comes from information about the coolant flow
The heat generation rate comes from information about the neutronics in the reactor
No analytical solution is possible

## Slide 6: In order to solve, make assumptions!
#1: steady state ->
#2: axisymmetric ->
#3: constant in z
#4: constant thermal conductivity

## Slide 7: Directly Solving for Temperature Profile
Boundary conditions: r0 = 0, r1=R, T’(0) = 0, T(R) = Ts
r0
r1

## Slide 8: Linear Heat Rate
  Where Qav is the radially averaged heat generation rate, in units of per-length, i.e. W/cm
Substitute LHR into previous equation on T0-Ts

## Slide 9: Alternate Geometries
Similar derivation with appropriate boundary conditions can be applied to plate and sphere geometries
Plate
x is the distance from the midplane of the fuel and tf is the plate fuel thickness
Sphere
r is the distance from the sphere center and Rf is the radius of the sphere

## Slide 10: Heat transport through the gap
The heat flux gives the rate, per unit area, at which heat flows in a given direction
The heat flux from the fuel is the LHR/pellet circumference
Heat flux from the fuel is the same as heat flux through the the gap – can make this assumption because Rf >> tg
Gap thickness = RIC-Rf = tg
Cladding thickness = ROC-RIC = tc
R0=0
R1=Rf
R2=RIC
R3=ROC

## Slide 11: Heat transport through the gap
Set heat flux fuel/gap equal
Gap conductance is defined as:
Gap conductance depends on the gas filling the gap
  For pure He, kgap=16x10-6 * T0.79 (W/cm-K)
  For pure Xe, kgap=0.7x10-6 * T0.79 (W/cm-K)
  Simple mixing rule: kgap = kHe(1-y) + kXey
    Where y is the mole/atom fraction of Xe
=

## Slide 12: Heat transport through the cladding
Heat flux through the cladding
Set equal your heat fluxes

## Slide 13: Heat transfer to the coolant
Heat is transported from the cladding to the coolant via convection
Tcool is the coolant temperature, hcool is the convective heat transfer coefficient between cladding wall and coolant
Adding gap + cladding + coolant:
+

## Slide 14: Summary of analytical solutions

## Slide 15: Solving for the temperature profile
You first solve for the transition temperatures.
Start from the coolant and work inward
Have a linear profile everywhere except in the fuel
Finally, solve for the temperature profile throughout the fuel
  TCO TCI
Tcool

## Slide 16: Fuel and Cladding Thermal Properties
Material | Density (g/cm3) | Heat Capacity Cp (J/g-K) | Thermal Conductivity k (W/cm-K) | Thermal Expansion Coefficient a (K-1)
UO2 | 10.98 | 0.33 | 0.03 | 1.2 x 10-5
Zr | 6.5 | 0.35 | 0.17 | 1.0 x 10-5
Stainless steel | 8.0 | 0.5 | 0.17 | 9.6 x 10-6

## Slide 17: Example Problem

## Slide 18: Temperature profile calculation example
Tcool = 580 K; LHR = 200 W/cm; hcool = 2.65 W/cm2-K
Rfuel = 0.5 cm; tclad = 0.06 cm; tgap = 0.003 cm; kf=0.03 W/cm-K
Work from outside->in, calculate cladding temperature
  Tco = (200)/(2*pi*0.5*2.65) + 580
  Tco = 604 K
Calculate inner cladding temp
Tci = (200*0.06)/(2*pi*0.5*0.17) + 604
Tci = 626 K

## Slide 19: Temperature profile calculation example
Calculate fuel surface temperature
Calculate gap conductance
  gap with He; kgap=16x10-6 * T0.79 (W/cm-k) ; assume Tci is appropriate for entire gap; kgap = 0.0026 W/cm-K; tgap = 0.003 cm
  hgap = 0.87 W/cm2-K
Tfuel = 200/(2*pi*0.5*0.87) + 626
Tfuel = 699 K

## Slide 20: Temperature profile calculation example
Calculate centerline temperature
T0 = 200/(4*pi*0.03) + 699
T0 = 1230 K
Full temperature profile

## Slide 21: Temperature profile calculation example
Parabolic temperature profile in fuel
Linear in gap and clad
Steep temperature drop over gap, very low thermal conductivity
Smaller temperature drop over cladding

## Slide 22: Temperature profile modification
Instead of pure He gap, 30% of gas is Xe; how is T0 affected?
First, how is gap conductance affected?
Gap conductance depends on the gas filling the gap
  For pure He, kgap=16x10-6 * T0.79 (W/cm-K)
  For pure Xe, kgap=0.7x10-6 * T0.79 (W/cm-K)
  Simple mixing rule: kgap = kHe(1-y) + kXey
  TCI, TCO, and Tcool is unchanged from previous example, also T0-Tfuel is unchanged
  kgap = ((16x10-6)*(626)0.79 )(1-0.3) + ((0.7x10-6)*(626)0.79 )(0.3) = 1.85E-3 W/cm-K

## Slide 23: Temperature profile modification
kgap = 1.85E-3 W/cm-K
hgap = 1.85E-3 / 0.003 = 0.62 W/cm2-K
Tfuel = 200/(2*pi*0.5*0.62) + 626 = 729 K
T0 – Tfuel = 530.5 K (unchanged from before)
T0 = 729 + 530.5 = 1259.5 K
Increase in T0 of 30 K
Caveat: linear mixing of gases is not the best approach

## Slide 24: Neutron flux varies axially, so does LHR
Taking a fuel rod with length, L = 2*Z0
LHR0 is the midpoint linear heat rate, i.e. @ z=Z0
, where Zex is the extrapolation distance
A typical value is 1.3

## Slide 25: Coolant temperature varies with Z
Each rod has a given flow area
Mass flow rate:
Coolant specific heat:

## Slide 26: Calculate LHR and Tcool with axial variation
mdot = 0.25 kg/s-rod; Z0 = 150 cm; LHR0 = 150 W/cm; CPW = 4200 J/kg-K; Tin= 570 K

## Slide 27: Summary
Developed analytical expressions for the temperature profile within a fuel rod
Required to make four assumptions:
  Steady-state solution
  Temperature is axisymmetric
  T is constant in Z
  Thermal conductivity is independent of temperature
Temperature profile in the fuel is parabolic, assume linear profiles in gap, clad and coolant
Can incorporate axial variation in Tcool with axial variation in LHR