## Slide 1: Fuel Types
NE 591: Nuclear Fuel Performance
Dr. Benjamin Beeler

## Slide 2: Fuel is the Heat Source
Fuel functions as a heat source, generating heat that is transferred to a coolant, which transfers heat through external loops, heat exchangers, etc., to run a generator

## Slide 3: Only certain materials can be used as nuclear fuel
A fissionable nuclide is capable of undergoing fission (even with a low probability) after capturing a high energy neutron
A fissile nuclide is capable of sustaining a nuclear fission chain reaction with neutrons of any energy
A fertile nuclide is a nuclide that, although not itself fissionable by thermal neutrons, can be converted into a fissile nuclide by neutron absorption
The fissile rule states that for a heavy element with 90 ≤ Z ≤ 100, its isotopes with 2 × Z – N = 43 ±2 are fissile (with some exceptions)

## Slide 4: Let’s try out the fissile rule
The heavy elements with 90 ≤ Z ≤ 100
  Thorium (Th), Protactinium (Pa), Uranium (U), Neptunium (Np), Plutonium (Pu), Americium (Am), Curium (Cm), Berkelium (Bk), Californium (Cf), Einsteinium (Es) and Fermium (Fm)
First, we will apply the fissile rule to U (2 × Z – N = 43 ±2)
  N = 2 Z – (43 ± 2)
  N = 2 × 92 – [41, 42, 43, 44, 45] = [143, 142, 141, 140, 139] neutrons
  So, U-231 through U-235 should be fissile

## Slide 5: There are only four fissile nuclides that are practical for nuclear fuel
U-235
  Naturally occurs in uranium in small amounts (0.7%). Can be enriched
Pu-239
  Bred from U-238 by neutron capture
Pu-241
  Bred from Pu-240 (which comes from Pu-239) by neutron capture
U-233
  Bred from Th-232 by neutron capture

## Slide 6: Fuel Types and Associated Reactor Types
UO2 – Light Water Reactors
  MOX
  ATF
UZr – Sodium Cooled Fast Reactors
UMo – Research Reactors
UC/UCO – High Temperature Gas Reactors
UN – Lead Cooled Fast Reactors

## Slide 7: Uranium Dioxide (UO2)
Reference fuel for nuclear power industry
Single phase, fluorite structure
Fabrication via sintering UO2 powder into pellets
Water coolant
Pellets are stacked inside Zircaloy cladding tubes

## Slide 8: UO2
Good!
  Very high melting point, about 2800 C
  Maintains a stable fluorite phase up to melting
  Very compatible with Zircaloy clad (no interaction zones forming/no FCCI)
  Relative stability in water
  Reasonably radiation resistant
    no amorphization
    Can incorporate a large number of fission products as substitutional defects

## Slide 9: UO2
Bad!
  Brittle
    thermal stress fractures, fragmentation
  Poor thermal conductivity
  Properties very sensitive to stoichiometry
  Limited linear heating rates
  Non-negligible thermal expansion/swelling