## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2025

## Slide 2: Last Time
Solid mechanics predicts the deformation of a body from its applied load
Elastic deformation and plastic deformation
Concepts of stress and strain
Elastic moduli and Elastic constants
Work hardening/strain hardening
Toughness, ductility, DBTT, etc.
Thin-walled cladding stresses

## Slide 3: Mechanics

## Slide 4: Small strain theory
In continuum mechanics, the infinitesimal strain theory is a mathematical approach to the description of the deformation of a solid body in which the displacements of the material particles are assumed to be much smaller than any relevant dimension of the body so that its geometry and the constitutive properties of the material at each point of space can be assumed to be unchanged by the deformation
With this assumption, the equations of continuum mechanics are considerably simplified
The small strain theory is commonly adopted in civil and mechanical engineering for the stress analysis of structures built from relatively stiff elastic materials

## Slide 5: Develop constitutive relations for thick-walled
We assume small strains, so the strain is defined with respect to displacement: u
We assume isotropic material response:

## Slide 6: Stress within a pressurized cylinder that has thick walls (radius/thickness<20)
The cylinder as an inner radius Ri and an outer Radius Ro
We assume there is no shear stress, so σrz = 0
We will begin with the r equation
Now we need our constitutive law
We combine these equations to get

## Slide 7: Develop equations for the stress within a pressurized cylinder with thick walls
We need one more relationship from the definition of the strain
From the previous slide, we have
If we combine these, we get
Again, from the previous slide
We end up with

## Slide 8: We now have an ODE so we can solve to get the stress
Our boundary conditions are σrr(Ri) = -p and σrr(Ro) = 0
After integrating twice, we get
From σrr, we can get σθθ from
From the end condition, we determine σzz
(a)
(b)
(c)

## Slide 9: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  Ri = 0.52, Ro = 0.58 cm, σy = 381 MPa
Which stress is the largest?
  σθθ
At what position r will the hoop stress be the largest?
  r = Ri = 0.52 cm
What is the stress at p = 5 MPa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 46.0 MPa
What is the stress at p = 9 Mpa?
  σθθ = 9*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 82.7 Mpa
Again, we don’t even get close to yielding

## Slide 10: We’ve now solved this same problem assuming thin and thick-walled cylinders

## Slide 11: THERMO-Mechanics

## Slide 12: Thermal Expansion
As the temperature increases, atoms have larger vibrations, causing the material to expand
This expansion doesn’t raise the energy of the material when unrestrained
This expansion can be treated as a strain, but as one that doesn’t cause stress

## Slide 13: Thermal Expansion
In isotropic materials, thermal expansion happens equally in all directions and is linear with temperature
In this equation
  T is the current temperature
  T0 is the temperature the original size was measured
  α is the linear thermal expansion coefficient
  I is the identity tensor

## Slide 14: Thermal Expansion
Though thermal expansion doesn’t directly cause stress, it can still lead to thermal stress

## Slide 15: What is the stress in a thin constrained rod of length L when it is heated to ΔT?
The rod has a Young’s modulus of E and an expansion coefficient of α

## Slide 16: The large temperature gradient within a fuel pellet results in large thermal stresses

## Slide 17: Consider the constitutive relations plus T
We assume small strains, so the strain is defined as
We assume isotropic material response, so

## Slide 18: Consider a cylinder with thermal expansion but not pressure
Similar to the equations we worked through before
Solving this ODE:

## Slide 19: What is the hoop stress in the cladding?

## Slide 20: Where is hoop stress equal to zero?

## Slide 21: The linear temperature gradient across the cladding causes axial thermal stresses

## Slide 22: Same approach to the thermal stress in a fuel pellet
The thermal stress is due to the temperature gradient

## Slide 23: Solve this stress ODE
The boundary conditions are:
Once we solve it, we obtain
Then we can solve the hoop stress
The axial stress is more complicated to obtain, but you end up with

## Slide 24: The fuel temperature gradient causes large thermal stresses

## Slide 25: Example

## Slide 26: How far do fuel cracks extend?
E = 200 GPa, ν = 0.345, α = 11.0e-6 1/K, σfr = 130 MPa, ΔT = 550 K
Solve for η
  – σfr / σ* = 1 – 3 η2
  3 η2 = 1 + σfr / σ*
  η = ( (1 + σfr / σ*)/3 )½
σ* = 11.0e-6*200*550/(4*(1 – 0.345) ) = 461.8 MPa
η = sqrt( (1 + 130/461.8)/3 ) = 0.65

## Slide 27: thermal expansion

## Slide 28: The gap changes as a function of time
Both the pellet and the cladding swell
But, as the gap decreases, the temperature changes, which again makes the gap change
The solution using the analytical equations is iterative, due to the dependence of the gap size and temperature

## Slide 29: Example

## Slide 30: Calculate the steady state temperature profile in the rod, including thermal expansion
LHR = 200 W/cm, δ0gap = 30 μm, Rf = 0.6, Tco = 600 K, TEXP,0 = 373 K, kgap = 0.0026 W/cm-K, tC= 0.06 cm, αf = 11.0e-6 1/K, αC = 7.1e-6 1/K
So, TIC = 600 + 18.7 = 618.7 K, Ts = 679.9 K, T0 = 1210.5 K
First, we will deal with expansion in the cladding
  Av(Rc) = 0.6 + 30e-4 + 0.06/2 = 0.633 cm
  Av(TC) = (600+618.7)/2 = 609.4 K
  ΔRc = 0.633*7.1e-6*(609.4 – 373) = 0.0011 cm

## Slide 31: Calculate the steady state temperature profile in the rod, including thermal expansion
Second, we deal with the fuel
  Av(Tf) = (1210.5 + 680)/2 = 945.25 K
  ΔRf = 0.6*11e-6*(945.3 – 373) = 0.00378 cm
The total change in the gap is 0.0011 – 0.0038 = -0.0027
However, that means the gap is smaller and so our temperatures were wrong!

## Slide 32: This calculation is repeated until the gap width stops changing significantly
The change in the gap does NOT affect the coolant or outer cladding temperatures, just the gap and fuel temperatures
Does fuel centerline temp go up or down with correction?
Iteration | δgap (cm) | Ts (K) | T0 (K)
0 | 0.003 | 701 | 1232
1 | 0.00066 | 644 | 1174
2 | 0.00097 | 652 | 1182
3 | 0.00094 | 651 | 1181
4 | 0.00094 | 651 | 1181

## Slide 33: last bit of Mechanics

## Slide 34: Relating Displacements to Stress
We have been determining the stress due to some internal pressure (or temperature)
Often, the information more readily obtainable are the displacements
Utilizing the previous equations, can use displacement to stress relationships for our geometry

## Slide 35: Assuming problem is axisymmetric

## Slide 36: Solve for the stress from the strain
Assume isotropic materials
Can perform matrix multiplication for the calculation of the stress, given the displacements

## Slide 37: Further simplify the problem to be 1D
No change in Z:

## Slide 38: Determine the strain and stress in the pellet for 1D case
Assume the radial displacement in the fuel pellet is ur(r) = 0.05r cm.
What is the strain tensor? At the outer edge:
We are dealing with UO2, so E = 200 GPa and ν = 0.345
  C11 = E (1 – ν)/((1+ν)( 1–2 ν)) = 200*(1–0.345)/(1.345*(1–2*.345)) = 314.2 Gpa
  C12 = E ν/((1+ν)( 1–2 ν)) = 200*0.345/(1.345*(1–2*.345)) = 165.5 Gpa
Now we can calculate the stresses
  σrr = 0.05*314.2 + 0.05*165.5 = 23.98 GPa
  σθθ = 0.05*165.5 + 0.05*314.2 = 23.98 GPa

## Slide 39: Example problem
Compute the stress and strain tensors in the center and at the outer edge (r = 0.5 cm) in 1D axisymmetric coordinates in a fuel pellet with ur(r) = r2/5. C11 = 314.2 Gpa, C12 = 165.5 Gpa.
First, calculate the strain tensor
εrr = ur,r = 2r/5
εθθ = ur/r = r/5
At the center there is no strain; at the outer edge
To calculate the stress, convert to a strain vector and multiply by elastic constant matrix
The stress in the center is zero
On the outer edge
  σrr = 0.2*314.2 + 0.1*165.5 = 79.4 GPa
  σθθ = 0.1*314.2 + 0.2*165.5 = 64.52 GPa

## Slide 40: Summary
We derived two analytical solutions for the stress in a pressurized cylinder
  Thin-walled cylinder
  Thick-walled cylinder
Increases in temperature cause most materials to expand
We call this thermal expansion, which is a strain that doesn’t inherently cause stress
Thermal expansion can cause stress when
  Deformation is constrained
  There are gradients in the expansion coefficient
  There is a temperature gradient
We developed analytical equations for thermal stresses
  in the cladding
  in the fuel