## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2024

## Slide 2: Housekeeping
MOOSE project due end of next week
Exam next Thursday: 2/29
Problem session next Tuesday: 2/27

## Slide 3: Last Time
Dr. Jiang covered an intro to numerical thermomechanics
Fuel performance codes are focused on predicting the temperature of the pellet and the stress in the cladding
All fuel performance codes
  Numerically model the temperature in the fuel
  Numerically model the stress in the cladding
  And consider gap pressure, closure, and heat transfer in some way
Last-Last Time:
  Gap size change due to thermal expansion
  Intro into defects and materials processing

## Slide 4: mechanistic modeling

## Slide 5: Microstructure-based fuel performance modeling
Operating Conditions
Neutron flux
Variables
Temperature
Displacement
Stoichiometry
Coolant T&P
Fuel
Microstructure variables
Average grain size
Dislocation density
U defect concentrations
Pu concentration
Fission product precipitate fractions
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Crack parameter
Cladding
Microstructure variables
Average grain size
Dislocation density
H concentration
Hydride fraction
Point defect concentrations
Loop density
2nd phase particle fraction
Gap variable
Gap fission gas concentration
Grain growth
Defect prod. & transport
Fission gas behavior
Densification
Microstructure evolution models
Plasticity
Grain growth
Defect prod. & transport
Hydrogen transport
Microstructure evolution models
Loop evolution
Plasticity
Fracture
Structure/property relationships connect the microstructure variables to the property values
Elasticity tensor
Thermal conductivity
Failure criteria
Dimensional change
Yield stress
Cladding
Property values
Elasticity tensor
Fracture stress
Melting temperature
Dimensional change
Thermal conductivity
Diffusion constants
Fuel Property values

## Slide 6: Example: fission gas behavior in the fuel
Take into account a finite set of variables to describe the state of the material
Utilize a mechanistic model of fission gas behavior to predict the evolution of the microstructure
Utilize this updated microstructure to inform a number of structure/property relationships
Model of fission gas behavior
Variables
Temperature
Displacement
Stoichiometry
Structure/property relationships
Elasticity tensor
Fracture stress
Dimensional change
Thermal conductivity
Gap conductance
Gap pressure
Dissolved fission products
Fission gas bubble fraction
Grain boundary fission gas bubble coverage
Gap fission gas concentration

## Slide 7: Multiscale separate effects experiments and simulations inform the development of the models
nm
μm
mm

## Slide 8: Microstructure-based models
Can provide a structure/property relationship to replace the existing burnup dependent model
For example, thermal conductivity, taking into account microstructural features and their evolution
Bulk conductivity
Fission gas
Intragranular porosity
Grain boundary and bubbles
κpr
Precipitated fission products
Vacancies and interstitials

## Slide 9: Parametrizing the mechanistic model
We employ multiscale modeling and simulation to determine the various parameters for the model
MD simulations conducted at LANL have been used to determine the coefficients for various point defects
MD simulations have shown that phonon scattering must be accounted for to accurately represent small bubbles
Mesoscale simulations have shown that GrB bubbles have a larger impact on the thermal conductivity
Maxwell-Eucken (no phonon scattering)

## Slide 10: Parametrizing the mechanistic model
A thermal resistor model is created to describe the impact of GrB bubbles on the thermal conductivity
MARMOT simulations are currently being used to inform the development of the precipitate multiplier

## Slide 11: Parametrizing the mechanistic model
Each term in the expression must be coupled to a corresponding state variable
The full model calculates the thermal conductivity as a function of:
  Temperature
  Point defect concentrations
  Intragranular bubble density and average radius
  Fractional coverage of bubbles on GBs and average radius
  Precipitate volume fractions and average sizes
Currently effects of precipitate fission products and individual point defects are neglected in the model, as they are not tracked or predicted in BISON

## Slide 12: Comparing with experiments…
The model under-predicts the temperature in most cases, but not all
Thus, the model is neglecting some resistive effects from the microstructure
Generally performs as well, and in some cases better, than the burnup based model
RISO-3 AN3
RISO-3 AN4
RISO II-3
US PWR TSQ0002

## Slide 13: UZr Fuel Performance Modeling
Development of a quantitative phase-field model of macroscale constituent redistribution in the U-Zr system, where model parameters were optimized, and the model validated against an independent data set
Calculation of surface tension based on molecular dynamics, which is used in the BISON gaseous metallic fuel swelling model

## Slide 14: U3Si2 Fuel Performance Modeling
Point Defect Diffusion, Fission gas swelling, thermal and irradiation creep

## Slide 15: TRISO Particle Fuel Performance Modeling
TRISO particle modeling is still under development from a mechanistic model standpoint
Imperfect data for many critical fission products through different layers
Data typically for UO2 only, not for UC or UCO fuel kernels

## Slide 16: FeCrAl
Evolution of compositional randomness (precipitation) will affect the mechanical properties of FeCrAl
Kinetic Monte Carlo simulations modeled the precipitation of alpha’ phase from bcc Fe-Cr alloys under thermal aging at various temperatures
Fe-Al alloys do not show any phase separation
Can determine critical temperatures for precipitation and the resulting microstructures to investigate potential hardening

## Slide 17: Summary
Researchers are working to develop materials models for the fuel and cladding that are mechanistic rather than empirical and that are based on the evolution of the microstructure rather than the burnup

## Slide 18: UO2 Radiation effects

## Slide 19: Radiation Damage
The macroscopic and observable results of exposure of solids to energetic particles are collectively known as radiation effects
Heat production from the nuclear fuel to generate electricity ensues mostly from the slow down of the fission products by nuclear or electronic interactions
As a direct consequence, there are also defects created along the path of the fission fragments leading to modification of the physical properties of the fuel
Most Frenkel defects (interstitial-vacancy pair) are produced by secondary collision cascades
Local charge neutrality prevents the formation of interstitials and vacancies as independent processes, as the cations and anions are charged species
In UO2, two anion vacancies need to be created for each cation vacancy, forming a Schottky trio
The dominant defect type is anion Frenkel pairs

## Slide 20: Loop Formation
Dislocations generally a mixture of screw and edge components in the shape of a loop
The most important slip system in UO2 is the one which minimizes the electrostatic energy, the easy slip along {100}<110> tends to minimize the intense repulsive force between cations
Prismatic loops are of interstitial type and consist of a disc-shaped layer of defects in a cluster
This defect cluster is more energetically favorable than dispersed defects in the bulk
Vacancy clusters will form into voids
Prismatic loops in UO2 from alpha particle irradiation

## Slide 21: Voids
Due to preferential absorption of interstitials at dislocations, we are left with a slight excess of vacancies in the bulk to nucleate and grow voids
Void nucleation can occur homogeneously by the collection of vacancies in the matrix, or heterogeneously at structural features (precipitates, grain boundaries, etc.)
The vacancy-rich radiation damage core is considered to be an important void nucleation mechanism in UO2
Vacancy diffusion then allows void growth
Gas atoms can often serve to stabilize small voids
Voids (bright spots) from alpha irradiation in UO2

## Slide 22: Radiation Effects
Chemistry changes
  two fission products are generated from each fission, resulting up to about 3% of the chemical species present at the end of life for commercial fuel
  the amount of fission products change both chemical and physical properties
Physical property changes
  The physical effects caused by atomic displacements are rather complex and depend on the relative sink strengths of a given material for interstitials and vacancies and on the temperature
  lattice parameter, thermal conductivity, elasticity, formation of the high burnup structure

## Slide 23: Thermal Conductivity Degradation
One of the major effects of defect formation is the degradation of thermal diffusivity, due to phonon scattering
Results obtained on irradiated UO2 show that the thermal conductivity is decreasing with increasing burn-up, and that at equal burn-up, samples with higher irradiation temperatures have higher thermal conductivity
There are mesoscopic and atomistic features that affect the thermal conductivity
The porosity existing in fresh fuels evolves during irradiation and has a strong impact on heat transport, because voids/bubbles have significantly lower kth than the lattice
Precipitates are formed by fission products that are insoluble in the UO2 lattice, forming oxide or metallic inclusions: can use composite theory to get effective thermal conductivities; typically, these precipitates INCREASE the thermal conductivity of the fuel

## Slide 24: Thermal Conductivity Degradation
Actinides, rare earths, and transition metals can form mixed oxides with UO2 (soluble fission products): these atoms act as phonon scattering centers as a result of the differences in bonding, radii, or mass, and thus decrease kth
Volatile fission products/gases are partially in solution and partially in bubbles, where they act as phonon scatterers or as low kth composite fractions
Point defects and extended defects contribute to the degradation of the thermal conductivity by scattering or limiting the mean free path of the phonons

## Slide 25: UO2 Thermal Conductivity
We have established correlations for thermal conductivity of fresh UO2 fuel as a function of temperature
  Where t = T/1000
  The first part of the equation describes the phonon interactions
  The second part describes electronic transport which becomes significant at high temperature

## Slide 26: UO2 Thermal Conductivity
UO2 thermal conductivity is low and decreases more during reactor operation
The thermal conductivity has been collected after various amounts of burnup to make empirical fits

## Slide 27: UO2 Thermal Conductivity
One empirical model used in BISON is the NFIR model
The model is a function of the temperature T (in C) and the burnup β (in MWD/kgU

## Slide 28: UO2 Thermal Conductivity
The Rf function switches between two kph functions, accounting for thermal recovery

## Slide 29: MOOSE/BISON Models
https://mooseframework.inl.gov/bison/source/materials/UO2Thermal.html
Fink-Lucuta
Halden
NFIR
NFI
Ronchi-Staicu
Toptan (NCSU alum)

## Slide 30: Other Physical Changes
An important effect of radiation damage is the volume increase of the crystal lattice, leading to macroscopic swelling of the fuel material
Alpha particle damage alone can cause approximately 0.4% swelling
Mechanical properties also vary with damage
Hardness increases as a function of dpa
Young’s modulus decreases with dpa

## Slide 31: High Burnup Structure (HBS)
At the beginning of the irradiation, the local power is ~10% higher on the pellet periphery, due to self-shielding effect in 235U fissions driven by neutrons entering the rods after interactions in the water
With increasing burnup, a strong capture of neutrons by U-238 in the resonance range occurs at the periphery of the fuel
This leads to the production of Pu-239, and leads to a higher fissile density and thus a further increase in the local power/burnup
This high local burnup area is on the outer ring of the fuel and is about 200 microns thick, which represents about 8% of the fuel

## Slide 32: High Burnup Structure (HBS)
When thermal recovery is not sufficiently efficient (at lower temperatures), the accumulation of defects at high burnup can lead to the instability of the crystalline structure, initiating a restructuring driven by the energy stored in the material
This can be amorphization (not observed in UO2) or recrystallization/polygonization
Polygonization is the rearrangement of dislocations into sub-domain walls with slightly misaligned grains
In UO2, grains subdivide from 10 microns in size to 100-200 nm size, and a densely porous structure is formed (~20% porosity)

## Slide 33: High Burnup Structure (HBS)
The increase of the relative porosity volume degrades the material conductivity and reduces the mean grain size
On the other hand, the intragranular irradiation defect-cleaning improves the fuel intrinsic thermal conductivity
Fission gas in HBS bubble is retained, not released
Exact mechanism of HBS formation is not fully understood, believe to be polygonization, interacting with fission gas bubbles, dislocation growth, and high levels of energy deposition

## Slide 34: High Burnup Structure (HBS)
HBS has a high fission gas retention capacity, and does not evolve toward an open system of interconnected channels, even when porosity reaches very high values
Thus, the HBS is a relatively stable structure, limiting pressure increase in the plenum
While burnup is higher in the rim region, the HBS polygonization removes/sweeps defects to new grain boundaries, removing some phonon scatterers
Despite high porosity, thermal conductivity increases, slightly decreasing centerline temperatures in high burnup fuel

## Slide 35: Radiation Effects Summary
Formation of loops of voids as primary defect clusters
Radiation effects include both chemistry and physical property changes
One of the key physical properties modified is the thermal conductivity
  have several empirical (and mechanistic) models to account for burnup and temperature
HBS forms towards the end of life, generating a fine-grained structure with high porosity
HBS retains fission gas and slightly increases thermal conductivity