## Slide 1: Nuclear Fuel Performance
NE-591-010
Spring 2021

## Slide 2: Last time
Corrosion is the environmental degradation of materials
Cladding oxidizes, forming ZrO2
The limiting step for oxidation is the oxygen transport through the oxide layer
  It begins being controlled by diffusion
  Then, a protective layer forms that slows oxidation
Hydrogen released by oxidation enters the cladding
Due to low solubility (that is a function of temperature), hydrides form
Hydrides are brittle, and so reduce the ductility of the cladding

## Slide 3: Metallic Fuel Microstructure and Performance

## Slide 4: Why metallic fuel?
It has demonstrated a high burnup capability beyond 20%
Metal fuel also has superior off-normal performance characteristics, in particular for the run-beyond-cladding-breach conditions due to the compatibility of metal fuel with sodium coolant
The inherent passive safety potential where metal fuel is far superior to other fuel types (less stored Doppler reactivity)
Metal fuel also allows a very simple injection-casting fabrication technique and electrorefining-based fuel cycle closure, which promises simpler waste management, proliferation-resistance, and much improved economics

## Slide 5: Why do we alloy?
Unalloyed swelling can reach >150% at target burnups
Anisotropic swelling of alpha U
  thermal expansion
  irradiation growth
Cavitation swelling is characterized by large irregular cavities that form by mechanical tearing at grain and sub-grain boundaries, resulting in a very deformed “swirled” microstructure

## Slide 6: Alloying attempts
Adjusted U
  Small amounts of Al, Fe, or Si
U-Fissium (U-Fs)
  Fissium is an artificial mixture of the natural elements represented among the fission products to simulate the chemical composition of the material resulting from fission
Further studies on U alloys have centered on elements that form extensive solid solutions with U in the high-temperature γ-phase, specifically Mo, Zr, Ti, and Nb
U-Nb and U-Ti show excessive phase decomposition to alpha-dominated systems
U-Mo is utilized in research reactors which operate at low T

## Slide 7: U-Zr (U-Pu-Zr)
Alloying with Zr increases melting point and stabilizes the high temperature bcc phase
Temperature range for fuel is ~800-1100 K
Typically 10 weight percent Zr (23 atomic percent)
Directly in multiphase region
  find bcc, beta, alpha U, delta UZr2, alternate bcc phases

## Slide 8: Fuel Fabrication
Injection casting
  starting materials are charged into the graphite crucible in the injection casting furnace
  The crucible’s interior is coated with yttria and the mold’s interior is coated by zirconia for protection against reaction with molten uranium alloy
  Silica tube molds with the top ends closed are set above the crucible
  After melting, furnace is made a vacuum, molds lowered, then Ar gas refills the furnace, with pressure difference serving to inject the liquid metal into the molds

## Slide 9: Fuel Redistribution
Zr diffuses via Soret diffusion up the temperature gradient
Zr also possesses different solubilities in each phase of U
This leads to distinct zones of Zr content in radial rings
A) gamma phase, high Zr content, B) beta phase-ish, low Zr content, C) alpha/delta phase, as-fabrication Zr content
Lower Zr content = lower melting temperature
Also, different elastic and thermal properties for each phase and each Zr content
A
B
C

## Slide 10: Swelling of Metallic Fuel
While oxide fuels well a few percent, metallic fuels swell by as much as 30 %
This swelling occurs very rapidly, e.g. in the first few percent burnup, then displays a linear increase
Fuel swells anisotropically: more radially than axially
Swelling is accounted for by low smear density
Swelling rate decreases due to fission gas bubble interconnection and release
Low slope of swelling vs burnup for burnup > 5% is largely due to solid fission product generation

## Slide 11: Fission Gas Release
Gas release is not wholly understood, but largely presumed to be intragranular bubble growth and interconnection
Bubble interconnection, and thus fission gas release, typically occurs within the first 3-5 percent burnup
There exists limited experimental data, but this is a key phenomenon affecting fuel swelling and performance
Gas released into the plenum leads to internal pressure increase

## Slide 12: Cladding Strain
Since most of the fission gas was released from the fuel at ∼30% swelling, it was clear that the pressure inside the fuel element could be decreased by providing a plenum for this gas
Thus, with smear density ~75% and a large plenum, allow for both swelling and gas release without excessive stress on cladding

## Slide 13: Radially Varying Bubble Morphologies
In the center part of the fuel pin, where the γ-phase predominates, large gas bubbles form; this is indicative of a higher plasticity of the fuel
Whereas at lower temperatures, where the U α-phase predominates, the characteristic tearing-type porosity is evident
The fission gas pressure in the center may result in a near-biaxial loading of the peripheral shell, the radial stress component being twice the axial component
This stress effect results in a larger diametral than axial strain, and hence anisotropic swelling

## Slide 14: Fission Gas Bubble Morphology in alpha vs gamma U
alpha
gamma

## Slide 15: alpha U Tearing
Between 400 and 600 C, alpha U swelling is overwhelmingly dominated by cavitation
Cavitation swelling is characterized by large irregular cavities that form by mechanical tearing at grain and sub-grain boundaries, resulting in a very deformed “swirled” microstructure
In addition to these large cavities, many small cavities, or tears, develop within the α grains, particularly in the 500–600 C range
These intergranular cavities are crystallographically aligned and appear to be related to twin boundaries

## Slide 16: Axial Varying Microstructure
The location of the radial zones essentially follows isotherms in the fuel which are determined by the various phase boundaries of the alloy
In the usual situation of upward coolant flow and a cosine-shaped axial power profile in the fuel, the peak fuel temperature occurs between the center and top of the fuel column

## Slide 17: Fuel-Clad Chemical Interaction
FCCI in an all-metallic fuel element is in essence a complex multicomponent diffusion problem
At least five major constituents participate in the diffusion process, in addition to minor alloy components such as C, N and O, as well as fission products
The potential problem of interdiffusion of fuel and cladding components is essentially twofold: (i) a weakening of the cladding’s mechanical properties; and (ii) the formation of relatively low melting point compositions in the fuel

## Slide 18: Cladding wastage mechanisms
Prior to accumulation of lanthanide FPs at the fuel–cladding interface (due to FPs migration), FCCI is characterized by a ferritic layer formation, which is a result of Ni depletion in austenitic cladding or decarburization of the martensitic cladding
Severe wastage is due to interaction of cladding with FPs, generating eutectic low melting phases
Fe-96Ln has a melting point of 770˚C, Fe-92Ce has a melting point of 590˚C

## Slide 19: Chemical Species Diffusion and Interaction
Lanthanides (Ln) ultimately control FCCI, and their presence at the internal cladding surface depends not only on burnup but also very strongly on their radial migration in the fuel
Nd and Ce are two of the most commonly found Ln in FCCI regions
Fission products diffuse into the Fe-based cladding and segregate along grain boundaries, further weakening the cladding
It is key to develop transport models for Ln species through the fuel, in order to develop a source term for FCCI, but very little is known about Ln transport in metallic fuel

## Slide 20: Metallic Fuel Performance Modeling - BISON
The mechanical performance of the fuel is governed by a model that represents the elastic moduli as functions of temperature, porosity, and zirconium and plutonium content
A creep model that is a function of fission rate, temperature, and porosity is also used
Eigen strains (stress free strains) are modeled by constant thermal expansion along with gaseous and solid fission product swelling models
The solid swelling model is a straight-forward model directly proportional to fission rate
The gaseous swelling model comes from a force balance applied to a bubble with the metallic fuel and generates porosity at all material points (quadrature points) in the domain

## Slide 21: Metallic Fuel Performance Modeling
The thermal conductivity model in the fuel is a function of temperature, porosity, and zirconium and plutonium content
The heat capacity models are functions of temperature and alloy phase
The fission gas model is simply based on fission rate for gas generation and the fission gas released is governed by the value of porosity
Cladding mechanical response is governed by constant elastic moduli and thermal expansion, with thermal and irradiation creep
Thermal conductivity and heat capacity models are functions of temperature
The redistribution of zirconium is governed by Fickian and Soret diffusion

## Slide 22: Metallic Fuel Performance Modeling
Compare BISON to EBR-II experiments

## Slide 23: Other Metallic Fuel Codes
LIFEMETAL
  ANL code that has evolved from the LIFE series of codes that perform steady-state and transient analyses for the thermal, mechanical, and irradiation behavior of nuclear fuel, and was originally developed for UO2
ALFUS
  ALloyed Fuel Unified Simulator, Japanese development (CRIEPI), is an irradiation behavior analysis code for metallic fast reactor fuel
FAST
  the current NRC thermal-mechanical fuel performance code that is the next evolution of FRAPCON

## Slide 24: Incorporation of lower length scale information
Surface energy
Porosity interconnection threshold
Fission gas bubble number density
Alpha tearing/initial porosity

## Slide 25: Summary
Metal fuel can go to high burnup, good accident performance, inherent safety, easy to make
Complex phase and composition environment
Rapid, substantial swelling, followed by fission gas release
Fission gas bubble behavior is very phase dependent
Observe constituent redistribution radially, in addition to axially varying microstructure
FCCI is a major factor in cladding failure, dependent upon thermodynamics and kinetics of a number of lanthanides, actinides and transition metals
We are trying to model all of this!