## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2025

## Slide 2: Housekeeping
Gone to TMS next week
Lectures will be recorded and posted on Panopto
This means no office hours next week either
Reach out on slack for questions!
Can maybe squeeze in a zoom call or two if it is really needed

## Slide 3: Last time
Five families of fission products, which change the fuel behavior
  soluble oxides, insoluble oxides, noble metals, volatiles, noble gases
Fission gas is released in three stages
  Fission gas production and diffusion to grain boundaries
  Grain boundary bubble nucleation, growth, and interconnection
  Gas transport through interconnected bubbles to free surfaces

## Slide 4: Fission Gas Release
Released fission gas enters the gap and plenum, causing various problems
Xe and Kr have very low thermal conductivities, reducing the gap conductance
The plenum pressure increases
The volatile fission gases corrode the cladding
They are also radioactive and hazardous, causing problems when the cladding is breached
Fission gas release experiments:
  Post irradiation annealing
    Fuel is irradiated at low temperature; Fuel is then placed into a furnace and heated; Gas atom release is then measured
  In-pile release
    Gas release is measured during reactor operation; It is much more difficult than post-irradiation annealing; Total amount released is measured by puncturing cladding after irradiation; Release with time can be estimated using a pressure transducer inside an instrumented fuel rod

## Slide 5: Fission Gas Release
Fission gas release models attempt to predict the rate at which gas is released from the fuel
To model fission gas release, ideally, we must model all three stages of gas release
  Diffusion of gas atoms to grain boundaries
  Growth and interconnection of grain boundary bubbles
  Transport of gas atoms through interconnected bubbles to free surfaces
The earliest models only considered Stage 1
Most models now consider stage 1 and 2
There are no models that consider all three stages, but some are under development

## Slide 6: Booth Model
The Booth model is the earliest model of fission gas release and only considers stage 1
A grain is considered as a simple sphere
Gas atoms are released at the grain boundary
The model solves the diffusion equation in 1D spherical coordinates
Assumptions
  cg(r, t)
  All grains are spheres of radius a
  D is constant throughout the grain
  Gas is produced uniformly throughout the grain
  Gas is released once it reaches the grain boundary
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = 0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 7: Modeling post-irradiation annealing
The initial gas concentration is cg0
No gas is produced
Solving this equation tells us the value of cg at any radius or time
However, we want to know the fraction of gas atoms that have made it to the grain boundary
We use the flux at the grain boundary
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = cg0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 8: Solving the Booth Model
This equation is solved using a Laplace transform after nondimensionalization
Will not go through the derivation (shown in Olander)
τ = D x t / a2
τ < π-2
τ ≥ π-2
Grain boundary
Gas atoms
Release

## Slide 9: Booth Example
For a diffusion coefficient for Xe of D = 8e-15 cm2/s, what fraction of the fission gas trapped in a post-irradiation annealed fuel pellet has escaped after one hour? It has an average grain size of 10 microns
  D = 8e-15 cm2/s
  a = 10e-4 cm
  t = 3600 s
Which f? τ = D x t/a2 = 2.88E-4 < p-2 = 0.101
  f = 6*sqrt(8e-15*3600/(pi*(10e-4)^2)) – 3*8e-15*3600/(10e-4)^2 = 0.0181

## Slide 10: Different expressions for fission gas release
Given the data from the previous example, can plot both
  t < p-2
  t > p-2

## Slide 11: Modeling in-pile release
The initial gas concentration is 0
Gas is produced due to fission, where y is the chain yield (y = 0.3017 for Xe and Kr) and the fission rate
Gas can also decay, where λ is the decay constant
  If we only consider stable stable products, λ = 0
For in pile release, the fraction is equal to
After solving with with a Laplace transform
The total gas production is gas atoms/cm3
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = 0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 12: Example
For a diffusion coefficient for Xe of D = 8e-15 cm2/s, what fraction of the fission gas trapped in an in-pile fuel pellet has escaped after one hour? It has an average grain size of 10 microns.
  D = 8e-15 cm2/s
  a = 10e-4 cm
  We have a short time (t=3600 s, ), so we can use:
  f = 4*sqrt(8e-15*3600/(pi*(10e-4)^2)) – 3/2*8e-15*3600/(10e-4)^2 = 0.0121

## Slide 13: As time progresses, both the fraction released and the produced gas increase

## Slide 14: Forsberg-Massih model
The Booth model ONLY considers stage one of fission gas release
Two stage Forsberg-Massih mechanistic model
  Considers intragranular diffusion diffusion to grain boundaries (stage 1)
  Also, grain boundary gas accumulation, resolution back into grain, saturation (stage 2)
  Assumes that once the bubbles on the grain face are interconnected, it is released (no stage 3)

## Slide 15: Forsberg-Massih model
2-stage F-M model over-predicts gas release because it neglects grain boundary bubble percolation (Stage 3)
Millett, Tonks, and Biner. JNM, 424.1 (2012): 176-182.

## Slide 16: Gas diffusion
The diffusivity of the fission gas depends on temperature and on irradiation
Experimental data shows three different regimes for the diffusivity
D = D1 + D2 + D3 cm2/s

## Slide 17: Gas diffusion
The effective fission gas diffusivity is slower due to trapping by intragranular bubbles
As the gas atoms diffuse towards the grain boundary, some are trapped by the small intragranular bubbles
Some are later knocked out by energized particles (called resolution)
The effective diffusion constant depends on the trapping rate rt and the resolution rate rr

## Slide 18: Fuel Swelling/Dimensional Change

## Slide 19: Fuel changes size and shape under reactor operation
Thermal expansion:
  increase in volume, decrease in density, caused by increasing temperature
Densification:
  Decrease in volume, increase in density, caused by shrinking of porosity left after sintering
Swelling:
  Increase in volume, decrease in density, caused by fission products
Irradiation Creep:
  Change in shape, constant density, occurs with applied stress less than sy

## Slide 20: Densification
Densification takes place during initial 5 - 10 MWd/kgU
  Small, as-built pores close due to effects of fission spikes and vacancy diffusion
  Large pores stable (in absence of large hydrostatic stress)
Empirical correlation for densification is a function of
  β - Burnup (in FIMA)
  Δρ0 – Total densification that can occur (a common value is 0.01)
  βD – Burnup at which densification stops ( a common value is 5 MWD/kgU)
  CD = 7.235 − 0.0086 (T(°C) − 25) for T < 750°C and CD = 1 for T ≥ 750 °C
[Maier et al, 1988]

## Slide 21: Fission product induced swelling
Fission product swelling results from three changes in the fuel microstructure
  Solid swelling: Accumulation of soluble and insoluble fission products in fuel matrix
  Gaseous swelling: Accumulation of gaseous and volatile fission products in intragranular and intergranular pores
  High burnup swelling: Restructuring of pellet rim with the accumulation of fission gas in a large number of small pores
after Garzarolli in [Rudling et al, 2007]

## Slide 22: Solid fission product swelling
The solid fission product swelling model is a function of:
  b – Burnup (in FIMA)
  ρ – Initial UO2 density (g/cm3)
Includes contributions from soluble oxides, insoluble oxides, and metallic precipitates

## Slide 23: Gaseous fission product swelling
Gaseous swelling varies strongly with temperature, fission rate, and stress
Empirical relationships dependent upon burnup and temperature
T < 1000K
  Fission gas atoms remain in fuel matrix or collect in small, isolated, intragranular pores (<1 nm)
  Intragranular pore size limited by fission spikes that drive gas back into fuel matrix
  Gaseous swelling constrained by fission gas release
T = 1000 to 1700 K
  Swelling takes place at hot interior of pellet
  Gas atoms in fuel matrix diffuse to grain boundaries and collect in pores
  Gas pressure causes bubbles to increase in size and to coalesce into larger pores
  Gaseous swelling opposed by applied stress
  Gaseous swelling also constrained by fission gas release

## Slide 24: The overall swelling behavior depends on temperature

## Slide 25: Total change in volume
The total change in volume is found by adding all components of dimensional change
  εtot = εth + εD + εsfp + εgfp
Example:
  fission rate = 2.5e13 f/(cm3 s)
  T(fuel) = 1400 K
  Tref = 300 K
  For densification: Δρ0 = 0.01 and βD = 5 MWD/kgU
  Total time: 2 weeks

## Slide 26: Example