## Slide 1: Fuel Types Continued
NE 533 Spring 2023

## Slide 2: Last Time
Course overview
My view of fuel performance
  heat delivery to coolant, length of operation, tolerance to accidents
Considerations for fuels
Why not pure U?
Intro to UO2 and MOX fuels for LWRs
Reminder to fill out the introduction forum post on moodle

## Slide 3: Accident Tolerant Fuel
USi fuels (U3Si2)
  A metal-ish compound, with higher thermal conductivity, higher uranium density
  Complex crystal structure (10 atoms unit cell) with effectively two sub-lattices
  Amorphizes at low temperatures
  Poor oxidation resistance
  Will require improved cladding, liners/coatings or fuel dopants

## Slide 4: Accident Tolerant Fuel
Cr-doped UO2
  Larger grain size, theoretically reduced fission gas release
  Cr changes the O potential present within the fuel, changing defect concentrations and mobilities
Coatings or alternate claddings – FeCrAl or SiC
  Improved radiation resistance, corrosion resistance, etc.

## Slide 5: Uranium-Zirconium (UZr)
Utilized in sodium cooled fast reactors (SFRs)
  EBR I, EBR II
Varied crystal structure and compositional environment
Easily alloyed with Pu, minor actinides (MA)
Can function as a breeder/burner fuel
Sodium coolant
Fe-based cladding

## Slide 6: Uranium-Zirconium (UZr)
Alloy metallic U with Zr to increase the melting point and to stabilize the high temperature body-centered cubic phase
Interesting phenomena
  30-50% swelling
  Constituent redistribution
  Alpha tearing
  FCCI

## Slide 7: Uranium-Zirconium (UZr)
Good Characteristics
  High thermal conductivity
  Stability to high burnups (> 20%)
  Flexible composition
  Inherent safety- negative reactivity feedback
  Good compatibility with Na coolant
Bad Characteristics
  Low melting point
  Dramatic fuel swelling that must be accounted for
  Incredibly complex microstructures/unpredictable behavior
  Fuel-Clad Chemical Interaction
  Very easily oxidized

## Slide 8: Uranium-Molybdenum (UMo)
New fuel being qualified for research reactors
Fuel foil, with Zr diffusion barrier, Al cladding
Will be utilized in ATR, NBSR, MITR, MURR

## Slide 9: Uranium-Molybdenum (UMo)
Microstructural phenomena of interest:
  Decomposition
  Fission Gas Superlattice
  Recrystallization
  Inter-diffusion region
  Carbides

## Slide 10: UC/UCO TRISO Fuels
TRISO: TRistructural ISOtropic particle fuel
Layered fuel in mm-sized particles
Layers:
  Fuel Kernel
  Buffer
  Inner Pyrolitic Carbon (IPyC)
  SiC
  Outer Pyrolitic Carbon (OPyC)

## Slide 11: UC/UCO TRISO Fuels
Can appear as UC, U2C3, or UC2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Rapidly corrodes in water
  Reacts with some cladding

## Slide 12: UC/UCO TRISO Fuels
High temperature gas reactors (HTGR) or molten salt reactors (MSRs)
Pebble bed and prismatic types
Particles are agglomerated with graphite into a larger pebble, or into a cylindrical block
Current designs utilize UCO, which is a heterogeneous mixture of UO2 and UC fuel
Helium cooled gas or molten salt cooled

## Slide 13: UC/UCO TRISO Fuels
Each individual pebble acts as its own containment, and allows fuels to go to much higher burnups and higher temperatures than UO2
Highly reliant on accurate fabrication processes that create high integrity, uniform layers and spherical particles
Integrity of the SiC is key for fission product retention

## Slide 14: Molten Salt Reactors
Molten Salt Reactor
  Utilizes flowing fuel salt (i.e., UF4-ZrF4-KF) with a secondary molten salt coolant loop (FLiBe)
  MSRE at ORNL, some modern designs
Stable Salt Reactor
  Utilizes fuel that is dissolved in molten salts (NaCl-(U/Pu)Cl3), contained in rods
  Molten salt coolant (NaF-ZrF, FLiBe, FLiNaK, etc.)
Can mix other actinides into the fuel in order to burn waste
Designed to be inherently safe
Molten salt corrosion is a big problem, as well as the lack of information on thermophysical properties of complex salt

## Slide 15: CANDU Reactors
Canada Deuterium Uranium: pressurized heavy water reactor
Natural uranium, as UO2, as the fuel source
Heavy water is the coolant, has a lower absorption of neutrons
Fuel pins are horizontal, as opposed to vertical
CANDU can be refueled online
Removes costs associated with enrichment

## Slide 16: UN – Lead Cooled Reactors
Can appear as UN, U2N3, or UN2
Advantages
  High thermal conductivity
  High fuel density
  Thermally stable
  High melting temperature
Disadvantages
  Corrodes in water
  Reacts with some cladding
  Difficult to manufacture
  Requires N-enrichment
Pb or Pb-Bi coolant
Operates in the fast spectrum

## Slide 17: Unique Fuel Designs
Lightbridge
  High Zr content UZr alloy
  Cruciform geometry fuel rods, combined into fuel elements
Kairos
  TRISO particle compacts with low density core
  Float in molten salt coolant for online refueling
NASA/LANL
  UMo fuel for space reactors: KRUSTY

## Slide 18: Fuel Summary Table
Property | UZr | UO2 | UC | UN | U3Si2
Corrosion resistance in water | Very poor | Excellent | Very poor | Poor | Very Poor
Compatibility with clad materials | Reacts with normal clad | Excellent | Variable | Variable | Variable
Thermal stability | Phase change at 665 and 770 °C | Good | Good | Good | Good
Uranium (metal) density (g/cm3) | 19.04 | 9.65 | 12.97 | 13.52 | 11.31
Melting point (°C) | 1205 | 2865 | 2850 | 2860 | 1665
Thermal conductivity (W/m-K) | 38 at 430 °C | 3 at 1000°C | 25 at 500°C | 20 at 750°C | 23 at 773°C

## Slide 19: Fuel Types Summary
There exist a number of nuclear fuels in different stages of utilization and development
Each reactor design or application has individual needs, and no one fuel is one size fits all
Need to balance safety, performance (normal, off-normal, extended), manufacturability, processing, waste, etc.

## Slide 20: Summary
Uranium is combined with O, C, N, transition metals for a variety of fuel types
UO2: ceramic, commercial reactor fuel, light water reactors
ATF: U3Si2 and Cr-doped UO2
UZr: fast reactor fuel
UMo: research reactor fuel
UC/UCO: high temperature gas reactors

## Slide 21: Questions?