## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2025

## Slide 2: Last Time
Ended the last module going through some UO2 radiation effects
Will continue microstructural effects, burnup effects, different phenomena
Start with the fuel, and work our way into cladding in this module
MOOSE projects due tomorrow night
Next week is paper presentation week, slides due Monday night
Meet the submission deadlines on moodle, I do not have them set up to receive late submissions!
Relevant seminar speaker today, NCSU alum

## Slide 3: grain Properties/Behavior

## Slide 4: Grain Boundaries
Materials are typically composed of various regions where the crystal lattice is oriented differently
When two grains meet, there is a plane of atoms that do not follow the crystal lattice called a grain boundary
Grain boundaries add energy to the material that is a function of their structure
A grain boundary’s energy is determined by its:
  Inclination – the orientation of the 2D grain boundary plane (2 degrees of freedom)
  misorientation – the rotation required to align one grain with the other (3 degrees of freedom)

## Slide 5: Grain Texture
The orientation of all the grains in a material is called the texture
The degree of texture is dependent on the percentage of crystals having a preferred orientation
  randomly oriented grains equals no texture
Texture is seen in almost all engineered materials, and can have a great influence on materials properties

## Slide 6: Grain size
In a polycrystal, there is also a distribution of grain sizes
The average grain size of the fuel has a significant impact on its behavior
Typical LWR fuel has an initial average grain size of about 10 microns
The average grain size impacts
  Fission gas release
  Swelling
  Thermal conductivity
  Creep
UO2 grain structures

## Slide 7: Grain boundary diffusion
Diffusion often occurs faster along grain boundaries than in the perfect crystal
Grain boundaries have more space than the perfect lattice
So, atoms diffuse faster along grain boundaries than through the perfect lattice
This means that grain boundary, or intergranular, diffusion increasingly dominates bulk (intragranular) diffusion
This can become more pronounced as the temperature is reduced
Grain boundary diffusion has a large impact on creep

## Slide 8: Grain boundary segregation
Impurity atoms (such as fission gas) and other defects move to grain boundaries
Due to grain boundaries having more open space, impurity atoms have a lower energy when they are on grain boundaries
This is called grain boundary segregation
Radiation induced segregation (RIS) is where radiation produces defects that drive towards the grain boundary and preferentially drag solute atoms

## Slide 9: Dislocation interaction with grain boundaries
Grain boundaries impede dislocation motion
The number of dislocations within a grain impacts how easily dislocations can traverse grain boundaries and travel from grain to grain
So, by changing grain size one changes barrier density, influencing dislocation movement and yield strength
This is called the Hall-Petch effect
  where σy is the yield stress, σ0 is a materials constant for the starting stress for dislocation movement (or the resistance of the lattice to dislocation motion), ky is the strengthening coefficient (a constant specific to each material), and d is the average grain diameter

## Slide 10: Grain boundaries and cracks
Materials often crack along grain boundaries
Grain boundaries can be weaker than the perfect lattice
  different bonding environment, increased extrinsic particles, etc.
Thus, fracture will often occur along grain boundaries (intergranular fracture)

## Slide 11: Grain size change
A single crystal has a lower energy state than a polycrystal, due to the grain boundary energy
So, grain boundaries migrate to reduce the energy
vGB = MGB (Pd – Pr)
  MGB is the grain boundary mobility
  Pd is the driving force (pressure) for grain growth
  Pr is the pressure resisting grain growth

## Slide 12: Grain growth
Due to grain boundary migration, the average grain size goes up with time during annealing/heat treating
As grain boundaries migrate, some grains grow and some shrink
Shrinking grains eventually disappear
The average grain volume
Therefore, as Ngrains decreases due to grain disappearance, the average grain volume goes up

## Slide 13: Grain boundary mobility
The grain boundary mobility is a function of temperature and GrB type
The grain boundary mobility is determined according to
  m4/(J s)
  kb = 8.6173e-5 eV/K is the Boltzmann constant
Both the pre-factor M0 and the activation energy Q change as a function of the grain boundary misorientation
We often use an average grain boundary for a material, taken from polycrystal measurements-> UO2: M0 (m4 /J-s) = 4.6e-09, Q (eV) = 2.77
What is the mobility of UO2 at 1600 K?
  MGB = 4.6e-9*exp(-2.77/(1600*8.6173303e-5)= 8.7e-18 m4/J-s

## Slide 14: Grain growth
There are various driving forces for grain growth
The most common driving force is the reduction of grain boundary energy
  , where γGB is the GB energy and R is the radius of curvature
  It is often called the curvature driving force, because it drives grain boundaries to be straight
  It also causes larger grains to grow at the expense of smaller ones
Other driving forces include
  Temperature gradients, Elastic energy gradients, Dislocation energy gradients
Velocity of a spherical grain:
Simplified size (diameter) of a spherical grain vs time:

## Slide 15: Maximum grain size
Consider a material with an average grain size D
The change in D can be written as
  k = 2 MGB γGB is a rate constant that can be determined from experiments
  Dm is the grain size at which the driving force equals the resistive pressure
For UO2:
Dm is a function of temperature microns

## Slide 16: Grain growth
Grain boundary motion is inhibited by pores, precipitates, solute atoms, etc.
Solute atoms (whether in interstitial sites or vacancies) can decrease the grain boundary mobility.
  This is called Solute Drag
  Even a small concentration of impurities can decrease the mobility by 3 to 4 orders of magnitude
Particles and pores resist grain boundary motion

## Slide 17: Irradiation effects on grain growth
Irradiation can accelerate grain growth
Can be significant with small grains and at low temperatures
https://doi.org/10.1016/j.actamat.2022.117856
https://doi.org/10.1063/1.4935238

## Slide 18: Fuel Densification
Remember that fresh fuel pellets are not fabricated to be 100% dense, more like 95-99% dense
Early in life, fuel pellets shrink, and the initial porosity is largely eliminated
In some ways, densification is a continuation of the sintering process
However, irradiation accelerates the process
Small pores close due to effects of fission spikes and vacancy diffusion
Large pores stable (in absence of large hydrostatic stress)
Pellets with higher initial density, densify less

## Slide 19: Densification
The driving force for densification is the change in free energy from the decrease in surface area of pores and lowering of the surface free energy
An empirical relation to describe densification has been built as a function of
  β - Burnup (in FIMA)
  Δρ0 – Total densification that can occur ~ 0.01
  βD – Burnup at which densification stops ~5 MWD/kgU, ~0.005 FIMA
  CD = 7.235 − 0.0086 (T − 25) for T < 750C and CD = 1 for T ≥ 750C

## Slide 20: Empirical models
Many models of reactor fuel behavior are fits to experimental data
They are typically correlated to burnup
Burnup is a measure of how much fissioning has taken place. Typical units are:
  MWD/kgU
  FIMA
It can be calculated from the volumetric fission rate
Units of this equation are FIMA
To convert from FIMA to MWD/kgU, multiply by ~950
after Garzarolli in [Rudling et al, 2007]

## Slide 21: Summary
The average grain size in UO2 impacts fuel behavior and performance:
  Fission gas release
  Swelling
  Thermal conductivity
  Creep
The material wants to reduce its energy by having large grains grow at the expense of small grains
Grain growth is reduced due to other defects reducing the grain boundary migration
Fuel densification is driven by reduction in surface area of pores – continuation of sintering process
Empirical models describe densification as a function of burnup

## Slide 22: Fuel chemistry

## Slide 23: Fuel Chemistry
UO2 is an ionic compound that must have balanced charges
What is the charge of a typical oxygen ion?
  O2-
Uranium valance states
  Possible: U3+, U4+, U5+, U6+
  Most stable: U4+, U5+, U6+
  Beyond UO2, can have U4O9, U3O8, UO3
The UO2 structure is very stable all the way up to the melting temperature and down to extremely low temperatures, even with irradiation damage
There is space in the uranium lattice that can accommodate fission products

## Slide 24: O/M ratio
The ratio of oxygen to uranium metal (O/M ratio) can vary
This is the stoichiometry
The homogeneity range of uranium dioxide extends to both hypo-(UO2-x) and hyper(UO2+x)-stoichiometric compositions in oxygen
The minimum and maximum oxygen contents in the dioxide correspond to the compounds with the formula of respectively UO1.67 at 2720 K and UO2.25 at approximately 2030 K
Will the O/M ratio go up or down during reactor operation?
  It is complicated, because of the formation of fission products that also react with the oxygen, and O interaction with Zr cladding

## Slide 25: Excess O
The crystal structure of UO2 can accommodate extra oxygen
Excess oxygen resides at interstitial locations
Oxygen in neighboring sites is displaced
Cation valence increases to maintain electrical neutrality
Fuel fabricated to be nearly stoichiometric; i.e., UO2.00± because:
  It is the most stable
  It has the highest melting temperature
[after Olander, 1976]

## Slide 26: Incorporation of Fission Products
As fission products form, the valence state of the uranium can change
Typical valence of soluble fission products is M3+
The uranium valence state changes to compensate
  Oxygen liberated by fission
  Fission products produced with M3+ valance state incorporated in fuel lattice
  Uranium oxidizes from U4+ to U5+ or U6+ to maintain local electrical neutrality

## Slide 27: Oxygen potential
The oxygen potential is a measure of how free the oxygen is to escape/move around
Oxygen potential is defined as:
or, equivalently:
  With = Chemical potential of oxygen in solution
  = Gibbs free energy of gaseous oxygen at temperature T and a standard pressure (1 atm)
It is possible to determine the stoichiometry from the oxygen potential