## Slide 1: NE 591: Advanced Reactor Materials
Fall 2021
Dr. Benjamin Beeler

## Slide 2: Last Time
Austenitic steels undergo excessive void swelling in fast reactor conditions
F/M steels have good mechanical properties, are cheap, and their microstructure can be tailored through composition and fabrication
M23C6 and monocarbide precipitate are prevalent both along grain boundaries and within the grains; M2X metallic precipitates form and can be converted to Laves phases
F/M steels swell very little due to fundamental nature of defects in ferrite, C-vacancy bonding, and dislocation-solute interactions
Tailoring of alloying elements has allowed for improved creep strength
Stress induced preferential nucleation/absorption (SIPN – SIPA)
Swelling interaction with creep

## Slide 3: advanced cladding

## Slide 4: Irradiation Embrittlement
Ferritic steels have these large monocarbides which aid in creep resistance
The lath boundaries are decorated with Cr rich M23C6 precipitates which increase the thermal stability
Embrittlement is caused by 1) segregation of elements to lath boundaries which make the grain boundaries decohesive, and 2) evolution of carbides and intermetallic phases
For removable components such as clad, which are subjected to high temperature and pressure with a residence time of a few years, creep embrittlement is the issue which decides their design and performance
For permanent support structures increase in hardening and loss in fracture toughness on irradiation are major issues

## Slide 5: Irradiation Embrittlement
The increase in the ductile to brittle transition temperature, DBTT, is known to be related to irradiation hardening, which is generally observed to saturate with fluence
Evidence for a possible maximum in DBTT was observed for the 12Cr steel irradiated in the range of 35–100 dpa in the FFTF
High fluence and/or high temperature are required before a maximum is observed
Thus, these properties are a balance between the point defect production and irradiation-induced precipitation
The precipitation during irradiation hardens the steel and irradiation accelerated recovery and aging soften the steel
The high temperature recovery produces an observable saturation in hardening above ~720K

## Slide 6: DBTT
BCC materials can undergo significant increase in the DBTT at low T for even 1 dpa
The minimum operating temperature to avoid embrittlement F/M steels is ~500 K
Extensive evaluation of the embrittlement behavior of the ferritic steels for different chemistry has been performed
Compositions around 9Cr show the least change in the DBTT
Chemical variation affects on DBTT changes has been thoroughly studied
Addition of phosphorous, copper, vanadium, aluminum, and silicon increase the DBTT

## Slide 7: DBTT
The 12Cr steels, HT9, show a larger shift in DBTT as compared to modified 9Cr–1Mo steel
The balance is always between nearly nil swelling resistant 12Cr steels and 9Cr steel which is less prone to embrittlement than 12Cr steels

## Slide 8: Features affecting Embrittlement
There are a number of microstructural features that can impact the embrittlement of F/M steels
Prior austenite grain size (PAGS)
The size of martensitic lath and packet (which is sensitive to austenitization temperature)
Tempering/annealing, which can increase carbide precipitate size
The generation of helium through (n,alpha) reaction
For low thickness components, the triaxial stress necessary for the embrittlement does not develop, which reduces the intensity of this otherwise serious problem of embrittlement in ferritic steels

## Slide 9: Ferritic/Martensitic Steels Summary
Refer to “last time” slide…
Embrittlement is caused by segregation of elements to lath boundaries and evolution of precipitates
Maximum DBTT shift occurs in F/M steels for high T or fluence
DBTT shift is minimized for 9Cr steels
Microstructure can impact the embrittlement behavior
In thin-walled materials, such as cladding, the stress state that leads to cladding embrittlement is typically not prevalent

## Slide 10: ODS Steels

## Slide 11: Oxide Dispersion Strengthened
Thermally stable oxide particles dispersed in the ferritic matrix improve the radiation resistance and creep resistance at high temperature
ODS steels have a strong potential for high burnup (long-life) and high temperature applications typical for SFR fuels
Typically, Y2O3 particles or Y2Ti2O7 particles
Y2O3 particle with surrounding matrix

## Slide 12: Y2O3 Decomposition
The fine distribution of Y2O3 particles is attained by the dissociation of stable Y2O3 particles which are forced to decomposed into the ferritic steel matrix during the mechanical alloying process
The lattice structure change of Y2O3 in the ODS steel during MA consists of three stages: (1) destruction of the lattice structure, (2) formation of a blurry lattice structure, (3) appearance of amorphous areas

## Slide 13: 9Cr-ODS
For nuclear applications, the choice of 9 wt% Cr with a tempered martensitic matrix is preferable to suppress the ductility loss by irradiation hardening and improve the microstructure stability and creep strength at high temperature
The high-temperature strength of 9Cr-ODS is drastically improved by nano-scale oxide particles dispersion in the matrix
The standard chemical composition of 9Cr-ODS being developed by the JAEA for SFR application is 9Cr–0.13C–0.2Ti–2W– 0.35Y2O3 (wt%)
The addition of titanium produces the nanoscale dispersion of oxide particles
Tungsten of 2 wt% is also added in order to improve high-temperature strength by means of solid solution hardening

## Slide 14: 9Cr-ODS microstructure
The microstructure of 9Cr-ODS steel cladding is basically tempered martensite, but includes some residual ferrite phases
Only the full martensite phase can be expected in 9Cr-ferritic steel without yttria under the same conditions
The high temperature strength is greatly improved with the ferrite, and thus control of ferrite is key in ODS fabrication

## Slide 15: Residual Ferrite
Annealing results in the formation and precipitation of Y–Ti complex oxide particles at elevated temperatures of 700C or higher
Since the reverse transformation of alpha (ferrite) to gamma (austenite) takes place at a temperature over 850C, alpha ferrite is attributed to the presence of the Y-Ti-O particles
These particles block the motion of the alpha-gamma interface, there by partly suppressing the reverse transformation from alpha to gamma-phase

## Slide 16: Mechanical Properties
The lifetime of a SFR cladding is mostly determined by the internal creep rupture strength with the internal pressure of the fission gas at a temperature of ~700C
PNC316 is austenitic steel used developed by JAEA for fast reactors
PNC-FMS is a F/M steel
9Cr-ODS steels have superior creep resistance and higher tensile strength

## Slide 17: Ferritic 12Cr-ODS Steel
Development of ODS steels began with purely ferritic types, similar to MA957
While these types of steel exhibit excellent creep rupture resistance, there is anisotropy of the rupture strength
If the Y2O3 content is kept sufficiently low, an equiaxed grain structure can be maintained, providing more isotropic mechanical properties

## Slide 18: NFAs
Nanostructured ferritic alloys (NFAs) are 12%–20% Cr ferritic stainless steels that are dispersion strengthened by a very high density of ultrafine Y-Ti-O nanofeatures
This high density can yield excellent strength and radiation resistance, but make fabrication processes very difficult
MA957 and Eurofer are examples of NFAs

## Slide 19: FeCrAl-ODS Steel
FeCrAl steels, with and without ODS are of interest since Al-containing steels produce the stable alumina (Al2O3) scale to prevent direct reaction of Fe with steam
A nominal composition of Fe-10Cr-6.1Al-0.3Zr (wt%) with 0.3wt% Y2O3 has been studied by ORNL
Zr is added to prevent Y-Al oxide particle formation

## Slide 20: Corrosion
Hot steam oxidation tests are fairly limited in ODS steels
Additional Cr improves corrosion resistance, and Al content greater than 2 wt% provides a protective barrier
Excess oxygen content in the alloys can serve to suppress corrosion
In systems with high amounts of excess oxygen, Zr content can further aid in corrosion resistance

## Slide 21: Liquid Na Compatibility
OSD-steels display excellent compatibility with liquid sodium
Both 9Cr and 12Cr ODS steels show no degradation in UTS after prolonged exposure to Na
Creep rupture behavior of ODS steels in air is identical to that in liquid Na
Under irradiation, this corrosion behavior may change, but has not been thoroughly studied

## Slide 22: Irradiation Effects
The stability of the oxide particles under irradiation is the key factor in these alloys maintaining their advantageous mechanical properties under operation
Ballistic dissolution is the ejection of atoms from oxide particles due to high energy PKAs and the disordering of the particles

## Slide 23: Irradiation Effects
At higher temperatures where vacancy diffusion is possible, ballistic dissolution works in conjunction with irradiation-assisted diffusion and changes the dispersion of oxide particles
The atoms ejected from oxide particles can diffuse back to the original oxide particles, stay in the matrix, or reach other oxide particles
Most research groups have reported that the size and number density of the oxide particles hardly change compared to how they were before irradiation
The predominant mechanism of these results are the recovery arising from back diffusion to the original oxide particles or re-join to other existing oxide particles

## Slide 24: Irradiation Effects
A large number of irradiation experiments have been performed and analyzed to study the evolution of oxide particles
It appears that there is no correlation between irradiation dose, irradiation temperature, and the trend of change in size or number density of oxide particles

## Slide 25: Irradiation Effects

## Slide 26: Irradiation Effects
Swelling:
  ODS steels are very swelling resistant, as the oxide particles trap vacancies and gas atoms, resulting in very small and homogeneously dispersed voids/bubbles
Hardening:
  hardness increases due to irradiation in ODS steels are smaller than in non-ODS steels
  Oxide particles dominate hardness, and act as sinks for generated point defects

## Slide 27: Summary
ODS is fabricated through mechanical alloying and subsequent annealing
9Cr-ODS steel has a unique structure consisting of tempered martensite and residual ferrite that induces superior strength through finely dispersed oxide particles
NFAs have a very high density of oxide particles, producing very high strength and creep resistance, at the cost of workability
FeCrAl-ODS can provide superior corrosion resistance while retaining the ODS influenced mechanical properties
Further in-reactor studies on ODS steels need to be performed
While performance of ODS steels is widely studied, current production is limited to laboratory scale, with prohibitive costs for large scale production