## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2024

## Slide 2: Last Time
Temporal and spatial discretization for numerical integration
Forward and Backward Euler (Explicit and Implicit methods)
  explicit can be sensitive to the timestep size
  implicit are harder to implement, but more stable for stiff problems
Finite difference, volume, and element
  all three are used in fuel performance codes and have strengths/weaknesses
  FD is fast, but works on a grid and is discrete
  FE is most flexible, continuous, utilized in MOOSE
Started into mechanics with concept of elasticity

## Slide 3: Mechanics

## Slide 4: Solid mechanics
When a load is applied to a body, it changes shape and perhaps size
Motions throughout a body are called displacements
  u(r, t)
Rigid body displacements do not change the shape and/or size
  the rigid body is translated
Changes in shape and/or size are call deformations
The objective of Solid Mechanics is to relate loads (applied force) to deformation

## Slide 5: Ideal springs
It can be instructive to view solids as a spring
When we apply some force F, we get some displacement x
  F = k x
When the spring is displaced by x, there is force that responds in the opposite direction equal to kx
Due to the displacement, there is a stored energy E = ½ k x2

## Slide 6: Observed deformation due to a force
Solid mechanics is similar to the behavior of an ideal spring but throughout a body
An applied load results results in deformation.
The internal strain is like the displacements x
The internal stress is like the internal force F

## Slide 7: Elasticity
Elasticity is the ability of a body to resist a distorting influence and to return to its original size and shape when that influence or force is removed
In elastic deformation, we are stretching the atomic bonds
The more we stretch the bonds, the more force it takes to stretch
When we release the load, the atoms spring back into their lattice sites

## Slide 8: Plasticity
Plasticity is the ability of a solid material to undergo permanent deformation, a non-reversible change of shape in response to applied forces
Plastic deformation is observed in most materials
The transition from elastic behavior to plastic behavior is known as yielding

## Slide 9: Plasticity
Plasticity is typically caused by two modes of deformation in the crystal lattice: slip and twinning
  Slip is a shear deformation which moves the atoms through many interatomic distances relative to their initial positions
  Twinning is the plastic deformation which takes place along two planes due to a set of applied
Ductility (total elongation), Yield Strength, etc. are dependent upon temperature and composition
Plasticity typically increases at higher temperature

## Slide 10: Stress
Stress is a physical quantity that expresses the internal forces that neighboring particles of a continuous material exert on each other
Stress is a force per unit area with SI units of Pa = N/m2
The stress is a 2nd order tensor (a 3 by 3 matrix): Cauchy stress tensor
σij = Fij/Ai
  i is the face the force is applied and j is the direction it is applied
Sigmas are normal stress components, taus are shear stress components

## Slide 11: Stress as a response
The stress in a material is the RESPONSE to an applied load (force) or an applied displacement
Uniaxial tension or compression
  Only one non-zero stress: σii (σ11, σ22, σ33)
  Tension means positive stress, compression negative
  Examples: Cables, tension tests
Pure shear
  Only one non-zero stress: (σ12, σ13, σ23)
  Examples: drive shaft
Biaxial tension/compression
  Two non-zero stress (e.g. σ11 = 1, σ22 = 2)
  Examples: Pressure cylinder or vessel
Hydrostatic compression (pressure)
  σ11 = σ22 = σ33 = -p
  Anything underwater

## Slide 12: Strain
Strain is a geometrical measure of deformation representing the relative displacement between particles in a material body
The strain in a tensile test is the deformation divided by a representative length
This is engineering strain, but strain can also be defined as “true strain,” accounts for shrinking of section area and the effect of developed elongation on further elongation
Strain is a second order tensor, like the stress
  Let u be a vector of the displacements
  The small strain tensor is
The common strain states are the same as the stress (uniaxial tension, etc.)

## Slide 13: Strain produces stress
A deformation (strain) results in stress within a material
For small strains, the stress is elastic and is a linear function of the strain
For larger deformation, some of the strain is elastic and increases the stress. The rest is plastic and does NOT contribute to the stress.
The elastic energy density in a material is a scalar quantity equal to

## Slide 14: Tensile testing
The most common means of determining mechanical properties is a uniaxial tension test
Apply a uniaxial load until failure
Properties that are directly measured via a tensile test include ultimate tensile strength, maximum elongation, etc., which can be utilized to determine Young’s modulus, Poisson’s ratio, etc.

## Slide 15: Stress/strain from a tensile test
A0 = Initial cross section area
A = deformed cross section area
P or F applied load/force
Engineering True
stress s
strain e

## Slide 16: Stress vs strain curves

## Slide 17: Using stress/strain curves
In the elastic portion of the stress-strain curve, the stress varies linearly with strain
The slope of the line is Young’s Modulus, E:
Poisson’s ratio, ν, is the ratio of the shrinkage in cross section due to the extension in the pulling direction
Can obtain the shear modulus from the elastic modulus and Poisson’s ratio

## Slide 18: Using stress/strain curves
The shear modulus, G, defines the stress to strain ratio in shear
For isotropic materials, G = E / ( 2 (1 + ν))
In matrix form, the elasticity/stiffness tensor from Hooke's law for isotropic materials can be written as

## Slide 19: Isotropic and Anisotropic
Being a linear mapping between the nine numbers σij and the nine numbers εkl, the stiffness tensor c is represented by a matrix of 3 × 3 × 3 × 3 = 81 real numbers
Given minor symmetries of the stiffness tensor, cijkl = cjikl, this 81 elastic constants can be reduced to 36
Major symmetries, cijkl = cklij, reduce this number from 36 to 21
Isotropic materials deform the same way no matter in what direction you deform them.
  They have 2 unique elastic constants, C11 and C12
Anisotropic materials behave differently in different directions
  The elasticity tensor can have 21 unique components defining anisotropy
  Orthotropic materials have 9 unique elastic constants
  Cubic structured materials have 3 unique elastic constants (UO2)
  Hexagonal structured materials have 5 unique elastic constants
Polycrystalline anisotropic materials can behave as isotropic, because the various grains average out

## Slide 20: Isotropic elastic constants for some materials
Material | E (GPa) | n
Aluminum | 70.3 | 0.345
Gold | 78.0 | 0.44
Iron | 211.4 | 0.293
Nickel | 199.5 | 0.312
Tungsten | 411.0 | 0.28
Zircaloy | 80.0 | 0.41
UO2 | 200.0 | 0.345

## Slide 21: Elastic constants are not “constant”
Properties change with temperature
Softening can be referred to as the decrease in elastic constants with temperature
Young’s modulus is typically a function of temperature, decreasing with increasing temperature
Shear Modulus and Poisson’s ratio can also change with T

## Slide 22: In actual materials, the stress and the strain change throughout the material

## Slide 23: von Mises yield criterion
The maximum distortion criterion (also von Mises yield criterion) states that yielding of a ductile material begins when the second invariant of deviatoric stress (J2) reaches a critical value
A material is said to start yielding when the von Mises stress reaches the yield strength
The von Mises stress satisfies the property where two stress states with equal distortion energy have an equal von Mises stress
The von Mises stress is used to predict yielding of materials under complex loading from the results of uniaxial tensile tests

## Slide 24: Stress/Strain Regions
Once the stress reaches the yield stress, it plastically deforms
σy is the yield stress
σU is the ultimate tensile stress
The final stress before rupture is called the fracture stress

## Slide 25: Permanent Strain
After plastic deformation, if you unload the sample, it still has the permanent strain
The plastic behavior has modified the microstructure, and has increases the yield point
After unloading, the strain hardening has changed the material
Thus, if you reload, the yield strain is often higher than it was previously

## Slide 26: The hardening behavior changes for different materials
K is a strength coefficient, n is the strain hardening exponent, e0 is the prior plastic strain, ep is the plastic strain, and sy is the yield strength
The strain hardening exponent is a material property, with a value between 0 and 1
A value of 0 means that a material is a perfectly plastic solid, while a value of 1 represents a 100% elastic solid.

## Slide 27: Dislocation motion
Plastic deformation occurs due to dislocation motion
A dislocation is a line defect
  Edge and screw type
When it moves, only a small number of bonds are broken at a time

## Slide 28: Dislocation are produced during deformation

## Slide 29: Dislocation motion causes plastic deformation, dislocation pileup causes hardening

## Slide 30: Dislocation Pile Up
Dislocation motion can be inhibited by barriers, including grain boundaries, precipitates, voids, bubbles, etc.

## Slide 31: Ductility
Ductile materials plastically deform significantly, brittle materials do not
Quantities defining ductility are total percent elongation at fracture (%EL) and the percent reduction in area (%RA)
The ductile–brittle transition temperature (DBTT) of a metal is the temperature at which the fracture energy passes below a predetermined value
Below the DBTT, failure is brittle
Cold working and neutron irradiation can increase the DBTT, potentially reducing ductility of reactor components

## Slide 32: As the strength increases due to dislocation pile-up, the ductility decreases
Toughness is the ability of a material to absorb energy and plastically deform without fracturing
Toughness is related to the area under the stress–strain curve
In order to be tough, a material must be both strong and ductile
Materials are often work hardened prior to utilization to modify mechanical properties

## Slide 33: Summary
Solid mechanics predicts the deformation of a body from its applied load
The strain defines the deformation
The stress defines the material’s response to the strain
Materials can have recoverable and permanent deformation
  Elastic deformation is recoverable and occurs due to the stretching of the atomic lattice
  Plastic deformation is permanent and results form the breaking of bonds
Elastic moduli and Elastic constants