## Slide 1: NE 795-014: Advanced Reactor Materials
Fall 2023
Dr. Benjamin Beeler

## Slide 2: Last Time
Finished TRISO
Exam next time
Let me know if you have questions

## Slide 3: Sodium Cooled fast reactors

## Slide 4: Sodium Cooled Fast Reactors (SFRs)
Two main families:
  Liquid metal cooled reactor, which utilizes MOX fuel
  Integral fast reactor, which utilizes metallic fuel
SFRs are designed for management of high-level wastes and management of plutonium and other actinides
Important safety features of the system include a long thermal response time, a large margin to coolant boiling, a primary system that operates near atmospheric pressure, etc.

## Slide 5: SFRs
Pool vs Loop
  In the pool type, the primary coolant is entirely contained in the main reactor vessel, which therefore includes not only the reactor core but also a heat exchanger (US EBR-2, French Phenix)
  In the loop type, the heat exchangers are external to the reactor tank (French Rapsodie, BN-350)

## Slide 6: SFRs
Currently operating SFRs:
  BN-600 (Russia), BN-800 (Russia), CEFR (China), FBTR (India), Joyo (Japan)
Benefits of liquid metal coolants:
  metals atoms are weak neutron moderators, allowing for fast neutron spectrum
  sodium melts at 371K and boils at 1156K, a total temperature range of 785K between solid and gas states, whereas water is only 100K at atmospheric pressure
  boiling temperature is well above operational temperatures
  sodium is non-corrosive, compatible with metallic fuel
  sodium has higher thermal conductivity than water
Drawbacks:
  sodium catches on fire in air, reacting with water to form hydrogen gas
  requires special precautions to prevent and suppress fires and limit sodium leaks

## Slide 7: History of SFRs
Sodium-cooled fast reactors were among the first to be designed, built, and operated
EBR-I
  ANL-W, INL
  Startup in Dec. 1950
  The world’s first breeder reactor
  Demonstrated the ability to breed fuel
  Utilized metallic fuel and NaK coolant

## Slide 8: Key SFRs in the US
EBR-II (1965-1994)
  Purpose was to demonstrate a complete breeder-reactor power plant with on-site reprocessing of solid metallic fuel
  It demonstrated its ability to self-cool its fuel through natural convection of the sodium coolant during the decay heat period following the shutdown
FFTF (1980-1992)
  Operated as a national research facility to test various aspects of commercial reactor design and operation, especially relating to breeder reactors
Large portions of current knowledge on metal fuel and fast flux environment derive from these reactors

## Slide 9: Increased Safety
Metal fuel has excellent transient capabilities
The metal fuel itself does not impose any restrictions on transient operations or load-following capabilities
The robustness of metal fuel is illustrated by the following sample history of a typical driver fuel irradiated during the EBR-II inherent passive safety tests conducted in 1986:
40 start-ups and shutdowns
5 15% overpower transients
3 60% overpower transients
45 loss-of-flow (LOF) and loss-of-heat-sink tests including a LOF test from 100% power without scram

## Slide 10: Increased Safety
Metal fuel also has benign run beyond cladding breach (RBCB) performance characteristics
After 150+ days of operation with a cladding breach, metallic fuel retained shaped and did not exacerbate the breach
oxide
metal
oxide

## Slide 11: Inherent Safety
Although the metal fuel melting temperature is much lower than that of oxide fuel, it is also much more difficult to raise the fuel temperature because of the 10X higher thermal conductivity
Thus, operating margins in terms of power can, in fact, be greater for the metal core than for oxide
The high thermal conductivity and the thermal inertia of the large sodium pool can shut the reactor down during very severe accident situations, without depending on human intervention
One experiment in EBR II (LOFWS) simulated station blackout, combined with loss of emergency power supply, failure of primary and secondary shutdown systems, and no operator action – a worst case
The rising coolant temperature during accident causes thermal expansion of the core components which enhances the neutron leakages and hence slowing down the chain reaction
Due to this negative reactivity feedback, the reactor power is shut down all by itself and the coolant temperature rise stops

## Slide 12: Summary of SFR Usage

## Slide 13: Metal fuel

## Slide 14: First Metal Fuels
Starting in the late 1940s, metallic fuels dominated the early development of nuclear reactors because of their key attributes of high fissile-atom density and good thermal conductivity
Alloys of U, Pu were of interest, and alloys with Th were pursued to increase thermal conductivity
Initial experiments with pure U metal met with spectacular swelling and growth, as observed in the mid 1950s

## Slide 15: Alpha U
The most important irradiation characteristic of α-U is its dimensional instability in the form of anisotropic growth and swelling, which results from the anisotropy of the orthorhombic crystal structure
In addition to anisotropic thermal expansion, irradiation growth occurs anisotropically
The current theory of this phenomenon is that fission-generated interstitials and vacancies form loops on {010} and {110} planes, respectively, as a result of the anisotropic thermal expansion induced in α-U by thermal spikes in displacement cascades

## Slide 16: Alpha U Swelling
The temperature dependence of the irradiation growth process takes on a bell-shaped form, due to recombination of point defects
In a polycrystalline sample, irradiation growth in individual grains results in shape changes and mismatched strains between the individual grains
The stress developed due to these mismatched strains can be released by plastic deformation at the grain boundaries; this is commonly referred to as tearing or cavitation
Cavitation swelling dominates between 400 and 600 C

## Slide 17: Alpha U Swelling
Lower temperature regime cavitation swelling results in a swirled microstructure, with irregular cavities formed by tearing of grain boundaries
At higher temperatures (500-600 C), the cavities along the grain boundaries can be crystallographically aligned, and are potentially related to twinning
Cavitation can be reduced by minor additions of alloying elements, which can serve to affect the defect evolution in the system

## Slide 18: Swelling in Gamma U
Swelling in the higher temperature phases occurs primarily by growth of fission gas bubbles, and is isotropic
All phases will also have solid fission product swelling
Fission gas is effectively insoluble in metallic U, and thus prefers to precipitate
Sufficiently large bubbles can maintain an equilibrium gas pressure by balancing the surface tension and the external pressure
This growth is described by the Young-Laplace equation
The external pressure is determined by the plastic flow characteristics of the fuel surrounding the bubble and the mechanical restraint of the cladding
Fission gas swelling can be substantial, and must be accounted for

## Slide 19: Alloying to modify properties
As with alpha U, small alloying additions were explored to limit the fission gas swelling behavior
Adjusted U – U alloyed with small amounts of Al, Fe, or Si
Additions form precipitates and act as point defect sinks, limiting swelling for low burnups
U-Fissium contained Mo-Ru, with lesser amounts of Rh, Pd, Zr, and Nb, and was the early EBR II fuel
Higher content alloys have focused on elements that form extensive solid solutions with U in the high-temperature γ-phase, specifically Mo, Zr, Ti, and Nb
These elements lower the temperature of the cubic γ-phase boundary, allowing more of the fuel to operate in the isotropic γ-phase; they also increase the solidus temperature, raising the margins at which the fuel melts
The addition of Zr and Mo seem to most substantially reduce the swelling of metallic U and low T and low burnup

## Slide 20: Accommodation of Swelling
With high-content alloys, calculations of fuel swelling and gas release showed that if 30-40% free volume was afforded inside the cladding, fuel could swell, and when it contacted the cladding, allowing for mechanical strength of cladding to counteract further radial swelling
It was found that the majority of fission gas is released by about 30% swelling, and by including a large plenum, stresses on cladding could be reduced

## Slide 21: Metal Fuel
Metal fuels are ideal for fast reactors because they have higher densities of fissile and fertile materials and provide higher breeding ratio
The burnup of metal fuel in the early days was limited to a few atom percent (at.%) because of the increase in the fuel–cladding mechanical interaction (FCMI) caused by gas swelling of fuel alloys
Reducing the fuel smear density to about 75% is effective in promoting fission gas release before fuel-cladding contact and in suppressing FCMI

## Slide 22: Base Metal Fuel System
The typical metallic fuel consists of a U(Pu)–10 wt% Zr fuel slug with ~75% smear density
The cylindrical fuel alloy rod is called a ‘fuel slug
The annular gap between the fuel slug and the cladding is filled with sodium (bond sodium)
A relatively large gas plenum (1-1.5x fuel length), which is a space above the fuel slug, is provided to mitigate the pressure of the fission gas accumulating during irradiation

## Slide 23: Closing the Fuel Cycle
An important factor in selecting a fuel form for fast reactors is ease of fuel recycling, including reprocessing and fuel refabrication
Pyrometallurgical processing, called ‘melt refining,’ can be combined with refining techniques to recycle spent metallic fuel
This recycling process has been demonstrated for uranium alloy fuels in the 1960s, where fuel alloys were recycled as many as four times, and the fuel was returned to the reactor within 4–6 weeks of its removal from the reactor core
Will talk more about this later

## Slide 24: The U-Zr System
Metallic uranium is alloyed with Zr to stabilize the bcc phase, increase the melting point, improve mechanical properties, and reduce swelling
Typical composition is 10 wt.%, or approximately 23 atom %
At relevant temperature ranges in SFRs, multiple phases will be present

## Slide 25: U-Pu-Zr
Ternary phase diagram isotherms
g: Body-centered cubic (bcc), has complete solid solubility for bcc e-plutonium and bcc b-zirconium
a: Orthorhombic allotropic modification of uranium that dissolves up to 15 at.% of plutonium, but has limited solubility for zirconium
b: Tetragonal allotropic modification of uranium that dissolves up to 20 at.% of plutonium, but has limited solubility for zirconium
h: A high-temperature intermediate phase in the U–Pu binary system that is believed to be tetragonal and has limited solubility for zirconium
z: A complex cubic U–Pu intermediate phase that dissolves up to 5 at.% zirconium
d: A hexagonal intermediate phase in the U–Zr system that occurs approximately at the composition UZr2 and has extensive solid solubility for plutonium

## Slide 26: U-Pu-Zr
The U-Pu-Zr system was the fuel choice for the Integral Fast Reactor design of the 1980s, and the current Versatile Test Reactor design
U-Pu-Zr alloys are the most recent alloys under active exploration, and thus have the most recent experimental data

## Slide 27: U-Pu-Zr Swelling
Swelling is typical of metallic fuels, in that it occurs rapidly, leveling off once in contact with the cladding
Fission gas release occurs within the first 5% burnup, corresponding with the rapid swelling
These fuels swell less in the axial direction than in the radial direction, if isotropic swelling is assumed

## Slide 28: U-Pu-Zr Swelling
The is believed to be due to the difference in swelling behavior between the hotter center of the fuel pin and the colder periphery
The gamma phase dominates in the center of the fuel pin at high temperatures
This phase has large gas bubbles, indicative of a higher plasticity of the fuel and, therefore, a lower capability to sustain shear stresses
gamma

## Slide 29: U-Pu-Zr Swelling
The alpha phase dominates on the colder periphery of the fuel pin, and has smaller, textured porosity
The alpha phase is known to have higher strength, and is assumed to be less plastic than gamma
The fission gas pressure in the center would can potentially result in a near-biaxial loading of the peripheral shell, the radial stress component being twice the axial component
A stress effect on swelling in the peripheral fuel zone would result in a larger radial strain, and hence anisotropic swelling
alpha

## Slide 30: U-Pu-Zr
An increase in the Pu content exacerbates the anisotropic swelling
This is believed to be driven by the redistribution of Zr along the temperature gradient of the fuel